## Slide 1: Simulating Real-Time Electron Impact Ionization Within the CEBAF Photo-gun Using a General Particle Tracer (GPT) Custom Element
J. T. Yoskowitz, J. Grames, C. Hernandez-Garcia, G. A. Krafft, G. Palacios-Serrano, M. Poelker, M. L. Stutzman, R. Suleiman, S. B. van der Geer, S. Wijethunga
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under contract DE-AC05-06OR23177.
LA-UR-23-30859

## Slide 2: Outline
Background and Motivation
Biased Anode Experiments
Ion Back-Bombardment Modelling with GPT
Conclusions & Ongoing Work

## Slide 3: Ion Back-Bombardment
Photocathode charge lifetime is determined by ion back-bombardment.
GaAs photocathodes, used to create polarized electron beams, are particularly susceptible to ion back-bombardment.
Charge lifetime: amount of charge extracted before QE falls to 1/e (~37%) of the initial value.
Initial QE
Charge Extracted
Charge Lifetime
Anode
e-beam
Cathode
Ions
Ions
6 cm Gap
Photocathode
Grounded Anode
Photocathode QE vs Charge Extracted

## Slide 4: Biasing the Anode
Biasing the anode with a positive voltage repels ions downstream of the anode, increasing charge lifetime.
Higher charge lifetime  higher current in the same amount of time, or same current for longer time.
Developed a realistic model to explain the charge lifetime improvement with the biased anode.
Anode
e-beam
Cathode
Ions
Ions
6 cm Gap
Photocathode
Biased Anode
Grounded Anode
Biased Anode
Photocathode QE vs Charge Extracted

## Slide 5: CEBAF Photo-gun
HV Cable
Gun Chamber
Anode Bias Feedthrough
E-Beam Direction
Cathode Electrode
HV Cable
Anode Electrode
Triple-Point Junction Shield
Support Tube
Gun Chamber
Photocathode
E-Beam Direction
Ceramic Spacers
Beam Pipe
6 cm Gap
Laser Direction
Inverted Insulator

## Slide 6: Grounded vs Biased Anode Configurations
Cathode: -130 kV
Grounded anode: 0 V
Biased anode: +1000 V
  Peak: ~ 350 V at 8 cm
Anode
Photocathode
Anode
Photocathode
Electric Potential On Axis
Electric Potential On Axis
(Zoomed in)

## Slide 7: Biased Anode Experiments
Experiments took place parasitically to three run periods at the CEBAF accelerator.
Anode alternated between grounded and biased configurations (RP1 and RP2).
Daily QE measurements to track degradation and calculate charge lifetime.
Periodic QE scans to measure spatial degradation.
 | Run Period 1 | Run Period 2 | Run Period 3
Dates | June 2019 – Sept 2019 (12 weeks) | Jan 2020 – Mar 2020 (11 weeks) | July 2020 – Sept 2020 (11 weeks)
Lasers/halls used | A, B, C | A, B, C, D | A, B, C, D
Total charge extracted | 245 C | 390 C | 247 C
Total beam current | 50 – 100 μA | 150 – 225 μA | 150 – 225 μA
Rep Rate | 499 MHz | 499 MHz | 499 MHz
Initial bunch size | 0.5 mm (rms) | 0.5 mm (rms) | 0.5 mm (rms)
Bunch length | 50 ps (rms) | 50 ps (rms) | 50 ps (rms)
Cathode bias | -130 kV | -130 kV | -130 kV
Anode bias | 0 V or 961 V | 0 V, 961 V, or 1000 V | 1000 V
 | Run Period 1 | Run Period 2 | Run Period 3
Dates |  |  | 
Lasers/halls used | A, B, C | A, B, C, D | A, B, C, D
Total charge extracted | 245 C | 390 C | 247 C
Total beam current | 50 – 100 μA | 150 – 225 μA | 150 – 225 μA
Rep Rate | 499 MHz | 499 MHz | 499 MHz
Initial bunch size | 0.5 mm (rms) | 0.5 mm (rms) | 0.5 mm (rms)
Bunch length | 50 ps (rms) | 50 ps (rms) | 50 ps (rms)
Cathode bias | -130 kV | -130 kV | -130 kV
Anode bias | 0 V or 961 V | 0 V, 961 V, or 1000 V | 1000 V

## Slide 8: QE Measurements
QE measurements measure the QE at the laser spot on the photocathode.
Laser spot shifted in run period 2 when the QE was too low.
Run Period 1
Run Period 2
Laser Spot 1
Laser Spot 2
Run Period 3

## Slide 9: Charge Lifetime and Improvement Ratios
Charge lifetime improved by on average with anode biased.
Interestingly, charge lifetimes for a given anode bias change throughout each run period.
Run Period | Anode Bias (V) | Charge Lifetime (C)
1 | 0 961 0 961 | 181 ± 8 424 ± 53 288 ± 39 303 ± 18
2 | 0 961 961 0 1000 | 85.9 ± 0.1 211 ± 9 401 ± 10 208 ± 4 370 ± 29
3 | 1000 | 350 ± 14
Charge Lifetime Table
Run Period | Improvement Ratio | Ratio Value
1 |  | 
2 |  | 
Run Period | Improvement Ratio | Ratio Value
1 |  | 
2 |  | 
Improvement Ratios
Average Improvement Ratio

## Slide 10: QE Scan
Series of QE measurements in a gridded pattern.
X/Y stepper motor moves laser spot.
Interpolate measurements to generate QE contour plot.
Compare successive scans to visualize QE degradation.
Red Circle: Photocathode Active Area, 5 mm diameter
Green Circle: Laser Spot, 2 mm diameter
Raw Data
QE Scan

## Slide 11: QE Scans: Run Period 1
Laser spot position: (-1.0 mm, -1.0 mm)
Time elapsed between scans: 111 days
Charge extracted between scans: 245.7 C
Red Circle: Active Area Green Circle: Laser Area
1 (Initial)
2 (Final)
2 - 1

## Slide 12: QE Scans: Run Period 2
Laser spot #1 : (-0.78 mm, 0 mm)
Laser spot #2: (1.63 mm, 0.57 mm)
Total time elapsed: 81 days
Total charge extracted: 404 C
QE Scans
Note: Scans are not correlated with bias or laser spot
QE Difference Scans
2
1
2-1
3
4
5
3-2
4-3
5-4
5-1

## Slide 13: QE Scans: Run Period 3
Laser spot position: (0.88 mm, 0.59 mm)
Time elapsed between scans: 81 days
Charge extracted between scans: 241 C
Red Circle: Active Area Green Circle: Laser Area
1 (Initial)
2 (Final)
2 - 1

## Slide 14: General Particle Tracer (GPT) Simulations with IONATOR
GPT is a particle tracking code.
Created the C++ custom element IONATOR to model electron impact ionization.
Features:
  Implements cross sections using Monte Carlo algorithms.
  Includes prevalent residual gases: H2, He, CO, CH4.
  User-defined gas densities and temperatures.
  Generates ionization statistics (particle energies, momenta, ionization cross sections) in a separate output file.

## Slide 15: IONATOR Flow Chart
The number of ions each macro-particle creates in a time step is given by
Gas density
Ionization cross section
Distance travelled in time step
Number of electrons per macro-particle
Monte Carlo algorithm ensures ionization simulations are probabilistic, instead of deterministic.

## Slide 16: Ion Production Rate
Ion Production Rate Per Unit Length
= Gas density (m-3)
= Ionization cross section (m2)
= Distance traveled by electron (m)
= Electron current (A)
= Elementary charge (C)
Example Calculations for H2 Gas
Electron Energy | IPR per length
Electron Energy | IPR per length
Assuming and
Ion Production Rate Per Unit Length

## Slide 17: Modelling the CEBAF Beamline
Created GPT simulations for each anode bias configuration in each run period.
Single electron bunch is tracked to a viewer 1.54 m away from photocathode.
Used a CST 3D electric field map of the CEBAF photo-gun.
Used GPT field maps for magnetic elements.

## Slide 18: Grounded vs Biased Anode Simulations
Parameter | Value
# Macro Particles | 
Total Bunch Charge | mC
Bunch Length | 50 ps (rms)
Transverse Diameter | 2 mm
Cathode Voltage | - kV
Anode voltage | 0 V (grounded) +1 kV (biased)
H2 density | m-3 ( Torr)
Simulation Region | m
Simulation Stages | ns , ns s
Parameter | Value
# Macro Particles | 
Total Bunch Charge | 
Bunch Length | 50 ps (rms)
Transverse Diameter | 2 mm
Cathode Voltage | 
Anode voltage | 0 V (grounded) +1 kV (biased)
H2 density | 
Simulation Region | 
Simulation Stages | 
Grounded Anode Simulation
Biased Anode Simulation
Anode
Photocathode
Primary Electron
Ion
Secondary Electron
Scattered Electron

## Slide 19: Back-Bombarding Ion Density Distributions: Grounded vs. Biased Anode (Run Period 1)
Grounded Anode (0 V)
Biased Anode (961 V)
Upstream of Anode
Downstream of Anode
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
(Scatter Plot)

## Slide 20: Back-Bombarding Ion Energy Density Distributions: Grounded vs. Biased Anode (Run Period 1)
Grounded Anode (0 V)
Biased Anode (961 V)
Upstream of Anode
Downstream of Anode
X (mm)
Y (mm)
Ion Energy Density (eV/mm2)
X (mm)
Y (mm)
X (mm)
Y (mm)
X (mm)
Y (mm)
(Scatter Plot)
Ion Energy Density (eV/mm2)
Ion Energy Density (eV/mm2)

## Slide 21: Back-Bombarding Ion Distributions vs QE Difference Scan
Run Period 1
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
Ion Energy Density
Ion Density
Ion Energy
Density (eV/mm2)
QE Difference Scan
Run Period 2
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
Ion Energy
Density (eV/mm2)
Run Period 3
X (mm)
Y (mm)
Ion Density (mm-2)
X (mm)
Y (mm)
Ion Energy
Density (eV/mm2)

## Slide 22: Conclusions
Biasing the anode increases the charge lifetime of the CEBAF photo-gun by 1.80±0.51.
Created IONATOR to model electron-impact ionization and simulate ion back-bombardment.
Back-bombarding ions created upstream of the anode are concentrated at the laser spots.
Back-bombarding ions created downstream of the anode are spread out over the active area.
Biasing the anode repels the vast majority of ions created downstream of the anode.
Back-bombarding ion distribution patterns correlate to the QE degradation patterns in all three run periods.

## Slide 23: Ongoing Work
Currently using IONATOR to predict ion back-bombardment for the 200 kV CEBAF photo-gun.
Determining how ion damage mechanisms (sputtering, implantation, etc.) contribute to QE degradation.
Studying time-dependence of charge lifetime improvement.

## Slide 24
jty@lanl.gov
J. T. Yoskowitz, J. Grames, C. Hernandez-Garcia, G. A. Krafft, G. Palacios-Serrano, M. Poelker, M. L. Stutzman, R. Suleiman, S. B. van der Geer, S. Wijethunga

## Slide 25
Backup Slides

## Slide 26
Photoemission and Quantum Efficiency
Photo-guns produce electron beams via photoemission.
Photoemission is described as a three-step process1:
  Photons excite electrons in the photocathode.
  Electrons diffuse through the material; some reach the surface.
  Electrons overcome electron affinity and escape the photocathode.
Quantum efficiency (QE): Ratio of # photo-emitted electrons to # incident photons.
1 W. E. Spicer, “Photoemissive, photoconductive, and optical absorption studies of alkali-antimony compounds”, Phys. Rev., vol. 112, pp. 114–122, Oct. 1958, doi:10.1103/PhysRev.112.114
1
e-
2
e-
3
Incident Photon
Photocathode
Photo-emitted Electron
e-
Excited Electron
Beam Current
Laser Power
Laser Wavelength

## Slide 27
CEBAF Polarized Electron Source Beamline
PHOTOCATHODE PREPARATION CHAMBER
SOLENOID
STEERING COILS
PHOTO-GUN VACUUM CHAMBER
BEAM POSITION MONITORS
DIPOLE MAGNET
BEAMLINE VALVE
VIEWER
BEAM POSITION MONITORS
STEERING COILS
STEERING COILS
BEAM POSITION MONITORS
(VIEWER)
FARADAY CUP
LASER

## Slide 28: Electron-Impact Ionization
A primary electron scatters off a target particle and ejects an electron.
The target particle becomes a positive ion.
The ejected electron is called the secondary electron.
The primary electron scatters away and is called the scattered electron.
The primary electron must overcome the ionization (binding) energy of the target particle.
Both the secondary electron and scattered electron can continue to ionize, provided they have sufficient kinetic energy.
+
+
-
-
-
-
Shell electron

## Slide 29: Ionization Cross Section
Probability of ionization given by the ionization cross section2:
  : Primary electron kinetic energy
  : Ionization energy
  : Relativistic factors
  : Ion-specific parameters
Low energy electrons are more likely to ionize.
Ionization Cross Section
Electron Energy | Ionization Cross Section (H2)
Electron Energy | Ionization Cross Section (H2)

## Slide 30: Ion Production Rate
= Gas density (m-3)
= Ionization cross section (m2)
= Distance traveled by electron (m)
= Electron current (A)
= Elementary charge (C)
Ion Production Rate Per Unit Length
Ion Production Rate Per Unit Length
Example Calculations for H2 Gas
Electron Energy | IPR per length
Electron Energy | IPR per length
Assuming and

## Slide 31: Secondary Electron Energy Distribution
In the Binary Encounter Dipole Model3, the distribution of possible secondary electron energies is given by the differential cross section:
  : Primary electron energy
  : Secondary electron energy
  : Ionization energy
  : Average electron energy in a subshell
  : Number of electrons in a subshell
  : Differential oscillator strength
Secondary electrons are likely to have low energy compared to the scattered electron.
Secondary Electron Differential Cross Section

## Slide 32: Ion and Scattered Electron Energies
The distribution of speeds of an ideal gas with temperature is given by the Maxwell-Boltzmann distribution (38 meV at 293 K):
The parameters of the scattered electron can be calculated from conservation of momentum and energy.
Maxwell-Boltzmann Distribution
(

## Slide 33: Laser Profile Measurements
Four 780 nm lasers (A, B, C, D) illuminate the photocathode.
Transverse intensity profiles were measured using a CCD camera and analyzed using BeamGage software5.
Laser diameter is ().
Laser | A | B | C | D
-diameter (mm) | 2.14 | 2.23 | 2.05 | 2.84
-diameter (mm) | 1.97 | 2.15 | 2.02 | 2.38
Laser | A | B | C | D
 | 2.14 | 2.23 | 2.05 | 2.84
 | 1.97 | 2.15 | 2.02 | 2.38
Laser Diameters (4
(Assume 2% uncertainty)

## Slide 34: Effect of Anode Bias on Electron Beam
  Beam deflection: Compare transverse beam positions using BPM’s.
  Beam size: Compare transverse beam size using viewers.
  Time of flight: Compare time of flight using RF chopper cavities.

## Slide 35: Beam Deflection vs Anode Bias
Used first two BPM’s to measure transverse beam position vs anode bias.
Predicted a mm total displacement at BPM #2 with 1000 V anode bias.
Measured mm total displacement at BPM #2 with 1000 V anode bias.
Can easily correct for displacement with steering coils.
Relative Beam Deflection vs. Anode Bias

## Slide 36: Beam Size vs Anode Bias
Relative Beam Size vs. Anode Bias
Used three viewers to measure transverse beam size vs anode bias.
Expect small change in beam size due to anode behaving as an electrostatic lens.
Resolution of CCD camera is μm/px
Beam size decreased by px ( μm) on viewer #2 with 1000 V anode bias.

## Slide 37: Time of Flight vs Anode Bias
RF Chopper Scans vs. Anode Bias
Took chopper scans across one slit to measure time of flight vs anode bias.
Slit width: at MHz.
Fit each set of chopper scan data with Gaussian function to determine phase of peak current.
Anode bias increases beam energy  shorter time of flight  positive phase shift.
Peak phase difference between 0 V and 1000 V is (499 MHz).
A
C
B