## Slide 1: Spin-Dependent Fifth-Force Search and Measurement of Compensated Ferrimagnetism in Terbium Iron Garnet using Neutron Spin Echo Spectroscopy and Neutron Radiography
INDIANA UNIVERSITY BLOOMINGTON
Caleb Hughes
Notes: Talk today about work we've done with neutrons and a candidate spin-source material that we hope to use to put lmits on exotic spin dependent potentials

## Slide 2: Open Questions
Search for Physics Beyond the Standard Model:
Spin-Dependent Fifth-Forces1,2
Characterize electron spin samples for other spin-dependent exotic force searches
Internal B fields in a compensated ferrimagnet near TC for the first time
Caleb Hughes
McGowan, A. (2021) 2021 was a big year for physics: We finally peeked beyond the standard model, TNW | Science. Available at: https://thenextweb.com/news/physics-beyond-standard-model-syndication (Accessed: April 14, 2023). Image: Daniel Dominguez/CERN
1. Dobrescu, B. A. & Mocioiu, I. Spin-Dependent Macroscopic Forces from New Particle Exchange. J. High Energy Phys. 2006, 005–005 (2006).
2. Leslie, T. M., Weisman, E., Khatiwada, R. & Long, J. C. Prospects for electron spin-dependent short-range force experiments with rare earth iron garnet test masses. Phys. Rev. D 89, 114022 (2014).
Notes: _ SM a success but leaves unanswered questions: dark matter, baryon asymmetry, etc
Some proposed particles result in predictions of spin dependent forces BSM
We search for these signatures
Have materials with polarizable electron spins
Goal was to further characterize those samples and better understand the ferrimagnetism that makes these ideal materials
Also a first investigation of internal b fields ….
search for possible exotic spin-dependent neutron electron interactions, including momentum-dependent interactions
Point: we want to search for signatures of new force carriers by direct force detection, mention that Thomas has the details., axion like particles
Part of goal of nuclear physics group is indirect detection of new particles by fifth-force detection
Some Solutions:
- Detection of Decay Products
- High Precision Measurements
- High Energy Measurements
- Force Measurements

## Slide 3: Spin-Dependent Potentials1,2,3
Caleb Hughes
S = 0 m ≥ 0
S =1 m > 0
S =1 m = 0
Fadeev, P. et al. Revisiting spin-dependent forces mediated by new bosons: Potentials in the coordinate-space representation for macroscopic- and atomic-scale experiments. Phys. Rev. A 99, 022113 (2019).
Dobrescu, B. A. & Mocioiu, I. Spin-Dependent Macroscopic Forces from New Particle Exchange. J. High Energy Phys. 2006, 005–005 (2006).
Moody, J. & Wilczek, F. New macroscopic forces? Phys. Rev. D 30, 130–138 (1984).
Notes: - Following foundational work of Moody and Wilczek as well as expansion by Dobrescu and Mociou, Fadeev et al derive 9 non-relativistic, Lorentz Invariant potentials from the Lagrangians shown (spin-0 boson, massive spin-1 boson, massless spin-1 boson), arranged based on combinations of coupling types: s and p, V and A, T and PT
Which potentials are we sensitive to? Asssume from Thomas' talk, but get more info for sure

## Slide 4: Spin-Dependent Potentials1,2,3
Caleb Hughes
S = 0 m ≥ 0
S =1 m > 0
S =1 m = 0
Notes: - Following foundational work of Moody and Wilczek as well as expansion by Dobrescu and Mociou, Fadeev et al derive 9 non-relativistic, Lorentz Invariant potentials from the Lagrangians shown (spin-0 boson, massive spin-1 boson, massless spin-1 boson), arranged based on combinations of coupling types: s and p, V and A, T and PT
Which potentials are we sensitive to? Asssume from Thomas' talk, but get more info for sure

## Slide 5: Constraint Examples
S. Hoedl et al., PRL 106 041801 (2011)
W. Terrano et al., PRL 115 201801 (2015)
[astro] G. Raffelt PRD 86, 015001 (2012)
[axion] R. J. Crewther, et al., Phys. Lett. B91, 487 (1980);
C. Baker, et al., Phys. Rev. Lett. 97, 131801 (2006)
Caleb Hughes
Notes: CITE GRENOBE
CITE DOBRESCU AND MOCIOIU
V_1 is spin-independent Yukawa interaction
Here, juxtapose 16 spin-dependant potential forms and source-mass/test-mass combinations for testing (may take a few slides, try and match at least 4 to a slide and will need to move through these somewhat quickly)
May only do spin-dependant ones here with axial polarization, save in-plane polarizations for later section

## Slide 6: Rare-Earth Iron Garnets (RIG)
Ferrimagnets of the form where R is Dy, Tb, Gd ,Yb, Ho, Er
Temperature dependent orbital compensation of magnetism associated with spin
Below room temperature but accessible with LN2 (Dy, Tb)
G. Dionne, Magnetic Oxides (N.Y., Springer, 2009)
Caleb Hughes
Notes: Replace with photo of tbig

## Slide 7: Orbital Compensation
Arrows are magnetic moments of each sublattice, iron in white and rare-earth in orange
Rare-Earth moment responds more strongly to T around TC
At TC, drops to 0
m1
m2
mTotal
m1
m2
T1 < T0
mTotal
m1
m2
mTotal = 0
TC < T1
T0
Caleb Hughes
Notes: make clear it is orbital compensation of magnetization associated with the Fe spins.

## Slide 8: Orbital Compensation
m1
m2
mTotal
sTotal
m1
m2
T1 < T0
mTotal
sTotal
m1
m2
mTotal = 0
sTotal
TC < T1
Arrows are magnetic moments of each sublattice, iron in white and rare-earth in orange
Rare-Earth moment responds more strongly to T around TC
At TC, drops to 0 but net-spin non-zero due to L
Caleb Hughes
T0
Notes: "...(theoretically) drops to zero."
this helps emphasize one of the motivations for our work: does it really happen microscopically?
Both lattices “contribute” to spin; more precisely Fe contribution is positive but Tb contribution is negative. But Tb spin magnitude is less, so spin cancellation is partial.

## Slide 9: What Beams Available/ What Techniques?
Successful preliminary tests at IU
Need higher flux….
Neutron Spin Echo Technique
NSE Spectrometer: BL-15 at Oak Ridge Spallation Neutron Source
Caleb Hughes
Neutron Sciences Directorate (no date) Neutron Spin Echo Spectrometer | Neutron Science at ORNL. Available at: https://neutrons.ornl.gov/nse (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 10: Neutron Spin Echo Technique
Start with polarized ensemble of neutrons
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 11: Neutron Spin Echo Technique
Polarized Ensemble
Induce non-adiabatic spin flip via π/2 coil
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 12: Neutron Spin Echo Technique
Polarized
π/2 spin flip
Precession: Guide field allows Larmor Precession proportional to ω*t. Slower neutrons spend longer time in the field and thus rotate more.
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 13: Neutron Spin Echo Technique
Polarized
π/2 spin flip
Larmor Precession 1
Induce non-adiabatic π-flip of spins.
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: About a different, orthogonal axis than pi/2 flip

## Slide 14: Neutron Spin Echo Technique
Polarized
π/2 spin flip
Larmor Precession 1
π spin flip
Precession: Guide field allows spins to Larmor precess back to original position
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 15: Neutron Spin Echo Technique
Polarized
π/2 spin flip
Larmor Precession 1
π spin flip
Larmor Precession 2
Echo: Spins realign
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Make clear no sample here

## Slide 16: Neutron Spin Echo Technique
Caleb Hughes
Spin echo (2023) Wikipedia. Wikimedia Foundation. Available at: https://en.wikipedia.org/wiki/Spin_echo (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 17: NSE Advantages
Works over a range of wavelengths
Sample can cause change to echo
Useful for RIG Ferrimagnets as a high B-resolution check of internal domain strength
Caleb Hughes
Proton Dynamics in Oxides: An Insight into the Mechanics of Proton Conduction from Quasielastic Neutron Scattering - Scientific Figure on ResearchGate. Available from: https://www.researchgate.net/figure/a-The-layout-of-a-generic-spin-echo-spectrometer-showing-its-principal-components-b_fig3_306254786 [accessed 15 Apr, 2023]
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 18: BL-15 NSE Setup
Sample in vacuum in small continuous-flow cryostat
Temperature control: two silicon diode thermometers, resistive heater in feedback loop: 30 mK accuracy typical
External field sensors: two fluxgate magnetometers flanking cryostat, Hall probe attached to sample on axis.
Caleb Hughes
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 19: Sample Mounting
Caleb Hughes
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 20: Measurements
Compensation Temperature
Transmission
Pi Coil Off
Small Q
Fifth-Force Search Trial Run
Caleb Hughes
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 21: Compensation Temperature
Hall probe directly above sample
Tc (Hall sensor): (251.34 +/- 0.85) K
Fluxgates outside cryostat
Tc (fluxgate sensor): (251.02 +/- 0.62) K
Two lakeshore temperature sensors
Caleb Hughes

## Slide 22: Compensation Temperature
Hall probe directly above sample
Tc (Hall sensor): (251.34 +/- 0.85) K
Fluxgates outside cryostat
Tc (fluxgate sensor): (251.02 +/- 0.62) K
Two lakeshore temperature sensors
Caleb Hughes

## Slide 23: Transmission Mode
Caleb Hughes
π/2 Flipper
Precession
coil
π flipper
Sample
Precession
Coil
π/2 flipper
Analyzer
Detector
S
Neutron Travel
T = 243 K
T = TC
Notes: No decoherence
Top left: neutron spectrum
Top right: Atari plot, shows wavelength vs. current. Current is current of phase coil, which is swept to determine maxima and minima, which correspond to the heat map. An echo has occurred when you get a vertical line, i.e. maximum independent of wavelength
Bottom Left: ???? 30 pixel x 30 pixel intensity plot?
Bottomr right: Counts as a function of phase current?
Although capable of rotating the instrument, we operated mostly in “transmission” mode

## Slide 24: Paramagnetic Scattering: Pi Coil Off
Caleb Hughes
π/2 Flipper
Precession
coil
π flipper
Sample
Precession
Coil
π/2 flipper
Analyzer
Detector
S
Neutron Travel
T = 230 K
T = TC
Notes: Spin flip scattering goes away at Tc
Chatterji page 531, (See Mike’s Email) (Chapter 11, Section 4)
Discuss paramagnetic scattering: only magnetic field componenet perpendicular to q scatters; canted angle of magnetic moments? Check low q to confirm
No evidence in phase current amplitude plot

## Slide 25: Low Q
Caleb Hughes
π/2 Flipper
Precession
coil
π flipper
Sample
Precession
Coil
π/2 flipper
Analyzer
Detector
S
Neutron Travel
T = 230 K
T = 230 K
Notes: For similar integration time, get much, much worse (implies not small q scattering, i.e. more likely a canted spin angle than misalignment of polarization axis?)

## Slide 26: Spin-Dependent Fifth-Force Search
Caleb Hughes
π/2 Flipper
Precession
coil
π flipper
Sample
Precession
Coil
π/2 flipper
Analyzer
Detector
S
Neutron Travel
T = TC
T = TC
S
Notes: Explicitly say why reversed direction

## Slide 27: Sayonara, SNS : Hello, HFIR
Caleb Hughes
 | SNS | HFIR
Number of Instruments | 20 | 13
Instrument Used | BL-15 (NSE) | MARS (Imaging)
Notes: https://commons.wikimedia.org/wiki/File:Spallation_neutron_source_logo.png
https://neutrons.ornl.gov/nse

## Slide 28: MARS
Multimodal Advanced Radiography Station (MARS)
HFIR beamline CG-1D
Radiography and computed tomography imaging capabilities
High spatial resolution, lower B field sensitivity
Use radiography to quantify n spin rotation
Caleb Hughes
Notes: Camera info? More specifics? L/D?
https://www.frontiersin.org/articles/10.3389/fenrg.2022.1102466/full
https://www.frontiersin.org/articles/10.3389/fceng.2022.1046627/full

## Slide 29: Magnetic Shielding
No ambient shielding in instrument area
Design Constraints:
4:1 length:diameter
Fits around cryostat
Doesn’t interrupt n travel
Minimized opening size
Shielding reduces field to acceptable levels
Caleb Hughes

## Slide 30: Samples
Reused main sample used in NSE experiment
Safety considerations
Redesigned holder for single sample
Caleb Hughes
Notes: How much to say here? May work better as a bullet point, or perhaps mention alternative samples, lack of need for repolarization, challenges etc.

## Slide 31: Neutron Flight Path
Caleb Hughes
Graphic by Krystyna Lopez
Notes: Credit K. Lopze for image

## Slide 32: Neutron Beam
Caleb Hughes
Notes: Credit K. Lopze for image

## Slide 33: Polarization
Caleb Hughes
Notes: SM = Super mirror

## Slide 34: Spin Transport
Guide Field elements maintain polarization in the direction of n travel
Field of ~100 G
Caleb Hughes

## Slide 35: Spin Manipulation
Beam collimated
Neutrons pass through sample and spin rotate
Exit to V-Coil
(sudden rotation via current sheet)
Exit to longitudinal coil
Adiabatic rotation
Caleb Hughes

## Slide 36: Spin Analyzer
Caleb Hughes

## Slide 37: Neutron Imaging
Caleb Hughes

## Slide 38: Measurement Strategy
Asymmetry measurement: spin-up vs. Spin-down
Coil current flipped
DATA SETS:
Ferrimagnetics checked by sweeping through temperatures
Fifth-Force data collected by 180 degree rotation
Caleb Hughes
Notes: Resolution? Built in? Maybe make a bullet point

## Slide 39: Temperature Sweep Data
Reversal of signal through Tc
Caleb Hughes
Image from Krystyna Lopez
Notes: What about domain level cancellation effects? What would we expect through a nonmagnetic material?

## Slide 40: HFIR Future
Proposal submitted for HFIR 2024-A run cycle
Improved magnetometry
Improved thermometry
Improved statistics
Order of Magnitude bound improvement
Caleb Hughes
Notes: Discuss upgrades for Gen 2 experiment (see dissertation)

## Slide 41
Questions?
This work supported by NSF grants
PHY-1707986 and PHY-2209481
Thanks!
Caleb Hughes
This work supported by DOE grant
DE-SC0010443
Collaboration
Indiana University:
Caleb Hughes, Lili Lommel, Krystyna Lopez, Mike Snow,
Michael van Meter
University of Illinois Urbana-Champaign:
Josh Long
Georgia State University:
Thomas Mulkey, Murad Sarsour
ORNL:
SNS:
Matt Frost, Mary Odom, Piotr Zolnierczuk
HFIR:
Peter Jiang, Erik Stringfellow, Yuxuan Zhang
Notes: Include lab photos, shed photos here

## Slide 42: Why Terbium?
Easily accessible Tc (~250 K)
TbIG has ½x spin density of DyIG, but 0.1x neutron absorption cross section
Novel
Caleb Hughes
G. Dionne, Magnetic Oxides (N.Y., Springer, 2009)
Notes: Need to test.

## Slide 43: It Works! (Externally…)
MPMS Squid Magnetometer
Tc = 253 +/- 1 K
Now we just need an internal probe…..
Caleb Hughes
Notes: Make sure to mention the plot is remnant magnetization of TbIG (that is, permanent magnetization of magnetized sample, with field removed) as a function temperature. There are several passes through Tc over (presumably) several hours, no degradation of room temperature magnetization, Tc very repeatable, etc.

## Slide 44: Neutrons as a Probe
Electrically Neutral
Non-destructive
Readily polarized spin
Low decoherence in matter
Caleb Hughes
Basics of neutron scattering (no date) Basics of neutron scattering - eneutrons. Available at: https://e-learning.pan-training.eu/wiki/index.php/Basics_of_neutron_scattering (Accessed: April 14, 2023).
Notes: Mention domain size?

## Slide 45: SANS
Tested samples for small-angle neutron scattering (SANS) using IU’s Low-Energy Neutron Source (LENS)
Multiple cycles through Tc; no change
No significant SANS as a function of T
Caleb Hughes
Instruments (no date) Center for Exploration of Energy & Matter. Available at: https://ceem.indiana.edu/lens/instruments/index.html (Accessed: April 14, 2023).
Notes: Checked (and improved) phase purity of the sample (add graphic if time)

## Slide 46: Ferrimagnets
Ferrimagnets exhibit anti-aligned sub-moments which contribute to a net moment
Temperature dependance of RIG ferrimagnets leads to cancelling of the net magnetic moment
Global or local?
Caleb Hughes
Libretexts (2021) 6.8: Ferro-, ferri- and Antiferromagnetism, Chemistry LibreTexts. Libretexts. Available at: https://chem.libretexts.org/Bookshelves/Inorganic_Chemistry/Book%3A_Introduction_to_Inorganic_Chemistry_%28Wikibook%29/06%3A_Metals_and_Alloys-_Structure_Bonding_Electronic_and_Magnetic_Properties/6.08%3A_Ferro-_Ferri-_and_Antiferromagnetism (Accessed: April 14, 2023).
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 47: Spin-Dependent Potentials1,2,3
“Static” spin-spin interactions
Velocity-dependent spin-spin interactions
Spin-Mass interactions
72 Independent couplings
[1] J. E. Moody and F. Wilczek, Phys. Rev. D 30, 130 (1984)
[2] B. Dobrescu and I. Mocioiu, J. High Energy Phys. 0611, 005 (2006) [3] Fadeev, Pavel, et al. Phys. Rev. A, vol. 99, no. 2 , doi: 10.1103/physreva.99.022113(2019)
Caleb Hughes
Notes: In this slide, Highlight potentials to be modified, maybe even show their contact terms, split?
CITE GRENOBE
CITE DOBRESCU AND MOCIOIU
V_1 is spin-independent Yukawa interaction
Here, juxtapose 16 spin-dependant potential forms and source-mass/test-mass combinations for testing (may take a few slides, try and match at least 4 to a slide and will need to move through these somewhat quickly)
May only do spin-dependant ones here with axial polarization, save in-plane polarizations for later section
Which depend on Spin-0 boson? Highlight them
Among those, V3 is the so-called dipole-dipole potential
The so-called monopole-dipole potential is given by V9 + V10.

## Slide 48: Neutron Spin Orientation
Caleb Hughes
Slide by Krystyna Lopez

## Slide 49: Field Integral
Caleb Hughes
Accuracy 100nTm
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 50: NSE Analysis
Preliminary Analysis Observable:
D(theta)/lamda dz = 6.18 +/- 0.114 rad/Angstrom m
Corresponds to a ~100 microT field
Caleb Hughes
I- = 0.5095 A
I- = 0.5095 A
I+ = 0.4621 A
I+ = 0.4621 A
I+ = 0.4621 A
I+ = 0.4621 A
Analysis by Thomas Mulkey (GSU)

## Slide 51: TEMPLATE
Hall probe directly above sample
Tc (Hall sensor): (251.34 +/- 0.85) K
Fluxgates outside cryostat
Tc (fluxgate sensor): (251.02 +/- 0.62) K
Two lakeshore temperature sensors
Caleb Hughes

## Slide 52: Calibration
Adjusted cryostat PID parameters
Leveled system wrt beam
Tested vacuum system
Caleb Hughes
Notes: What calibrations were done? Checked the Hall probe, but ended up not needing that data. What did we calibrate before we had neutrons on target? Review logbook for this info.

## Slide 53: Spin-Dependent Fifth-Force
Caleb Hughes
π/2 Flipper
Precession
coil
π flipper
Sample
Precession
Coil
π/2 flipper
Analyzer
Detector
S
Neutron Travel
Notes: Include Walt’s design here
Have to replace Bell Jar
Wires coated for higher emissivity

## Slide 54: INTENTIONALLY BLANK
T = 240 K
T = 251 K
T = 260 K

## Slide 55: INTENTIONALLY BLANK
T = 240 K
T = 251 K
T = 260 K
T = 261 K
T = 241 K
T = 250.5 K
Spin up
Spin up
Spin up
Spin down
Spin down
Spin down

## Slide 56: Analysis (NSE Compensation Temp)
T = 230 K
Allow Sample to Flip neutron Spins
Retain Echo (noisier, longer integration)
R = 2.75 * 10^3 +/- 6.46
Caleb Hughes
Notes: Want to be able to explain this– probalistic process, less efficient than coil driven flips
Explain R

## Slide 57: Analysis (NSE Compensation Temp)
T = 240 K
Interference Pattern Blurring
Decrease in signal amplitude
R = 48.4 +/- 0.402
Caleb Hughes
Notes: Want to be able to explain this– probalistic process, less efficient than coil driven flips

## Slide 58: Analysis (NSE Compensation Temp)
T = 251 K (Tc)
Interference Pattern Gone
Near Elimination of signal amplitude
R = 0.539 +/- 0.113
Caleb Hughes
Notes: Want to be able to explain this– probalistic process, less efficient than coil driven flips

## Slide 59: Analysis (NSE Compensation Temp)
T = 260 K
Interference Pattern Returning
Oscillations Returning
R = 19.4 +/- 0.179
Caleb Hughes
Notes: Want to be able to explain this– probalistic process, less efficient than coil driven flips

## Slide 60: Analysis (NSE Compensation Temp)
T = 270 K
Interference Pattern Clear
Oscillations Clear
R = -653 +/- 1.7
Caleb Hughes
Notes: Want to be able to explain this– probalistic process, less efficient than coil driven flips

## Slide 61: Spin-Dependent Potentials1,2,3
“Static” spin-spin interactions
Velocity-dependent spin-spin interactions
Spin-Mass interactions
72 Independent couplings
[1] J. E. Moody and F. Wilczek, Phys. Rev. D 30, 130 (1984)
[2] B. Dobrescu and I. Mocioiu, J. High Energy Phys. 0611, 005 (2006) [3] Fadeev, Pavel, et al. Phys. Rev. A, vol. 99, no. 2 , doi: 10.1103/physreva.99.022113(2019)
Caleb Hughes
Notes: Furthering the work of Moody and Wilczek, Dobrescu and Mocioiu lay out 16 potentials
Reread paper

## Slide 62: Spin-Dependent Potentials1,2,3
“Static” spin-spin interactions
Velocity-dependent spin-spin interactions
Spin-Mass interactions
72 Independent couplings
[1] J. E. Moody and F. Wilczek, Phys. Rev. D 30, 130 (1984)
[2] B. Dobrescu and I. Mocioiu, J. High Energy Phys. 0611, 005 (2006) [3] Fadeev, Pavel, et al. Phys. Rev. A, vol. 99, no. 2 , doi: 10.1103/physreva.99.022113(2019)
UNDER REVIEW
Caleb Hughes
Notes: In this slide, Highlight potentials to be modified, maybe even show their contact terms, split?
CITE GRENOBE
CITE DOBRESCU AND MOCIOIU
V_1 is spin-independent Yukawa interaction
Here, juxtapose 16 spin-dependant potential forms and source-mass/test-mass combinations for testing (may take a few slides, try and match at least 4 to a slide and will need to move through these somewhat quickly)
May only do spin-dependant ones here with axial polarization, save in-plane polarizations for later section
Which depend on Spin-0 boson? Highlight them
Among those, V3 is the so-called dipole-dipole potential
The so-called monopole-dipole potential is given by V9 + V10.