## Slide 1: Slim Edge for LGADs
October 20th 2023
Gabriele Giacomini
EIC-Related Generic Detector R&D Proposal Review Meeting

## Slide 2
Explain in more detail the designs of the edges.
Answers to reviewers’ questions - 1
Modified termination:
(several variants will be designed):
- termination down to 1 floating guard Ring
- shrinking (or elimination) of grounded GR
- Substrate contact smaller and closer
trench
Pad contact
GND Guard Ring
Substrate contact
Termination
cutline
800 um
Standard termination,
even for a 20um thick substrate
Active area
Guard Ring
Trench will go here
50um

## Slide 3
Is simulation supporting your choices?
Answers to reviewers’ questions - 2
Yes, a great deal of TCAD simulations was already carried out by a SULI student this summer (J. Duncan, U, Memphis).
Depletion region hardly extend beyond one GR which is within 50 um from grounded area, even at high voltages.
50um thick substrate
Region equipotential with back
(200V)
Diode @ GND
Back @ -200V
20um thick substrate
Region equipotential with back
(80V)

## Slide 4
What designs won’t be implemented between 100% and 60% financing?
The 4” wafers will be populated with many different designs, to push the limits of the different technologies.
The wafers will have a common lithographic mask set, so all designs that we can think of will be implemented.
However, the number of techniques that will be explored to have slim edges will be reduced accordingly.
100% : KOH etch w and w/o alumina deposition, RIE w and w/o alumina deposition, DRIE, …
60%: no DRIE or other ideas which will mature during the projects
Answers to reviewers’ questions - 3

## Slide 5
Why do you not include DRIE (Deep Reactive Ion Etching) in the program? Such a machine may not be available at BNL but they are widely available at University fabs. Inclusion would make the project more complete.
Answers to reviewers’ questions - 4
Although we don’t have experience in DRIE, we can certainly profit from this project to gain some.
DRIE will require – beside the facility – a furnace for boron diffusion (not a BNL either, but we are users of, for example, Cornell Nanoscale Facility https://www.cnf.cornell.edu/ - so the process can be carried out at Cornell), and PECVD filling to planarize the surface and allow several other lithographies (contact opening, metal, passivation opening).
It is certainly a very elegant and working solution, but it takes some effort (need 100% of funding).
[1] L. Pancheri et al 2016 JINST 11 C12018, https://iopscience.iop.org/article/10.1088/1748-0221/11/12/C12018

## Slide 6
What lithography is needed after the trench etch? Can it be the last step?
Yes, passivation opening will be the last step.
To resist the KOH attack, a layer of nitride (~ 100nm – already tested) will be deposited. Then we have to open the nitride in the pads area, for testing and contacting. This requires litho.
Answers to reviewers’ questions - 5
P+ CZ wafer
P- epitaxial layer
nitride
P+ CZ wafer
P- epitaxial layer
nitride
P+ CZ wafer
P- epitaxial layer
Example of process

## Slide 7
What guard ring geometry do you plan to use? How much space does it take?
In the wafer, there will be placed many design variants, however we’ll focus on few GRs, closely spaced, order of ~ 50um or less.
TCAD simulations suggests that, if the substrate is thin, GRs are hardly biased at all.
Measurements on test structures tell that 1 GR is enough to sustain very high voltage.
Answers to reviewers’ questions - 6
Chart: Leakage Current vs Voltage for 20 Micron Substrate – 1 Guard Ring only
TCAD and I-V by J. Duncan, U. Memphis, SULI 2023
20 um thick substrate.
Back at 80V
GR stays at ~ 60V.

## Slide 8
Can the trench be used to isolate the backside from the front so that the front side is at ground potential?
Answers to reviewers’ questions - 7
60mm
Not in the present plan: both the substrate and the epitaxial active layer are p-type.
The voltage applied to the back propagate to the front side because of:
  the etched/diced wall of the scribeline/trench due to defects
  by the hole accumulation layer induced by the alumina passivation layer.
  by the undepleted region at the border (equipotential to the back).
  at the top surface, at the edge of the device, a p+ layer terminate the surface and is equipotential to the back.
Undepleted region
P+ implant
Defects or alumina layer
Map of the electrostatic potential
Pad @ GND

## Slide 9
Project description

## Slide 10
Standard Termination for silicon sensors
Strip sensor on 300-um thick substrate
Pad contact
GND Guard Ring
Substrate contact
Termination
cutline
800 um
Low-Gain Avalanche Diode on 20um thick
HPK not that different
Scribeline/Cutline placed at 3x (substrate thickness) to avoid depletion region touching defect-full cut.
 1mm from active area
While LGADs are built on thin substrates, the 1mm “rule-of-thumb” is present in all devices by all manufacturers.
Can we cut-down the distance?

## Slide 11
Active edge
If cutline are “passivated”, defects are shut down and they do not act as generation center  no leakage current even if depletion region extends up to the cutline
Depletion region must stay away from the defect-full scribeline, or a large current injected into the device.
The standard way to passivate is by etching a vertical trench
(Deep Reactive Ion Etching – DRIE) and doping.

## Slide 12
Trench etching by DRIE
Classical method, used for a few PS/HEP experiments
on thick wafers (~ 500 – 100 um )
R&D at FBK(Trento , Italy) towards ATLAS IBL, M Povoli et al 2013 JINST 8 C11022
L. Pancheri et al 2016 JINST 11 C12018
For XFEL

## Slide 13
Why go with Slim Edge?
When tiling sensors, dead areas appear w/o slim edges
Powder diffraction experiment
Slim edges for:
Minimize dead areas
Facilitating tiling
Smaller devices for the same Fill Factor
  (particularly critical for LGADs, which suffer from low yield)

## Slide 14
Case for thin substrates
In thin (20-50um thick) substrates, depletion region extends ~ 50um, as space is needed to allocate the GR (lithographic constrains).
In the undepleted region, a cutline can be placed.
No need of any treatment (to be tested)?
Most likely, need to produce a clean cut and passivation.
Active area
Floating GR
Undepleted substrate
70 um
DRIE is the standard option (known to work) but other means may be good enough to achieve the same result.

## Slide 15
Trench etching
Chemical etching (KOH)
+ alumina passivation
RIE silicon etching
  proved to be enough for thin substrates.
Cleaving, laser dicing, …
Passivation of Atomic Layer Deposition of aluminum oxide available at BNL.
Used to induce a hole accumulation layer at the Si/AlO interface.

## Slide 16
Fabrication
Current-voltage at the probe station for basic functionality
Transient Current Technique to assure charge collection efficiency.
Testing
All fabrication carried out in class-100 clean room at BNL, except for:
  nitride/alumina deposition (CFN at BNL)
  DRIE + boron diffusion – if funds allow – at Cornell
  Ion implantation
4” wafer populated with a large number of (small area, ~ mm2) test structures, differing for number of Guard Rings, distance from the scribeline, termination structure, trench etching method, …

## Slide 17
Budget
one year project
100% budget is 130k (overhead included),
mainly labor (2 weeks PI, 1 month clean-rom engineer, 2 months tech)
  80-60% scenario:
    work reduced accordingly to fit the budget
    less exploration of slim edge techniques
month 1-2: production of photolithographic masks and definition of the clean-room process
month 3-4: silicon substrates ready for trench etching
month 5-6. first wafers completed with trenches
month 7. static characterization of device and next plans laid down
month 8-9. Deliverables: method #2 for trench etching/passivation
month 10. static characterization of device
month 11 -12. additional methods for trenching, reports/papers.