## Slide 1: A high intensity polarized beam photogun for the Ce+BAF positron source
Towards 5X the beam current of the state-of-the-art CEBAF photogun
Carlos Hernandez-Garcia for the Ce+BAF team
6 in
CEBAF
130 keV
polarized
GTS
300 keV un-polarized
Prototype
500 kV
Positron Working Group Workshop ,Washington, DC, March 18-20, 2024

## Slide 2: Designing a 1 mA polarized photogun as beam driver for positron production
Two challenging injectors have to be built considering two high risk R&D areas
High current polarized e-source > 1 mA
High power e+ conversion target.
(Andriy Ushakov)
e+ beam to CEBAF
Polarized e- injector > 120 MeV
> 100 kW target & cw-collection beam line

## Slide 3: A photogun generating 1 mA CW beam will produce:
  86 C in a day
  600 C in a week
  2400 C in a month
Consequently the photocathode 1/e charge lifetime should be >1 kC, meaning the photogun can operate:
for ~ one month without intervention or
for a few weeks at a time at even higher beam current levels

## Slide 4: What does a photogun need to provide for generating > 1 mA CW polarized beam?
  High polarization photocathodes with high QE > 1%
  Vacuum chamber with total Pressure < 1e-12 Torr
  High Voltage
  Long 1/e charge lifetime t > 1000 C

## Slide 5: CEBAF polarized e- source @ 1 mA?
Gun2 Photocathode (Fall 2016 – Spring 2017)
QE = QE0 e -(Q/Lifetime)
Gun vacuum ~ 1x10-12 Torr
Lifetime ~200 C (s4D ~ 1mm, I~200 mA)
[µA]
We have demonstrated polarization from the CEBAF PES remains steady up to 1 mA/499 MHz
The charge lifetime (at 0.2 mA) is about 200 C
This would provide only 2-3 days of positrons
High polarization at 1 mA
Slide by J. Grames

## Slide 6: CEBAF lifetime improvement with biased anode (GaAs/GaAsP)
With a >400 C lifetime we could operate at 1 mA for almost 1 week
Improving charge lifetime of CEBAF photogun
Ions downstream of the anode are repelled back towards the beamline by the positive anode potential
J. T. Yoskowitz et al., 12th Int. Particle Acc. Conf. IPAC2021, Campinas, SP, Brazil, doi:10.18429/JACoW-IPAC2021-WEPAB104
Slide by J. Grames

## Slide 7: Developing polarized photocathodes with > 1% QE (DOE NP FOA LAB 20-2310)
B. Belfore et al., Appl. Phys. Lett. 123, 222102 (2023); doi: 10.1063/5.0170106
Graph courtesy M. Stutzman (JLab)
Graph courtesy S. Marsillac (ODU)
  MOCVD
  GaAs/GaAsP-DBR
  ~ 90% pol, ~ 2% QE
JLAB-ODU-BNL
780 nm
780 nm
  Strained Super Lattice
  GaAs/GaAsP
  ~ 85% pol, ~0.3% QE
CEBAF
  CBE/MBE
  GaAs/GaAs/P
  InGaAs/InAlGaAs
  ~85% pol, ~ 1% QE
JLAB-UCSB
780 nm

## Slide 8: GaAs/GaAsP charge lifetime at milliamp current
J. Grames, P. Adderley, J. Hansknecht, R. Kazimi, M. Poelker, D. Moser, M. Stutzman, S. Zhang, “Milliampere beam studies using high polarization photocathodes at the CEBAF Photoinjector” Polarized Sources, Targets and Polarimeters Workshop, Dajeon South Korea (2017)
Days
Results from PSTP’17 suggests increasing laser spot size is viable to exceed >500 C lifetime; however we need to build another gun to test this assertion.
CEBAF (<1 mm2)
4𝜎 ~ 1 mm
Trend we want to realize
4𝜎 ~ 10 mm
Test performed with un-biased anode

## Slide 9: Larger size electrodes are needed for large size laser spot on photocathode
CEBAF photocathode puck
Prototype photocathode puck
The Cornell photogun demonstrated up to 65 mA CW non-polarized beam from a ~ 4 mm diameter laser spot
B. Dunham et al., APPLIED PHYSICS LETTERS 102, 034105 (2013)
CEBAF electrode
Cornell electrode
12 in
6 in

## Slide 10: Polarized electron source for Ce+BAF
We want to deliver > 1 mA for weeks on end…
Two weeks @ 1 mA ≈ 1 kC
By increasing the laser size and biasing the anode charge lifetimes of 1 kC might be possible
CEBAF
anode biasing
Gun Charge in 2 weeks [Coulombs]
Gun Current to make positrons [mA]
Ce+BAF
large laser size
Slide by J. Grames
Improving vacuum

## Slide 11: Improving photogun extreme high vacuum conditions
Pump down “ultimate pressure” setup
Low carbon steel exhibits VERY low hydrogen outgassing rate. Our measurements consistent with those of Park et.al.,
Chongdo Park, Taekyun Ha and Boklae Cho, "Thermal outgassing rates of low-carbon steels," J. Vac. Sci. Technol. A 34, 021601 (2016); https://doi.org/10.1116/1.4936840
Test stand to measure hydrogen outgassing rate
Slide courtesy M. Poelker
CEBAF photogun
316 stainless steel
R&D
low carbon steel
CEBAF photogun vacuum chamber after 400 C heat treatment

## Slide 12: What else does a photogun need to provide for generating > 1 mA CW polarized beam?
  High Voltage
  Low limit
  Photocathode surface charge limit
  Space charge within the electron bunch
  High limit
  Field emission
  Minimum energy required for beam capture by the MeV SRF booster
  Commercial supply chain challenges manufacturing compact conical insulators
  High voltage power supply ($0.5 M, needs SF6)
  High voltage commercial components operational limits
CEBAF photogun performance
130 kV, no field emission
~0.2 mA CW from 4𝜎 ~ 1 mm laser spot
~ 85% polarization beam injected to 0.5 MeV capture RF cavity
JLab FEL photogun performance
350 kV, some field emission
10 mA CW from 4𝜎 ~ 8 mm laser spot
Non-polarized beam injected to 10 MeV SRF booster

## Slide 13: Addressing the high voltage limit for a 1 mA polarized photogun
Field emission free operation:
  Requires ~ 100 kV higher than operating voltage for field emission high voltage processing
Minimum gun voltage for beam capture by SRF booster:
  200 – 300 kV
There is no conical insulator capable of > 400 kV
  A compact, conical insulator is instrumental in the photogun design to minimize vacuum chamber volume and area
  A large insulator is required also for supporting larger electrodes
JLab demonstrated (2023) 500 kV using a very large, custom inverted insulator with SF6 intervening volume mating to a modified HV cable receptacle
  This proof of principle is not directly applicable to a photogun design
There is no cable that fits this insulator
C. Hernandez-Garcia, Positron Working Group Workshop, March 18-20, 2024
SF6 intervening layer
Funded through: NP FOA LAB 20-2310
18 in

## Slide 14: In 2023 we received a DOE HEP U.S.-Japan (FOA LAB 23-2858) grant to develop a 500 kV insulator fitting commercial HV cables
Electrostatic models in CST are being developed
The electrostatic potential simulations of the insulator will be used for designing a test electrode
500 kV insulator prototype model
Chart: Curve length [cm]
Commercial HV cable rated to 400 kV

## Slide 15: Progress on the HEP funded FOA: Initial meeting with industry
Kyocera:
  Understands the opportunity to become a (likely sole) provider for inverted insulators for photoguns
  Willing to develop prototype insulator
  Will provide various material samples of new proprietary material to U. of Tsukuba for HV characterization
We met with Kyocera in September to discuss the design and evaluation of a new 500 kV insulator
KEK, Tsukuba, Japan, Sept. 28th, 2023

## Slide 16: JLab has demonstrated capability to develop and operate high intensity, high polarization photoguns using inverted geometry insulators
16
16
250 kV
R28
375 kV
R30
500 kV
concept
We are ready to develop a prototype high current AND high polarization photogun for
Ce+BAF
CEBAF 130 keV 0.2 mA CW > 80% polarized beam
Gun Test Stand (GTS)
keV, 5 mA CW magnetized beam
CEBAF
GTS
SF6 intervening volume
test
Maximum applied voltage without breakdown
Achieved!