## Slide 1
An Introduction to
Polarized Solid Targets
Chris Keith
Jefferson Lab Target Group
PSTP
2024
Thomas Jefferson National Accelerator Facility

## Slide 2
Outline
Target and Polarization Basics
Dynamic Nuclear Polarization
Polarized Target Equipment
  Target Materials
  Magnets
  Refrigerators
  Microwaves
  NMR
In-beam Behavior
Tensor Polarization & Deuteron NMR Signals
What to Expect this Week

## Slide 3
Luminosity
Luminosity is a measure of the intensity of the beam + target interaction
= # beam particles hitting the target per second
= Avogadro’s number (# nuclei per gram)
= target density (g/cm3)
= target length (cm)
Experiment (location) | Beam s-1 | Target material | Length cm | Luminosity 1035 s-1 cm-2 | Limiting factor
MOLLER (Hall A c. 2026) | 4 x 1014 | Liq. Hydrogen | 125 | 20 000 | Beam power
Typical experiment (Hall A/C) | 2 x 1014 | Liq. Hydrogen | 10 | 1000 | Target boiling
Polarized gas target (Hall C) | 2 x 1014 | 3He | 60 | 20 | Radiation damage
Polarized solid target (Hall C) | 6 x 1011 | NH3 | 3 | 10 | Radiation damage
Polarized solid target (B) | 6 x 1010 | NH3 | 5 | 1 | Detector rates
GlueX (D) (photon beam) | 108 | Liq. Hydrogen | 30 | 0.001 | Tagger rates
Beam current
Target thickness

## Slide 4
Polarization
Polarization is a measure how many target spins are pointing in a specified direction (usually a magnetic field)
= fraction of spins up (down)
= vector polarization
= magnetic dipole moment
= Larmor (resonance) frequency
Magnetic field, z
I
n
For spin-1/2 (protons, electrons, 3He, etc)
Deuterons (spin-1) also have a 2nd type of polarization (more on this later)

## Slide 5
Thermal Equilibrium
The Zeeman interaction lifts the degeneracy of the spins and produces (2I + 1) energy states.
Magnetic field
Energy
0
-1/2
+1/2
h
An oscillating field at the resonance frequency will induce transitions between the states (spin flips)
N+
N-
Left undisturbed, an ensemble of spins will eventually come into thermal equilibrium with its environment and the levels will be populated according to the Boltzmann relation

## Slide 6
Thermal Equilibrium
The spins approach equilibrium in an exponential manner.
The 1/e constant is T1, the spin-lattice relaxation time.
T1 depends on the temperature, field, and sample purity.
Appreciable nuclear polarization requires ultra-low temperatures and high magnetic fields.
PTE, the thermal equilibrium polarization, is given by the Brillouin function
for spin-1/2
Electrons are much more forgiving.
Electrons: short T1
Nuclei: long T1
PTE

## Slide 7
Dynamic Nuclear Polarization
Thermal equilibrium (aka “Brute-Force”) polarization of nuclear requires very high magnetic fields and ultra low temperatures.
Almost all polarized solid targets utilize a different polarization method:
Dynamic Nuclear Polarization (DNP)
  Select an appropriate dielectric solid with the nucleus you want to polarize (usually protons or deuterons)
  Implant it with a low concentration (10-4) of unpaired electron spins (paramagnetic impurities)
  Polarize the electrons at a moderate field and temperature (∼ 5 T/ 1 K)
  Transfer the electron polarization to the nuclei

## Slide 8
Dynamic Nuclear Polarization
Thermal equilibrium (aka “Brute-Force”) polarization of nuclear requires very high magnetic fields and ultra low temperatures.
Almost all polarized solid targets utilize a different method:
Dynamic Nuclear Polarization (DNP)
  Select an appropriate dielectric solid with the nucleus to polarize (eg protons or deuterons)
  Implant it with a low concentration (10-4) of unpaired electron spins (paramagnetic impurities)
  Polarize the electrons at a moderate field and temperature (∼ 5 T/ 1 K)
  Transfer the electron polarization to the nuclei
EXAMPLE
TEMPO-doped butanol
Butanol has 10 free protons
TEMPO has one unpaired electron

## Slide 9
Dynamic Nuclear Polarization
An oscillating field can produce
Electron spin flips at the ESR frequency ne = 28 GHz/ T
Proton spin flips at the NMR frequency np = 42.6 MHz/ T
Double spin flips are “forbidden”
ESR
NMR
Magnetic field, z
Consider an electron – proton “pair” in a strong magnet field
The Zeeman interaction will produce four energy levels
electron
proton

## Slide 10
Dynamic Nuclear Polarization
The dipole-dipole interaction between the two spins mixes the pure spin states
An oscillating field can now produce the “forbidden” transitions where both spins flip
Flip-flips at ne - np
Flip-flops at ne + np
a
b
-
a
b
+
a
b
+
a
b
-
flip-flip
flip-flop
000
000
000
000
r
Magnetic field, z

## Slide 11
Dynamic Nuclear Polarization
Consider a single electron spin surrounded by several protons in a high field at low temperature. (Say, 5 T and 1 K)
The electron is polarized by the field and temperature, but the protons are not.
Microwaves at ne – np induce flip-flip transitions between the electron an a nearby proton
The electron relaxes back to its ground state (T1 ∼ 0.1 s)
The proton does not (T1 > 100 s)

## Slide 12
Dynamic Nuclear Polarization
Consider a single electron spin surrounded by several protons in a high field at low temperature. (Say, 5 T and 1 K)
The electron is polarized by the field and temperature, but the protons are not.
Microwaves at ne – np induce flip-flip transitions between the electron an a nearby proton
Microwaves continue to drive these transitions until all the proton spins are opposite the electron (positive polarization)

## Slide 13
Dynamic Nuclear Polarization
Consider a single electron spin surrounded by several protons in a high field at low temperature. (Say, 5 T and 1 K)
The electron is polarized by the field and temperature, but the protons are not.
Microwaves at ne + np induce flip-flop transitions
and lead to negative polarization.
One unpaired electron can polarize about 104 nuclear spins

## Slide 14
Dynamic Nuclear Polarization
This method of dynamic polarization is called the SOLID EFFECT.
Microwave
absorption
Polarization
ne – np
ne + np
ne
Jeffries (1957)
Abragam and Proctor (1958)
The SE requires a very narrow ESR line and produces a polarization curve with well resolved + and – polarization peaks.
“One electron polarizes one proton, one spin-flip at a time” -cdk
Most modern-day target materials don’t display this behavior, so other “spin-transfer” mechanisms are needed to explain how DNP works.
Cross Effect: “Two electrons polarize one proton.”
Thermal Mixing: “A network of electrons polarizes a network of protons.”
TEMPO + BUTANOL
Microwave
frequency
Microwave
absorption
Polarization
ne – np
ne + np
ne
Microwave
frequency
0
TEMPO

## Slide 15
Polarized Target Equipment
There are five major components to a typical solid polarized target system
  Target sample
  Magnet
  Refrigerator
  Microwaves
  NMR
Superconducting
Magnet
Vacuum Pumps
Refrigerator
Microwaves
NMR
Target Sample
For optimum results, the field-to-temperature ratio should be at least 5:1
Historically this has meant
2.5T & 0.5 K
5T & 1K

## Slide 16
Target Material
DNP target material is characterized by three main quantities:
  Maximum polarization (“Can you make it higher?”)
  Radiation resistance (“Why is the polarization going down?”)
  Dilution Factor, the ratio of polarized to unpolarized nucleons (“What’s all this junk?”)
Material
Dilution Factor (%)
Polarization (%)
Butanol, C4H9OH
13.5
> 90%
Ammonia, NH3
17.7
> 90%
Lithium hydride, 7LiH
25.0
90%
Material
Dilution Factor (%)
Polarization (%)
d-Butanol, C4D9OD
23.8
> 80%
d-Ammonia, ND3
30.0
50%
Lithium deuteride, 6LiD
50.0
55%
Radiation resistance
Comments
moderate
Easy to produce and handle
high
Works well at
5T and 1K
extremely high
Slow polarization,
long relaxation
Chemically doped (eg TEMPO)
Radiolytically doped

## Slide 17
Magnets
Typical polarizing fields for DNP are 2.5 – 5 T, generated by superconducting magnets
We typically aim for a field uniformity of about 100 ppm over the sample volume
In many cases, the structure of the magnet dictates the range of available scattering angles → frozen spin target
COMPASS 2.5 T magnet
Solenoid + correction coils + saddle coils
CLAS12 5 T solenoid
Solenoid + counter windings
JLab 5 T split coil
Pseudo Helmholtz geometry
Rotate for longitudinal or transverse polarization

## Slide 18
Refrigerators
Maximum polarization requires cooling the target sample ≾ 1 K
The only practical forms of refrigeration are the evaporation of 4He (or 3He) and 3He-4He dilution refrigeration
Evaporation Refrigeration
Liquid 4He has a normal boiling point of 4.2 K and a latent heat of vaporization, L = 80 J/mol.
The cooling power is ,
where is the rate of evaporation (mol/s)
The temperature can be lowered by reducing the vapor pressure (pumping), but the pressure (and cooling power) drops rapidly with temperature.
The practical limit is about 1 K.
Vacuum chamber
LHe dewar
Transfer line
Valve
Liquid
Vapor
Target sample
Vacuum pump
Heat exchanger
4.2 K
Superfluid
Below 2.2 K 4He is a superfluid with outstanding thermal conductivity and heat transport.
DNP targets operating at 5 T and 1 K have become the de facto standard for experiments with intense, ionizing beams.
Horizontal 1 K refrigerator for CLAS12 polarized target

## Slide 19
Refrigerators
Maximum polarization requires cooling the target sample ≾ 1 K
The only practical forms of refrigeration are the evaporation of 4He (or 3He) and 3He-4He dilution refrigeration
Dilution Refrigeration
Below 0.8 K a mixture of 3He and 4He will separate into two distinct phases.
The upper phase is mostly 3He (concentrated)
The lower phase is mostly 4He (dilute), but always contains ≥6.6% 3He.
Heat is removed when 3He from the conc. phase dissolves into the dilute phase.
The practical limit is less than 0.01 K.
T2
4He pump
Condenser
Heat exchanger
Heat exchanger
Vacuum chamber
Liquid: >1% 3He
Vapor: <97% 3He
The “still” ~ 0.7 K
Mixing chamber
3He pump
Heater
Frozen Spin Targets
Compared to evaporation refrigerators, “DilFridges” are much more difficult to build and operate.
They are mostly used to cool frozen spin targets for lower-intensity beams and high-acceptance detectors.
Horizontal dilution refrigerator for Hall B frozen spin target

## Slide 20
Frozen Spin Targets
Frozen Spin Targets are used to take advantage of high acceptance detectors (eg Crystal Ball)
Nuclear spin relaxation is strongly temperature dependent and reaches 1000s of hours at ultralow temperatures
Target sample is dynamically polarized in a massive, high-field polarizing magnet
Scattering data is acquired with the sample in a thin, low field holding magnet
Requires cooling sample to milliKelvin temperatures
Beam heating limits beam flux to ∼108 s-1
Polarization
Time
Polarize (+)
High Field
Polarize (-)
High Field
Take beam (+)
Low field
Take beam (-)
Low field
Mainz-Dubna Frozen Spin Target
Holding coils, JLab Frozen Spin Target

## Slide 21
Microwaves
The microwave frequency for DNP is determined by the magnet: 28.02 GHz/T
The microwave power is determined by the field & temperature combination:
  2.5 T & 0.5 K: ∼4 mW/g
  5.0 T & 1 K: ∼100 mW/g
Extended Interaction Oscillator
100 W @ 70 GHz (2.5 T)
20 W @ 140 GHz (5.0 T)
CPI Canada
IMPATT Diode
1 W @ 70 GHz
0.3 W @ 140 GHz
VA Diode, Inc
Microwaves are transmitted thru metal waveguide
Rectangular outside the cryostat
Oversized circular inside
Typical rectangular waveguide losses
70 GHz (WR-12): -2 dB/m
140 GHz (WR-6): -6 dB/m
Measure the microwave power at the target
At 1 K the 4He evaporation rate increases ∼16.8 slpm per watt of power

## Slide 22
NMR
CW-NMR is the standard method to measure the nuclear polarization
A weak RF field, polarized ⟂ to Bo will induce both upward and downward transitions with equal probability as it sweeps through the resonance frequency
The net emission (or absorption) of energy is proportional to (N+ - N-), the polarization
The constant of proportionality can be measured with the microwaves off and the sample at its thermal equilibrium (TE) polarization
Care must be given to not use too strong RF or dwell at the resonance frequency. This can drive the populations to equality (saturation).
Species | Spin | NMR Freq (MHz/T)
1H | ½ | 42.58
2H | 1 | 6.54
3H | ½ | 45.41
3He | ½ | -32.44
6Li | 1 | 6.27
7Li | 3/2 | 16.55
13C | ½ | 10.71
14N | 1 | 3.08
15N | ½ | -4.32
19F | ½ | 40.08
N+
N-
(Emission)
(Absorption)

## Slide 23
NMR
RF Signal
Generator
Reference
Signal
Output
ADC
Phase-Sensitive Detector
Phase-adjust cable
Cryostat
nl/2 cable
NH3 @ Thermal Equilibrium 0.3%
NH3 @ +85%

## Slide 24
In the Beam
Two observable effects of a high intensity beam
Beam Heating
Immediate polarization drop of a few percent
Proportional to volume-to-surface area of the sample
Use numerous mm-sized grains of material immersed in helium coolant
Increase the beam spot on the target sample (or raster the beam)
In a rastered beam, each bead can warm as much as 2-3 K, but cools back to 1 K in milliseconds
Surface
temperature, TS
Liquid helium temperature, TL
Interior
temperature, T(r)

## Slide 25
Radiation Damage
Fresh ⌀2cm target: anneal after 5 x 1015 e-/cm2
  700 hrs @ 1 nA
  70 hrs @ 10 nA
  7 hrs @ 100 nA
Radiation Damage
Slow loss of polarization
Production of radiolytic, paramagnetic impurities (e-, atomic H, etc) reduces T1
Some materials (LiH, NH3) are naturally more radiation resistant than others (butanol, propandiol)
  Increase the beam spot on the target (raster)
  Adjust microwave frequency as dose increases
  Warm (anneal) the sample to ∼100 K to remove unwanted impurities
  Replace the sample after 5-10 anneals

## Slide 26
Radiation Damage
Images from the most recent JLab polarized target experiment:
Run Group C in Hall B
⌀1.5 x 5 cm3 sample container filled with ND3
Beam spot on target
Thermoluminescence during anneal

## Slide 27
Tensor Polarization
We need (2I+1) = 3 numbers to describe the spin populations of the deuteron (spin-1)
Total number of spins
Vector polarization
Tensor polarization (alignment)
If the three levels are populated according to a Maxwell-Boltzmann distribution
(aka ”Spin Temperature”)
In a high-intensity experiment using ND3,
Pmax ≈ 50%
Qmax ≈ 20%
Can we increase the tensor polarization?

## Slide 28
NMR Lineshape of Deuterons
Deuteron has a magnetic dipole moment, m = 4.33 x 10-27 J/T = 0.86 mn
Deuteron also has an electric quadrupole moment, eQ = 2.86 e.fm2
eQ interacts with electric field gradients within the lattice (or molecule) and shifts the energy levels by an amount hnQ
nD = deut. Larmor freq. (6.54 MHz/Tesla)
nQ = quadrupole freq. (335.6 kHz for ND3)
= 1/8 (e2qQ/h)
eQ = deuteron quadrupole moment
eq =electric field gradient
q = angle between eq. & B
m = +1
m = 0
m = -1
q
Example:
the ND3 molecule
N
D
q = 0
cos2 q = 1/3
q = p/2

## Slide 29
NMR Lineshape of Deuterons
m = +1
m = 0
m = -1
If nQ = 0 (or )
Equal splitting → same frequency
+1 ↔ 0
-1 ↔ 0
q
frequency

## Slide 30
NMR Lineshape of Deuterons
m = +1
m = 0
m = -1
At
Transitions split to
higher and lower frequencies
+1 ↔ 0
-1 ↔ 0
frequency

## Slide 31
NMR Lineshape of Deuterons
m = +1
m = 0
m = -1
At
Transitions split to intermediate frequencies, in opposite direction
to 0° case
+1 ↔ 0
-1 ↔ 0
p/2
frequency

## Slide 32
NMR Lineshape of Deuterons
m = +1
m = 0
m = -1
At
Transitions split to intermediate frequencies, in opposite direction
to 0° case
+1 ↔ 0
-1 ↔ 0
p/2
frequency

## Slide 33
NMR Lineshape of Deuterons
In amorphous or polycrystalline samples, all values of q are possible, although not with equal probability
+1 ↔ 0 transition
-1 ↔ 0 transition
The size of this transition is proportional to (N+ - N0)
The size of this transition is proportional to (No – N-)
The size of the sum is proportional to (N+ - N-)
the vector polarization!

## Slide 34
NMR Lineshape of Deuterons
P = 0.25
Q = 0.05
N+
N0
N-
N+
N0
N-
N+
N0
N-
P = 0.50
Q = 0.20
P = 0.75
Q = 0.48
Ts ≈ 1 mK
Ts ≈ 2 mK
Ts ≈ 0.5 mK
Ts = spin temperature
in a 2.5 T field
As the polarization increases
The size of the signal increases:
The asymmetry between the two transition increases:

## Slide 35
NMR Lineshape of Deuterons
As the polarization increases
The size of the signal increases:
The asymmetry between the two transition increases:
Ts = spin temperature
in a 2.5 T field
N+
N0
N-
N+
N0
N-
N+
N0
N-
Ts ≈ -1 mK
Ts ≈ -2 mK
Ts ≈ -0.5 mK
P = -0.25
Q = 0.05
P = -0.50
Q = 0.20
P = -0.75
Q = 0.48

## Slide 36
What to Expect this Week
Karl Slifer: Polarized target program at University of New Hampshire
Masataka Iinuma: Polarized target for tests of time-reversal invariance
Gerhard Reichertz: NMR of hyperpolarized fluorine-19
Victoria Lagerquist: Frozen spin targets and thin superconducting magnets
Allison Zec
Chhetra Lama
Nathaly Santiesteban
Elena Long
Michael McClellan
James Brock: Target development lab at Jefferson Lab
Mikhail Yurov: DNP program at Oak Ridge National Lab
Vibodha Bandara:
Kenichi Nakano:
Silviu Covrig-Dusa: Designing targets using computational fluid dynamics
Tsuneo Kageya: Lithium-deuteride target for JLab
Nadia Fomin: Polarized target development at University of Tennessee
Monday
Tuesday
Wednesday
Friday
(polarized gas targets II)
The New Hampshire Block