## Slide 1: Polarized Electron Sources
Topics discussed:
GaAs – 50 years of experience
Today’s ‘spin crisis’
Vacuum
Matt Poelker
Video by Mateus Silva Rêgo

## Slide 2: Electrons discovered!
1869-1875 Crookes tube: ‘cathode rays’ = stream of free electrons created via ionization of residual gas by DC voltage
‘Vacuum tubes’ invented ~1904 superseded the Crookes tube, operating at lower pressure. Free electrons no longer generated via ionization, but via heated filament - electrons released by thermionic emission
J. J. Thomson credited with ‘discovery’ ~ 1897, awarded the Nobel Prize for physics in 1906 for this work. Estimated mass of electron compared to lightest known element, hydrogen
Video by Mateus Silva Rêgo

## Slide 3: The First (DC High Voltage) Photogun
Started with a thermionic gun housing, circa 1976
Gallium Arsenide was known to have polarized internal electrons when optically pumped by circularly polarized light
(Ekimov and Sakarov, JETP Letters 13, 495, 1971)
Bell and Spicer had shown that the conduction band electrons could be photoemitted by adding Cs-O monolayers to the surface
Gallium Arsenide as source of polarized electrons proposed by Garwin, Pierce and Siegmann in 1974

## Slide 4: First Photoinjector
‘Photoemission of spin-polarized electrons from GaAs’, Daniel T. Pierce and Felix Meier, Phys. Rev. B 13, 5484 – June 1976
Polarized electrons accelerated at SLAC December 1977
E122 announces parity violation June 1978 - an important verification of the Standard Model

## Slide 5: Always Tweaking the Design
Endless quest for perfection
1
3
4
2

## Slide 6: Key Features of a Polarized Photogun
Photocathode
  High Polarization
  High QE (photoemission yield)
  Long Lifetime
Vacuum
  Static Vacuum
  Dynamic Vacuum
High Voltage
  Eliminating field emission
Drive Laser
  Reliable, phase locked to machine
  Adequate Power
  Wavelength Tunable

## Slide 7: Making Polarized Electron Beams
Use circularly polarized light to selectively populate the conduction band with electrons of a particular spin state )
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
1
3
s -
s -
GaAs energy levels
Energy vs wave vector
Circled numbers represent transition probabilities
mj: angular momentum quantum numbers
Valance band
Conduction band
(spin up)
(spin down)
(left circ.)

## Slide 8: Making Polarized Electron Beams
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
1
s+
s+
Energy vs wave vector
Valance band
Conduction band
(spin up)
(spin down)
GaAs energy levels
Use circularly polarized light to selectively populate the conduction band with electrons of a particular spin state )
Circled numbers represent transition probabilities
mj: angular momentum quantum numbers
(right circ.)

## Slide 9: How to eliminate the valence band degeneracy?
m j = -3/2
m j = -1/2
m j = -1/2
+1/2
+1/2
+1/2
+3/2
-1/2
3
3
s+
s -
This is what we want
Maximum Polarization 100%
hh: heavy hole
lh: light hole

## Slide 10: How to eliminate the valence band degeneracy?
PhD thesis, Paul Zorabedian, SLAC Report 248, 1982
Compress the GaAs crystal using a hydraulic press!
Hard to keep the sample from shattering
Stress splits the degeneracy of valence band

## Slide 11: There’s a better way
Lattice mismatch provides stress
Pablo Saez, PhD Thesis, SLAC Report 501, 1997
The band gap of the substrate layer must be larger than surface layer
Lattice constants must differ enough to introduce suitable strain
Adjust lattice constant of substrate by varying concentration of third element
1% lattice mismatch provides equivalent force of hydraulic press!

## Slide 12: Strained-Layer GaAs – a game changer
Zn dopant
~5.1018
(cm-3)
625 μm
2.5 μm
2.5 μm
100 nm
GaAs1-x Px (0<x<0.29)
GaAs
p-type GaAs
substrate
GaAs buffer
GaAs0.71 P0.29
MOCVD-grown
Polarization ~ 75% at ~ 850nm
QE ~ 0.1%
Strain relaxation – that’s the problem with this photocathode
Thickness beyond ~ 10 nm problematic
  Balancing QE vs Polarization
Required finicky modelocked Ti-sapphire lasers
No arsenic cap
Manufactured by Bandwidth Semiconductor

## Slide 13: Quantum Engineering
Nanometer scale layers
eg., GaAs/GaAsP strained superlattice
GaAs substrate
Strain-relaxed GaAsP buffer layer
GaAs
GaAsP
GaAs
GaAsP
GaAsP
GaAsP
GaAs
GaAs
GaAs
Only excite electrons from heavy-hole mini-band
×
NEA surface
Conduction mini-band
Heavy hole mini-band
Light hole mini-band
Slide courtesy Toru Ujihara, PESP 2008
Electrons tunnel through very thin buffer layers!!
D. Luh et al., SLAC, PESP2002

## Slide 14: Strained Superlattice GaAs/GaAsP – today’s benchmark
5.1019
5.1017
5.1018
Be
(cm-3)
GaAs1-x Px (0<x<36)
5 nm
14 pairs
625 μm
2.5 μm
2.5 μm
3 nm
4 nm
GaAs
GaAsP
p-type GaAs
substrate
GaAs buffer
GaAs0.64 P0.36
GaAs
MBE-grown epitaxial spin-polarizer wafer
Polarization ~ 85 to 90% at 780nm
QE ~ 1%
Thin layers eliminate strain relaxation – but complicate fabrication
Arsenic cap very beneficial
Highly doped surface layer to combat surface charge limit
Can use frequency doubled gain-switched diode laser/fiber amplifier to provide cheap RF-pulsed light at 780 nm
Manufactured by SVT Associates

## Slide 15: Experimenters appreciate higher polarization
This means it takes less time to do an experiment with same level of statistical accuracy
Compton Polarimetry at Hall A

## Slide 16: Today’s ‘spin crisis’
Today, there no longer exists a commercial supplier of strained superlattice GaAs/GaAsP photocathode. oh no! the physics community has come to expect 90% polarization – we can’t go back to bulk GaAs and 35% polarization
Historically, Labs worked with Universities to demonstrate high polarization photocathodes. Mostly this happened at SLAC, Nagoya University, and St. Petersburg Polytechnic University. T. Maruyama, Prof. Nakanishi, and Prof. Mamaev were central figures
DOE then assisted the commercialization of high polarization photocathodes via SBIR/STTR program: Bandwidth Semiconductor and SVT Associates in USA
DOE to the rescue….(let’s do what we did ‘last time’)
Ongoing programs:
  JLab and BNL partnered with Old Dominion University (Prof. Sylvain Marsillac)
  JLab and University of California Santa Barbara (M. Stutzman, C. Palmstrøm)
  BNL and Sandia National Lab (L. Cultrera and Center for Integrated Nanotechnology)
  BNL and Structured Materials Industries, Inc (L. Cultrera)
  Cornell University, and Center for Bright Beams

## Slide 17: Imperfect Vacuum = Finite Lifetime
Ionization cross-section for H2
Most ions created at low energy
200kV
Ion bombardment - notice characteristic “trench” from laser spot to electrostatic center of photocathode

## Slide 18: Improve Vacuum and Improve Lifetime
Gas Load inside a polarized photogun comes from:
leaks (real and virtual)
outgassing from the vacuum chamber walls and things you put inside the gun
from the accelerator beamline
Make Gas Load small and Pump Speed large
Limited selection of pumps for UHV and XHV
Q= gas load, q= outgassing rate, A = surface area, S = pump speed

## Slide 19: Pumpdown: effect of outgassing on p(t)
In a “perfect” vacuum vessel of volume V, pumped with constant pumping speed S, if p(t) is the pressure at time t, without leaks, permeation or outgassing:
Volume depletion
Pressure
time
10-4
10-5
10-6
1
10
100
1000
ln(p) versus ln(t)
with 0.5 < n < 1.2
Slide from G.Vandoni, CERN

## Slide 20: Phenomena behind outgassing
Surface:
Adsorption
chemisorption/ physisorption
Desorption
Bulk:
(Dissociation and) Permeation
Diffusion
Molecules deposited while exposed at atmospheric pressure desorb under vacuum
(Dissociation) and diffusion of atomic species in the near surface, through microcracks and the oxide layer
Diffusion from bulk of atomic H, trapped during manufacturing process, recombination at the surface and desorption as H2
Permeation through thin walls and elastomeric seals
Outgassing:
Combination of all these!
All relatively well understood and modeled:
It’s their combination which is not easy to understand!
Slide from G.Vandoni, CERN

## Slide 21: Get rid of the water…
H2
H2O
CO
CO2
“Residual Gas Analysis” of
un-baked vacuum chamber:
We need vacuum 10-11Torr
What does “bake” mean? It means heat the vacuum chamber at 250oC for 30 hours to rid the interior surface of the photogun of adsorbed water

## Slide 22: Post-Bakeout
H2
CO
CO2
CH4
These compounds are chemically inert

## Slide 23: Get rid of the hydrogen…
‘VIRGO/LIGO” bake: 400oC bakeout for 9 days, under vacuum
Our stainless-steel measurements
"Effect of heat treatments and coatings on the outgassing rate of stainless-steel chambers”, Journal of Vacuum Science & Technology A 32, 021604 (2014)
?
Low carbon steel

## Slide 24: Get rid of the hydrogen…
‘VIRGO/LIGO” bake: 400oC bakeout for 9 days, under vacuum
Our stainless-steel measurements
"Effect of heat treatments and coatings on the outgassing rate of stainless-steel chambers”, Journal of Vacuum Science & Technology A 32, 021604 (2014)
?
Low carbon steel

## Slide 25
Back up slides