## Slide 1: A facility for testing bulk superconducting MgB2 cylinder for the production of holding magnetic fields for polarized targets and nuclear fusion fuels
Giuseppe Ciullo
INFN-Ferrara & University of Ferrara
Interest on Bulk Superconducting material :
in polarized nuclear targets a magnetic holding field is required,
nuclear targets might feel detector fields, influencing the polarization axis.
We are interested in fundamental studies on the orientation between projectiles and targets: indipendent fields and shielding of the surrounding fields are required.
We are around the interaction point, then we look for low thickness of material, low Z, reducing, or avoiding, material for powering, transportability from the preparation laboratory to the experimental site.

## Slide 2: Outline of the idea for nuclear polarized target CLAS12-type
Choose a MgB2 S.C. cylinder surrounding the target.
Set an outer transverse field.
Cool down the S.C. Cylinder in the IBC (In Beam Cryostat) at 4 K
Ramp down the outer magnetic field.
The perfect diamagnetism of the S.C. MgB2 generates self supercurrents,
which mantain the seen field inside the cylinder.

## Slide 3: Moving to experimental or test sites
IBC (In Beam Cryostat) can be moved and inserted in CLAS-12.
In case of increasing of CLAS-12 field: supplementary self supercurrents in the MgB2 will mantain the transverse field.
Everything without any power supply and corrent leads, or coils, in the surrounding.

## Slide 4: Outline of the Idea for Polarized Fuel for nuclear fusion tests
Polarized
Atomic
Beam
T= 3-10K
Cold
Head
Recombinig Polarized
Atoms in hyperpol. molecules
Cold Head with an MgB2 cylinder
providing a holding field,
in this case it will parasitically
mantain the solenoidal field of the recombination chamber.
The cylinder hosts inside substrate for
condensation and it will be useful for
transportation for fusion studies and tests.
... our starting point for faisibility study is a magnetic field of 1 T.

## Slide 5: The compact «self» magnet
By
Bz
Advantages
No Power feeding
No Copper and Coils
Auto tuning
Semplicity
Low cost of production
few mm of thickness
External Magnet
Available Waste Material Machinable ( G. Giunchi)
diameter 39 mm - length 90 mm
thickness ~1 mm
M. Statera et al. (2015). IEEE Tr Appl. S:C., vol. 115(3): 1 - DOI: 10.1109/TASC.2015.2388855
Cylinder
MgB2
Shielding longitudinal fields
Mantaining transverse fields.
90 mm
39
mm

## Slide 6: Production of MgB2
Discovered 2001 (J.Nagamatsu [1] Nature 410(2001) 63).
Different techinques of production:
Japanese scientists: high pressure sintering – HIP (Hot Isostatic Pressing)[1] or UHP (Uniaxial Hot Pressing).
American Scientists: Mg vapor sintering of B fibers [2]
Italian Scientists: Mg Reactive Liquid Infiltration [3]
(Italian Patent Edison Spa pat., G. Giunchi, S.Ceresara 2001)
[1] J.Nagamatsu et al. Nature 410 (2001) 63.
[2] P.C. Canfield et al. PRL 86 (2001) 2423].
[3] G. Giunchi et al. Int. J.Mod.Physics B 17 (2003) 453.
Available Waste Material Machinable
( G. Giunchi)
diameter 39 mm - length 90 mm
thickness ~1 mm

## Slide 7: Field Cooling - Field Trapping
J. J. Rabbers et al. “Magnetic shielding capability of MgB2 cylinders” Supercond. Sci. Technol. Vol. 23, 2010
Field Cooling (FC), early cooling with applied field of 2 T, lowering down the applied field Bappl ,
Bhall measures the self field.
Bappl
BHall
P100 MgB2 L = 70 mm
Rext=17.75 mm, Rint=9 mm

## Slide 8: Field Trapping (Field Cooling)
7.5 hours to cool down from RT to 13 K
Field trapping after more than 12 h (thermal homogeneity?)
Low Temperature 13 K
Ramp down of the current feeding the magnet: : 0.25 A/4 s (0.06 A/s)
942 mT
A) temperature CLTS [K]
C) temperature RhFe [K]
B) current [A]
D) magnetic field @ center [mT]
cylinder
cold head
turbo pumps
316L chamber
Al chamber
pole Fe ARMCO
yoke
Cu coil
nylon support
Feasibility studies with oxford-Edwards
cold head 6/30

## Slide 9: Zero Field Cooling or shielding
J. J. Rabbers et al. Supercond. Sci. Technol. 23 (2010) 125003.
Zero Field Cooling (ZFC)
early cooling without external field, increasing up the applied field, Bappl, BHall provides the penetrated fields.
Bappl
BHall
cylinder
cold head
turbo pumps
316L chamber
Al chamber
pole Fe ARMCO
yoke
Cu coil
nylon support

## Slide 10: MgB2
.
G. Giunchi Internationl Journal of modern Physics B 17 (2003)
For the condition of
HD-ice at 4 K
Current density
Jc ≥ 10 000 A mm-2
(extrapolated)
Low Z
Cheapper than LTS and HTS
Machinable: spark erosion and diamond tools
To be conservative we assumed
for our preliminary studies
Jc ≥ 1 000 A mm-2
Jc experimental data for
SG (Small Grain size) continuous
and LG (Large Grain size) dashed line

## Slide 11: T Characterization in the feasibility study
Trapping Field
(Field Cooling)
Shielding
Zero Field Cooling
Evidence of Tc = 39.5 K
Good Performance @ T < 20 K
Good Reproducibility
More sensitive to T
Good performance at lower T
Reproducibility after many thermal cycles, quenches or flux jumps,
opening of system and change of thermal insulation materials
(2016 vs 2018)

## Slide 12: New cold head (on loan from FZJ –R. Engels)
Better thermal stability and lower themperature
RDK-415D Sumitomo (SHI Cryogenics Group):
1st stage 35 W @ 50 K ,2nd stage 1.5 W @ 4.2 K
(previous: 30 W @ 77 K, 6 W @ 10 K) .
2nd stage
1st stage

## Slide 13: Upgraded system @ FE
Scroll pump
1- iron yoke, 2 –coils, 3-iron poles, 4- nylon support, 5A –Al Chamber, 5B-5C SS chambers, 6-cold-head, 7B -7A TM pumps, 8A-8B Penning gauges

## Slide 14
TRhFe
under the copper can holding and shielding sensors and cylinder

## Slide 15: Locations of the transv. and long. Hall probes
TCernox
S3=S3mrt(middle radial transverse)
S2= S2mct(middle center transverse)
S4= S4ect(edge center transvere)
S1=S1mcl (middle longitudinal)
S5=S5ecl(edge center longitudinal)
S6=S6ert(edge radial transverse))
59.2 mm

## Slide 16: New power supply and transv. magnetic fiedl
OCEM-CAEN - NGPS 200 A- 50 V high stability power supply
Preliminary tests with 110 A (980 mT), now max current allowed on the coil 168 A (1 200 mT)..

## Slide 17: MgB2 cylinders
Different
Boron (99.5 % pure) precursor
grain size (mm) from Boron chip (mm)
mechanically grounded
and sieved to less
than (P)nnn mm.
P40
P160
P160
P100
P160
P100
P100
Unknow
used
for prel.
studies
Smaller the grain size higher transport characteristics,
but less thermal stability at lower T and lower B.
Connectivity P100 ~ 61 %, P40 ~89 %, PAM~73 %
thickness in mm
Length 97.05 – 97.5 mm
2.75
2.75
3.0
3.0
2.75
4.0
3.0
3.0

## Slide 18: Control, monitoring and DAQ
Pressure Monitoring (Mon.) & Recording (Rec.)
(Ppv ~ 10-2 mbar, Pbp ~ 10-6 mbar, Pch ~ 10-8 mbar)
Water circuit temperature 1) Water in,
2) Cryo Water out,
3) magnet body,
4) magnet water out.
Mon. & Rec.
Magnet power supply Monit. & Rec.
Hall probe
Monit. & Rec.
Cold head heater contr. Monit. & Rec.
Temperature sensor monit. & Rec.
Room Temperature
and Humidity
Mon. & Rec.

## Slide 19: Cooling down W.O. cylinder less than 3.5 (4.5) h against > 7.5 h (blind)
TCernox
TRhFe
under the copper can holding and shielding sensors and cylinder
TRhFe

## Slide 20: Temperature dependency of Hall probe
S3=S3mrt (middle radial transverse)
S2= S2mct(middle center transverse)
S6=S6ert(edge radial transverse)
S4= S4ect(edge center transverse)

## Slide 21: Field Cooling-Magnetization
TRhFe
TCernox
Bn is the corresponding Sn corrected byTcernox
Ramping down from110 A:
from Bappl 980 mT
to zero
with
P100 #6

## Slide 22: Trapped field vs Heating power (i.e. T)
11
mm
48 mm
TCernox
TRhFe
P100 #6
B2
B3
B4
B6

## Slide 23: Trapped Field vs Ramp down speed
11
mm
48 mm
P100 #6
B2
B3

## Slide 24: Trapped field vs Bappl
11
mm
48 mm
P100 #6
B2
B3
B4
B6

## Slide 25: How long the fields can stay an how stable is?
DB ~ 0.02 mT in 15 days
P100 #6

## Slide 26: Zero Field Cooling (ZFC ) Shielding
TRhFe
Ramping up to 110 A:
to Bappl 980 mT.
P100 #6

## Slide 27: Shielding vs Heater power (Temperature)
B2
B3
B4
B6

## Slide 28: Shielding vs Bappl
B2
B3
B4
B6

## Slide 29: How long works the shield and how stable is it?
B2
B3
B4
B6

## Slide 30: From SC to NC then Back in SC
in 1/2 hour,
we can go from superconducting state to the normal conducting one, and back at the set temperature.

## Slide 31: And the other cylinders: P40 #7, P160 #8
P40 was the first one istalled after the upgrade, but ...
Smaller the grain size higher transport characteristics,
but less thermal stability at lower T and lower B.
Connectivity P100 ~ 61 %, P40 ~89 %, PAM~73 %
Jc experimental data for
SG (Small Grain size) continuous
and LG (Large Grain size) dashed line

## Slide 32: P40 #7 Sample Ramp down 0.05 A/s
Bmct = 868 mT
Bmrt = 893 mT
Bect = 334 mT
Tcernox = 13.6 K
TRhFe = 8.6 K
Bmcl = 6.4 mT
Becl = -152 mT
Bert = 410 mT
11 mm }
11 mm }
{48 mm
}
}
59.2 mm }

## Slide 33: P40 #7 Sample Ramp down 0.05 A/s long
Bmct = 868 mT
Bmrt = 893 mT
Bect = 333 mT
Tcernox = 13.6 K
TRhFe = 8.6 K
Bmcl = 6.4 mT
Becl = -152 mT
Bert = 410 mT
11 mm }
11 mm }
{48 mm
}
}
59.2 mm }
Imagnet = 0 A

## Slide 34: Shielding 110 A ramp up 0.05 A/s
Early
Zero Field Cooling
then after
reaching the lowest
temperature
Ramp up the
external field.
P40 #7

## Slide 35: At higher temperature no flux jump
... but lower trapped field with respect to the P100 #6.
P40 #7

## Slide 36: MAGNETIzzAZION: less Trapped field and decreasing speedly (10 times more)
P160 #8
P100 #6

## Slide 37
SHIELDING: higher Bin
and increasing speedly (100 times more)
P160 #8
P100 #6

## Slide 38: Conclusions and Plans
We have in hands the system for testing «global» behavior of real bulk MgB2 cylinders.
We can investigate the behavior of the cylinder with different preparation procedure also checking their reproducibility on the nominal label P160, P100, P40 and PAM cylinders.
We can test the superconducting behavior from the reached low temperature (TRhFe 9 K - Tcernox 13 K) to the normal state transition.

## Slide 39
  Experimental tests on
    Trapping of Tranverse field and shielding of longitudinal field (target).
    Trapping of longitudinal field (fusion), but this is less critical than transverse field-
    Mapping of field for tranverse self field and external longitudinal field, mapping of longitudinal field.
  Checking theoretical model and tuning of them on data for field generation and shielding.
  Long time stability test for crossed beam in time interval for JLab targets and fusion test.
  Stability under movement in working conditions
FE apparatus at LASA-Milano (or...)
(Laboratorio di Acceleratori e Superconduttività Applicata)
  At LASA is under plan to put in operation a 10 T superconducting solenoid.

## Slide 40: Thanks to the organizers for accepting the contribution and to the audience for the attention.
I’d like to mention people involved in this work
Ferrara: Barion Luca, Contalbrigo Marco, Lenisa Paolo
Ferrara: SQUID measurements on MgB2 sample of the production
Spizzo Federico and Del Bianco Lucia
Bari: Tagliente Giuseppe – DAQ
JLab: Lowry Michael, Sandorfi Andrew – HD-Ice and simulations
Milano: Statera Marco

## Slide 41: Spare Slides for details

## Slide 42: TEsts and measurements on P40 #7

## Slide 43: Tests and measurements on P100 #6

## Slide 44: TEsts and measurements on P100 #6

## Slide 45
TEsts and measurements on P160 #8

## Slide 46: Shielding long term stability 1.5 -280 h.
Bmct = 147 mT
Bmrt = 118 mT
Bect = 687 mT
Bert = 661 mT
11 mm }
11 mm }
{48 mm
Bmcl = 21mT
Becl = 177 mT
Tcernox = 13.6 K
Bfed = 962.5 mT
Imagnet = 110 A
59.2 mm }
TRhFe = 8.6 K
... ended on monday 19/9

## Slide 47: CLAS12 INTEGRATION
SC magnet
4.5 T
persistent mode
LHe pumped (1.7 K)
shock absorbers
courtesy of A. Sandorfi
In Beam Cryostat
MgB2 magnetization
HDice insertion
courtesy of X. Wei
In Beam Cryostat
entering CLAS12
47

## Slide 48: Longitudinal polarized target

## Slide 49: Our starting point for faisibility study

## Slide 50: Lowry simulations

## Slide 51: Lowry simulations

## Slide 52: Production of MgB2 by Mg-RLI (Mg Reactive Liquid Infiltration)
Fill a steel container by B Power and large chunks of MgB2,
weld the container and perform thermal treatment at about 900-950 oC in conventional oven for 12-24 h.
Critical temperature
(TC) 39.5 K
High density 2.4 g/cm3
High connectivity
Very high superconducting characteristics
High value of critical currents