## Slide 1: Amorphous Carbon-coated Storage Cell Tests for the Polarized Gas Target at LHCb
Ralf Engels (IKP-2@FZJ/GSI)
PSTP2024 / 26th September 2024 / for the SPIN@LHCb project
Notes: 25 minutes + 5 minutes discussion

## Slide 2: The Experimental Setup
internal experiments –
with the circulating beam
external experiments –
with the extracted beam
p, p, d, d
with momenta up to 3.7 GeV/c

## Slide 3: ABS and Lamb-shift polarimeter
6-pole
magnet
6-pole
magnet
rf-transition
N+
N-

## Slide 4: PIT at ANKE@COSY
Main parts of a PIT:
  Atomic Beam Source
    Target gas
  hydrogen or deuterium
    H beam intensity (2 hyperfine states)
    8.2 . 1016 atoms / s
    Beam size at the interaction point
    σ = 2.85 ± 0.42 mm
    Polarization for hydrogen atoms
    PZ = 0.89 ± 0.01 (HFS 1)
    PZ = -0.96 ± 0.01 (HFS 3)
  Lamb-Shift Polarimeter
  Storage Cell
M. Mikirtychyants et al.; NIM A 721 (0) 83 (2013)

## Slide 5: The Experimental Setup
2nd life of the ANKE ABS:
Measure the polarization of H/D atoms and H2 / D 2 / HD molecules after the recombination of polarized atoms from an ABS
PRL 124:113003 (2020)
PRL 115:113007 (2015)
Beam
Hydrogen Atoms are Radicals
Target Density: increased by a factor ~100 : 1014 atoms/cm2
Polarization must be preserved !!!
Problems:
Magnetic impurities must be avoided
Most chemical reactions, mostly recombination, destroy at least 50% of the polarization
Vaccum and Beam regulations do not allow all kinds of materials

## Slide 6: The Experimental Setup
2nd / parallel life of the ANKE ABS:
Investigation of the nuclear polarization during:
Recombination processes
Wall interaction
---

## Slide 7: HD Molecules
Surface: Fomblin on Fused Quarz
T = 80 K / B = 0.528 T / E = 0.3 keV
Pz (H) = - 0.77
Pz (D) = - 0.79
Pzz (D) = + 0.69
Signal of the Photomultiplier [a.u.]
R. Engels et al., Phys. Rev. Lett. 124 113003 (2020)
Magnetic Field [a.u.]

## Slide 8: Storage Cell Coating
Which surface coatings are working ?
1.) Aluminium cells -> Bad secondary-electron yield -> Beam disturbance
2.) Teflon cells -> Isolator -> Beam disturbance
3.) Water ice -> Vacuum problems !!!
4.) Fomblin oil -> Vaccum problems !!!
→ CERN: What about a carbon coating ???

## Slide 9: Recombination on Carbon in the ISM
● Direct recombination is not probable due to energy and momentum conservation
● 3-particle interactions are very rare at these densities
● Recombination on a carbon surface as catalyser?

## Slide 10: Recombination on Carbon in the ISM
Possible Recombination Mechanisms:
WWU Münster; Phys. Institute,
Prof. H. Zacharias
Strong C-H Bond (~ 4.3 eV) prevents recombination
Radiation induced Desorption

## Slide 11: The Experimental Setup

## Slide 12: Radiation Test for Lyman-αlpha
Possible Light Source: Dissociator of the ABS
Bright Balmer light visible -> are there even Lyman photons ?
Reflections on aluminum surface for Lyman photons ~ 100%
Bachelor Thesis of Onur Bilen (HHU)

## Slide 13: Storage Cell Coating
Which surface coatings are working ?
1.) Aluminium cells -> reflects Lyman-α photons
2.) Teflon cells -> transmission through the surface ?
3.) Water ice -> reflects Lyman-α photons / transmission through the surface ? (O-H: ~ 4.8 eV)
Expectation for Carbon: -> Large Recombination in Combination
with Lyman-α radiation !

## Slide 14: Preparation of new Storage Cell
A 200 nm amorphous carbon-coated storage cell was provided by Pedro Costa Pinto from CERN
Requirements:
- High polarization preservation
- No recombination
4 gold plated tungsten wires run along the inside of the storage cell
Installation into the interaction chamber
●
●
●
●

## Slide 15: The Experimental Setup

## Slide 16: Mass spectroscopy
H+
H2+
H3+

## Slide 17: The Experimental Setup

## Slide 18: Lyman Spectra for H
Polarization spectrum of the Weak Field Transition Unit for H+ at B~0.5 T

## Slide 19: Lyman Spectra for H2
Polarization spectrum of the Weak Field Transition Unit for H2+ at B~0.5 T

## Slide 20: Polarization of the Protons
Proton fraction: a = 0.04 ± 0.15 95.5% < c < 100%
Wall collisions: n = 435 ± 236
Initial molecular pol.: Pm = 0.57 ± 0.03
Initial atomic pol.: Pa ≈ 0.8
Master Thesis of
Tarek El-Kordy
(FH Aachen)
Bc = 5.4 mT

## Slide 21: Conclusion
● (Exceptionally) high recombination rate: 95.5% < c < 100%
driven by Lyman-α photons.
● No dominant water layer present; no buildup of water layer on
amorphous carbon.
● Initial molecular polarization (fit): Pm = 0.57 ± 0.03 (Pa= 0.78).
(Large B field is needed to decouple I and J)
T. El-Kordy et al.; „Amorphous carbon-coated storage cell tests for the polarized gas target at LHCb”, NIM A 1068, November (2024) 169707