## Slide 1: Polarized Photocathode R&D at BNL and spin consideration for the EIC
September 22-27, 2024
Newport News, VA
Electron Ion Collider, Brookhaven National Laboratory
On behalf of the collaborator
Jyoti Biswas

## Slide 2: In collaboration with
BNL: Erdong Wang, John Skaritka, Luca Cultrera, Omer Rahman, Mengjia Gaowei, Kali Mondal, Wei Liu, Mike Blaskiewicz
Electron –Ion Collider
Jyoti Biswas
JLAB: Joe Grames, Matthew Poelker, Carlos Hernandez-Garcia, Gabriel Palacios-Serrano
ODU: Sylvain Marsillac, Adam Masters
CUNY ASRC: Tai-De Li

## Slide 3: EIC - polarized electron requirements
Electron –Ion Collider
Jyoti Biswas
Have existing hadron storage ring, electron storage ring and injector are new.
Phase I :7 nC / bunch; Phase II: 3 bunch train of 7 nC/bunch
At least 85% spin polarization from the source.
1.3 GHz linac with 7 nC bunch.
image courtesy: Vahid Ranjbar

## Slide 4: Polarized Electron Sources – HVDC gun
EIC 350 kV DC electron gun
EIC gun includes new features:
Large cathode area
Active cathode cooling
High gradient
Movable electrically insulated anode
3BG gauge | Gun Vacuum
Baseline | torr
67.5 uA | torr
3BG gauge | Gun Vacuum
Baseline | 
67.5 uA | 
This gun meet all EIC requirements
Electron –Ion Collider
Jyoti Biswas
Layout of the beamline including the DC gun and prep chamber
Wang et al., Appl. Phys. Lett. 124, 254101 (2024), https://doi.org/10.1063/5.0216694

## Slide 5: GaAs photocathode
Electron –Ion Collider
Jyoti Biswas
GaAs
GaAsP
Superlattice GaAs
ESP
Q
ESP
Q
GaAs
GaAsP
Superlattice DBR GaAs
Problems associated with GaAs photocathodes
Needs low Torr Vacuum.
Optimized surface doping needed
Laser induced heating could damage the QE
Transfer from facility to facility is challenging
SL pairs
DBR
TEM cross section image of SL-DBR
Biswas et el., NAPAC 24, 10.18429/JACoW-IPAC2024-MOPR77

## Slide 6: Chapter 1: GaAs photocathode R&D
Electron –Ion Collider
Jyoti Biswas
Optimize pre-cleaning and heat treatment
Optimize surface doping and DBR pairs
GaAs with 2D protection layer
“SPIN Crisis”
(lack of reliable SL-GaAs
R&D effort on
SL-GaAs (DBR)

## Slide 7: Optimizing pre-cleaning and heat treatment
Extracted charge vs laser power
A typical SL-DBR structure
Incorporated HCL wet etch & reduced heat treatment temperature of 450°C for DBR cathode.
Test in HVDC gun shows, higher charge could be extracted from the cathode, limiting surface charge effect.
Electron –Ion Collider
Jyoti Biswas
Secondary Ion Mass Spectroscopy (SIMS)
TEM images
HCL wet etch

## Slide 8: Optimizing doping and DBR pairs
Electron –Ion Collider
Jyoti Biswas
Mott Polarimeter located at EIC, BNL.
Surface doping of shows higher polarization and 16 pairs of DBR shows higher figure of merit .
Biswas et el., NAPAC 24, 10.18429/JACoW-IPAC2024-MOPR77

## Slide 9: GaAs with 2D protection layer
Electron –Ion Collider
Jyoti Biswas
G.Wang and N.Moody et al.
npj 2D Materials and Applications 17 (2018). doi:10.1038/s41699-018-0062-6
Schematic of the graphene transfer on GaAs
Successful growth of SL-GaAs with CsO activation layer underneath the graphene.
Similar activation of bulk GaAs was performed. We obtained better results on SL-GaAs with a cap layer.
Graphene protection layer makes the GaAs cathode less susceptible to heating.
Can sustain coarse vacuum environment with the protection layer. Meaning vacuum transfer of activated GaAs is a possibility.

## Slide 10: Chapter 2: Electron Spin consideration for EIC
Electron –Ion Collider
Jyoti Biswas
EIC 1.3 GHz pre-injector layout including DC gun, spin rotator, and bunching section
solenoid:
z
Electron spin from the gun is longitudinal
Two spin rotator will be used to rotate the spin vertical

## Slide 11: Spin rotator – Wien Filter
Electron –Ion Collider
Jyoti Biswas
Schematic of the Wien filter for S-DALINAC and CEBAF
Name | Energy [keV] | Bunch charge | Plate length [cm] | Gap [cm] | Ey [MV/m] | Bx [mT] | Feedthrough (each) | Ref.
CEBAF | 130 | 2 pC | 32.28 | 1.5 | 1.6 | 9.1 | 12.4 kV | 1
CEBAF | 200 | 2.7 pC | 32.28 | 1.3 | 2.7 | 13 | 17.5 kV | 2
CEBAF | 300 |  | 32.28 | 1.3 | 4.3 | 18.8 | 28.5 kV | 2
S-DALINAC | 100 | 4 pC | 38.10 | 2.0 | 0.756 | 4.6 | 12 kV | 3
MAMI | 100 | 0.02pC | 32 | 2.0 | 1.07 | 6.56 | 12.5 kV | 4
EIC | 320 | 7 nC | 45.92 | 7.0 | 1.44 | 6.080 | 50.5 kV | 5
https://accelconf.web.cern.ch/ipac2021/papers/mopab324.pdf
https://inspirehep.net/files/a7bbe70b5f54adc3b7e7f320651d2dd7
https://accelconf.web.cern.ch/p07/PAPERS/MOPAN013.PDF
https://www.sciencedirect.com/science/article/pii/S0168900206014434
https://www.jacow.org/ipac2024/pdf/MOPC24.pdf
In EIC, its highly space charge dominated beam, prototyping is essential.

## Slide 12: EIC Wien Filter Design
Electron –Ion Collider
Jyoti Biswas
Parameter | Value
Bunch charge | 7 -14 nC
Energy | 320 keV
L | 45.92 cm
EY | 1.44 MV/m
BX | 60.88 G
Electrode gap | 7 cm
Feedthrough | 50.5 kV each
7 cm
14 cm
Y
X
Z
At the centerline [X =0, Y=0]
(< 1%)
Z [m]
X
Y
Well matched E and B field achieved

## Slide 13: EIC Wien: Beam dynamics (with 7 nC)
Electron –Ion Collider
Jyoti Biswas
7 nC beam with space charge on, with triplet focusing
Cross-section of the magnet and yoke with 3D shaping
MAMI used triplet and doublet for focusing.
Transverse shaping is essential to better match both in longitudinal and transverse direction.
7 nC space charge dominated beam can go through both Wien Filter.
Thin quads in triplet configuration are used in beam dynamics. Quad optimization is in progress.
Y
X

## Slide 14: Summary
Optimized pre-cleaning and heat treatment of MOCVD grown DBR GaAs/GaAsP photocathodes.
Wet etching with HCL and lower heat treatment temperature of 450°C shows lowering of surface charge effect in HVDC gun.
Rugged GaAs with 2D protection layer underway.
Initial design of the Wien Filter is showing promising results.
7 nC space charge dominated beam can go through both Wien.
Quadrupole lens in triplet configuration are used for beam focusing.
Quadrupole design optimization is ongoing.

## Slide 15
Electron –Ion Collider
Jyoti Biswas
Thanks for your attentions!
Questions
Suggestions

## Slide 16: Backup
Electron –Ion Collider
Jyoti Biswas

## Slide 17
Magnet for the Wien
Z
X
Y

## Slide 18
Beam deflection Comparison: single particle in Parmela
Y [cm]
Wien Version: v1.9
Y [cm]
Wien Version: v2.1
Wien -1
Wien -1
Without 3d shaping
With 3d shaping