## Slide 1: GaAs-based Spin-polarized photocathode research at Cornell
Matthew Andorf

## Slide 2
Acknowledgements to:
NP-DOE DE-SC0023517
HEP-DOE DE-SC0021002
NFS PHY-1549132 CBB
Ivan Bazarov
Jared Maxson
Adam Bartnik
Alice Galdi (now @U. of Salerno)
Sam Levenson (graduate student)
Mark Reamon (undergrad)
The Bright Beams Lab

## Slide 3: High current and spin polarization
One of the remaining challenges for photocathodes is a robust, spin-polarized electron source
GaAs is by far the most studied spin-polarized electron source
Charge lifetime: The amount of current extracted before the QE degrades by 1/e
  1000 C is state of the art6 hours at 50 ma!
PEPPo
Cornell ERL gun

## Slide 4: Cornell Photocathode Lab
Vacuum level is below 10-10 Torr

## Slide 5: Cornell Photocathode Lab
Bialkali growth chamber
Cs,Sb,Te sources+O2 leak valve, thermally regulated with pneumatic valve control
Quartz microbalance (QMB) for deposition monitoring
Substrate heater

## Slide 6: Cornell Photocathode Lab
AUGER Chamber
Auger Electron Spectroscopy-To characterize surface chemistry
Low Energy Electron Diffraction-Chararacterize surface crystallinity
Cs, O2 leak valve.
Insulated, bias-able cathode holder

## Slide 7: Cornell Photocathode Lab
Mott polarimeter
20 keV target bias + Einzel lens beamline
Tungsten scattering target
Measure spin-polarization

## Slide 8
Negative Electron Affinity activation of GaAs
For high QE, GaAs is “activated” to Negative Electron Affinity (NEA)
  NEA means the bulk conduction band minimum is larger than the vacuum level
NEA is typically achieved by depositing a monolayer of Cs-Oxidant onto the GaAs surface can be done by:
  Co-deposition: Cs is deposited until QE peaks, at which point an oxidant is leaked while Cs source remains on
  Yo-yo method: the cathode is over cesiated at which point the cesium source turns off. It is then exposed to an oxidant until the QE peaks, the oxidant is then turned off and cesium source back on. The cycle is repeated numerous times.
Either O2 and NF3 can be used for an oxidant
Problem: A monolayer is a fragile thing!
  Chemical poisoning: Interaction with residual gas
  Ion back bombardment: residual gas is ionized and accelerated towards the cathode
V. Khoroshilov at al. (2020). Journal of Physics: Conference Series. 1482. 012013 DOI: 10.1088/1742-6596/1482/1/012013.

## Slide 9: Sb-based recipes
Various activation recipes were compared to Cs-O2
  Overall, Cs-O2 produced the highest QE while Cs-Sb had the worse
  Including O2 in the activation improved QE of Sb containing recipes
The QE was monitored over time to determine robustness
  All Sb activations outperformed pure Cs-O2 and pure Cs-Sb had the longest lifetime.
Co-deposition of Cs-Sb-O finds a happy middle ground
  10x Improved lifetime over Cs-O activation.
  10x improved QE over Cs-Sb activation at bandgap

## Slide 10: Sb-based activations-trade offs
Cs-O-Sb co-deposition recipe was further refined through scanning the Sb layer thickness:
  QE and electron spin-polarization decrease with Sb layer thickness
  0.12 nm layer results in only a small QE decrease while preserving max spin-polarization!
Cultrera et al, “Long lifetime polarized electron beam production from negative electron affinity GaAs activated with Sb-Cs-O: Trade-offs between efficiency, spin polarization, and lifetime (2020)”

## Slide 11: CsI surface treatment of GaAs
S.J. Levenson et al. IPAC’24. MOPR82
Use of CsI increases dark lifetime of GaAs!
  30 second 1% HCl chemical etch+6 hour anneal at 600 C
  ~1 nm of CsI deposited on GaAs surface. Activated with Cs. Poor lifetime and QE.
  Sample annealed and re-cesiated. Lifetime improvement with comparable QE Cs only GaAs activation
  Additional anneal further improves lifetime at expense of QE
  Lifetime improvement not simply the result of additional annealing cycles

## Slide 12: CsI surface treatment of GaAs
AFM performed at each step of surface treatment process
As received
After HCl etching
600 C anneal 6 hours
After CsI deposition
After 2nd 600 C, 6 hour anneal

## Slide 13: CsI surface treatment of GaAs
XPS analysis performed on pre- and post-annealed GaAs samples
  Pre-annealed sample confirms presence of CsI
  No Iodine detected on post-annealed sample!
  Strong suppression Cs20
XPS analysis in collaboration with Q. Zhu and M. Hines, Cornell Chemistry Department

## Slide 14: Ion back bombardment
An electron beam can ionize residual gas which will be positively charged
Ions will be accelerated towards the cathode and cause damage
So far, results have been in growth chamber
  Low current (1-100 nA)
  Low voltage (-18 V)
  Main source of degradation comes from vacuum poisoning
In a high voltage DC gun, induced damage from ion back bombardment is more severe
  Lower energy ions can sputter off activation layer
  High energy ions damage GaAs crystal structure
Operation at high voltage and current is critical to testing efficacy of alternative activation layers!
J. Grames et al. PRAB 14, 043501 (2011) doi: http://dx.doi.org/10.1103/PhysRevSTAB.14.043501
Image courtesy J. Grames

## Slide 15: The HERACLES Beamline
A beamline dedicated to the study of high current beam running:
Former CU-ERL gun 200kV @ 10 mA
Ion clearing electrodes
75 kW beam dump
EPICS based control system

## Slide 16: Beamline and Diagnostics
Thermal couples register beam induced temperature rise at the dump
Beamline
2 Solenoids, 3 corrector pairs (hor/vert)
2 clearing electrodes
3 screens, 1 quad detector
1 Faraday cup
EMS system (not implemented)
Solenoid scan characterizes cathode MTE
GPT simulation of fields/beam envelope

## Slide 17
HERACLES high current performance
Cs3Sb cathode on stainless steel puck
10 mA max current, limited by radiation trips
8 mA constant current for 3 + hours with no significant change in cathode QE
M. Andorf et al. NIMA: 1052 168240 (2023) https://doi.org/10.1016/j.nima.2023.168240

## Slide 18: HERACLES DRIVE LASER
Drive Laser for high current GaAs operation
  Ti:Sapphire oscillator: lasing at GaAs bandgap energy
  Ti:Sapphire excited with external 532 nm diode laser
  Easily switch between IR and green operation

## Slide 19: HERACLES growth chamber
Upgraded HERACLES to have an MBE growth chamber
3 Effusion cells (Cs, Sb, Te)+oxygen leak valve
Reproduced Sb-based activation lifetime improvements in growth chamber
Ready for high current runs!

## Slide 20: Initial high current runs
On going campaign to determine optimal Sb thickness for operational lifetime improvement
  Average beam current of 1 mA operated at 532 nm
  10-15 C of charge extracted per run
  More runs to come!
Sb Thickness (Angstrom) | 0 | 0 | 0 | 1 | 1 | 2
Lifetime (C) | 14.3 | 9.88 | 29.7 | 26.7 | 26.1 | 6.4

## Slide 21
Thank you for your attention!

## Slide 22
BACK UP SLIDES

## Slide 23
NEA GaAs can be generated by forming a heterojunction at the surface with another semiconductor (activation layer) subject to two criteria:
  In the activation layer, the gap from the fermi level to vacuum should be smaller than GaAs’s bandgap (~1.4 eV).
  So that photoemission does not occur from activation layer, its bandgap should be larger than GaAs’s.
    This criteria can be violated if the activation layer is sufficiently thin
The above suggest using p-doped GaAs with an intrinsic semiconductor with a small electron affinity for the activation layer
Cs3Sb and Cs2Te can form the NEA heterojunction
  Known to be less sensitive to chemical poisoning
  As a photoemitters they are robust at high currents
  This indicates Cs-Sb Cs-Te may be a very robust activation layers!
p-type
intrinsic
GaAs with alternative activation layers