## Slide 1
Development of GaN as a Robust Spin-Polarized Photocathode at Cornell University
Samuel J. Levenson
2024 Workshop on Polarized Sources, Targets, and Polarimetry
Newport News, VA, USA September 26, 2024

## Slide 2: Acknowledgements
M.B. Andorf
I.V. Bazarov
J. Encomendero
D. Jena
J.M. Maxson
V. V. Protasenko
H.G. Xing
B.D. Dickensheets
A. Galdi
Special thanks to J.K. Bae, B.A. Carmona, L. Cultrera, N. Otto, and M. A. Reamon

## Slide 3: Spin-Polarized Electron Sources

## Slide 4: Spin-Polarized Electron Sources
Goals for Sources
>90% spin polarization
Spin orientation reversibility
mA-scale current delivery
Low emittance and energy spread
Long operational lifetime

## Slide 5: GaAs Photocathodes
Photocathode
GaAs Cathode
Cs
Cs
Cs
Cs
Cs
Cs
Cs:GaAs photocathode excited with circularly polarized light
Goals for Sources
>90% spin polarization
Spin orientation reversibility
mA-scale current delivery
Low emittance and energy spread
Long operational lifetime
Strained GaAs: >90% spin polarizations
Journal of Applied Physics. 127, 124901 (2020)
>90% polarizations achievable with strained GaAs
52 mA record current (un-polarized)
<150 meV energy spread
High quantum efficiencies (QE)
Commercially available

## Slide 6: GaAs Photocathodes
Photocathode
GaAs Cathode
Cs
Cs
Cs
Cs
Cs
Cs
Cs:GaAs photocathode excited with circularly polarized light
Goals for Sources
>90% spin polarization
Spin orientation reversibility
mA-scale current delivery
Low emittance and energy spread
Long operational lifetime
Strained GaAs: >90% spin polarizations
Journal of Applied Physics. 127, 124901 (2020)
>90% polarizations achievable with strained GaAs
52 mA record current (un-polarized)
<150 meV energy spread
High quantum efficiencies (QE)
Commercially available
Needs Cs layer, making the cathode unstable, sensitive and short-lived

## Slide 7: Spin Polarized Photoemission
P3/2
P1/2
m = -1/2
m = +1/2
m = -1/2
m = +1/2
m = -3/2
m = -1/2
m = +1/2
m = +3/2
Spin Angular Momentum
Spin Angular Momentum
+1 in orange
-1 in green
3
1
2
3
1
2
Split-off
Spin Angular Momentum
Opposite-handed circularly polarized light
D. T. Pierce & F. Meier. Phys. Rev. B 13, 5484.1976.

## Slide 8: Gallium Nitride (GaN)

## Slide 9: Gallium Nitride (GaN)
Can be grown in hexagonal Wurtzite or cubic zinc-blende orientations
Zinc-Blende GaN
Just like GaAs!

## Slide 10: Gallium Nitride (GaN)
Can be grown in hexagonal Wurtzite or cubic zinc-blende orientations
Zinc-Blende GaN
Just like GaAs!
E1
E2
E3
Wurtzite GaN
Non-Degenerate Valence Band!

## Slide 11: GaN as a Spin-Polarized Source
  Wurtzite or Zinc-Blende orientation
  >50% QE achievable with W-pGaN
  Comparable spin relaxation time to GaAs (~5 ns)
  Could be strained for high polarization
  3.2 eV band gap is conveniently at the second harmonic of Ti:Sapphire
  Less Cs to get to NEA stronger bond to Cs?
  NEA with Cs only
GaAs for comparison: = 0.34 eV

## Slide 12: GaN as a Spin-Polarized Source
  Wurtzite or Zinc-Blende orientation
  >50% QE achievable with W-pGaN
  Comparable spin relaxation time to GaAs (~5 ns)
  Could be strained for high polarization
  3.2 eV band gap is conveniently at the second harmonic of Ti:Sapphire
  Less Cs to get to NEA stronger bond to Cs?
  NEA with Cs only
GaAs for comparison: = 0.34 eV
J. Vac. Sci. & Technol. B 32, 06F901 (2014)

## Slide 13: Our Cubic GaN Photocathode
Sample grown in molecular beam epitaxy growth chamber
AFM Images

## Slide 14: Our Cubic GaN Photocathode
Sample grown in molecular beam epitaxy growth chamber
AFM Images
Anti-phase boundary (APB) defects, characteristic of growths on 3C-SiC

## Slide 15
Our Hexagonal GaN Photocathode
Sample grown in molecular beam epitaxy growth chamber
AFM Images

## Slide 16
Our Hexagonal GaN Photocathode
Sample grown in molecular beam epitaxy growth chamber
AFM Images
Much better-quality surface than the cubic sample!

## Slide 17: Activation to NEA

## Slide 18: Activation to NEA
3.2 eV and 3.4 eV band gaps

## Slide 19: Activation to NEA
Lifetime monitored at respective threshold photon energies
GaAs activated in same chamber, monitored at 780 nm for reference (factors of 20 & 12 lifetime difference)
Higher QE/Lifetime in W-GaN likely due to better crystal quality

## Slide 20: Time to measure the spin polarization!

## Slide 21: Time to measure the spin polarization!
But first….

## Slide 22: Theoretical Excitations
Recall the band structure and excitation of GaAs
340 meV
1.43 eV

## Slide 23: Theoretical Excitations
ZB GaN
3.2 eV

## Slide 24: Theoretical Excitations
ZB GaN
3.2 eV
15 meV

## Slide 25: Theoretical Excitations
ZB GaN
3.2 eV
15 meV

## Slide 26: Theoretical Excitations
ZB GaN
3.2 eV
15 meV
3.4 eV
W GaN

## Slide 27: Theoretical Excitations
ZB GaN
3.2 eV
15 meV
3.4 eV
W GaN
5 meV
17 meV

## Slide 28: Theoretical Excitations
ZB GaN
3.2 eV
15 meV
3.4 eV
W GaN
5 meV
17 meV

## Slide 29: Theoretical Excitations
ZB GaN
3.2 eV
15 meV
3.4 eV
W GaN
5 meV
17 meV
~1 nm wavelength window!

## Slide 30
We therefore have very stringent light source requirements
- Design requirements:
  - Tunable from 360 nm – 390 nm
  - 1 nm bandwidth
  - 1-2 µW power at sample
  - Circularly polarized

## Slide 31
1032 nm pulsed femtosecond laser 20 W
Optical Parametric Amplifier Tunable 600-800 nm 2% efficiency
Frequency-doubling
BiBO crystal
Diffraction grating
Single-mode optical fiber
Linear polarizer and quarter-wave plate
- Design requirements:
  - Tunable from 360 nm – 390 nm
  - 1 nm bandwidth
  - 1-2 µW power at sample
  - Circularly polarized
We therefore have very stringent light source requirements

## Slide 32
1032 nm pulsed femtosecond laser 20 W
Optical Parametric Amplifier Tunable 600-800 nm 2% efficiency
Frequency-doubling
BiBO crystal
Diffraction grating
Single-mode optical fiber
Linear polarizer and quarter-wave plate
- Design requirements:
  - Tunable from 360 nm – 390 nm
  - 1 nm bandwidth
  - 1-2 µW power at sample
  - Circularly polarized
Femtosecond pulsed laser + optical parametric amplifier + frequency doubling
  20-40 mW of UV light
  1.5 nm linewidth
  Widely tunable
Frequency-doubling
BiBO crystal
We therefore have very stringent light source requirements

## Slide 33
1032 nm pulsed femtosecond laser 20 W
Optical Parametric Amplifier Tunable 600-800 nm 2% efficiency
Frequency-doubling
BiBO crystal
Diffraction grating
Single-mode optical fiber
Linear polarizer and quarter-wave plate
Final result: 1.4 nm bandwidth at Mott Polarimeter
- Design requirements:
  - Tunable from 360 nm – 390 nm
  - 1 nm bandwidth
  - 1-2 µW power at sample
  - Circularly polarized
We therefore have very stringent light source requirements

## Slide 34: Results
Peaks: W: 17%, ZB: 29%
Do these measurements make sense?

## Slide 35: Modeling the Cubic Sample
Initial excited spin polarization approximated with model for ZB structures by D’yakonov and Perel
Excited distribution peaks at 50% maximum, as expected
Mixing of split-off band with light and heavy hold bands

## Slide 36: Model
Scale model to approximate de-polarization effects
Peak (measurement maximum) at 33%, on par with that of GaAs
Note that the peak was scaled according to a fit with our data!

## Slide 37
Model
Gaussian light spectrum with variable bandwidth (B) and center at lambda
Since the spin-orbit splitting is so small, need to consider measuring spectrum with incident light spectra
Calculate effective polarization based on the light bandwidth

## Slide 38
Model
Measurements confirm bandwidth limit
Our 1.4 nm bandwidth measurements may be close to the theoretical maximum.
We get good agreement with the convolved DP Model
Spin depolarization mechanisms may be similar to those in GaAs

## Slide 39: Hexagonal Sample
The W-GaN ESP spectrum extends far into the bandgap
  Why?

## Slide 40: Hexagonal Sample
The W-GaN ESP spectrum extends far into the bandgap
  Why?
Mg-acceptor ~200 meV into bandgap

## Slide 41: Hexagonal Sample
The W-GaN ESP spectrum extends far into the bandgap
  Why?
Mg-acceptor ~200 meV into bandgap
3/2 character seen in Mg-acceptor level in single-crystal sample

## Slide 42: GaN Spin Polarization Outlook
While an interesting result, further work is needed for GaN to be used practically
Strained GaN
InGaN
Distributed Bragg Reflector
Things already done with GaN can be applied to photocathodes! Like…
C. Zhang et al. Appl. Sci. 2019, 9, 1593
D S Arteev et al 2018 J. Phys.: Conf. Ser. 1135 012050

## Slide 43: Conclusion
GaN may be a more robust option than GaAs for spin-polarized electron beam production
Spin-polarization measured from ZB and W GaN photocathodes, small SO splitting/bandwidth limited measurements
Advances already made with GaN may provide the next industry standard spin polarized photocathode
Thank you so much for your attention!!

## Slide 44: Mott
Linear Polarizer
¼-Waveplate
Cathode
Circular Polarized Light
Unpolarized Light
Tungsten Target
Scattering Detector
Scattering Detector
θ
θ
Polarization Measurement
Set light wavelength (λ)
Circularly polarize light:
Linearly polarizer
λ/4 Waveplate
Count scattered electrons on each detector (NL & NR)
Bend electron trajectory for transverse spin orientation
Fiber Head