## Slide 2: Nb films
Sergio Calatroni for the new CERN SRF & films team

## Slide 3: SC Nb coatings for RF cavities @ CERN
LEP200
LHC
HIE-ISOLDE
1.5 GHz
Low-
200 MHz

## Slide 4: A short history of Nb/Cu at CERN
LEP 200: 288 4-cell 352 MHz Nb/Cu cavities
LHC: 16 monocell 400 MHz Nb/Cu cavities
HIE-ISOLDE: 20 QWR 101 MHz Nb/Cu (phase 1+2)
R&D: 200 MHz, 400 MHz, 500 MHz, 1.3/1.5 GHz, =1 elliptical and = 0.48…0.85 elliptical, QPR resonator…
CERN activities in the field stopped circa 2000, and resumed a few years ago because of HIE-ISOLDE
This is known, and so what? Let’s see a few old slides

## Slide 5: BCS resistance at zero RF field, 4.2 K, 1.5 GHz
RBCS at 4.2 K
Nb bulk: ~900 n
Nb films: ~400 n
RBCS at 1.7 K
Nb bulk: ~2.5 n
Nb films: ~1.5 n
1
10
350
400
450
500
550
600
650
700
750
800
850
900
2
5
20
RBCS (4.2K) [n]
1+0/2
Nb bulk
Mean free path measured by RF frequency shift.
Please! Do such measurement for Nb bulk for N2 and like treatments!
Question: What would be the RF field dependent BCS for films (new measurement techniques unavailable 10 years ago)

## Slide 6: Effect of external magnetic field
Losses due to trapped external magnetic field at 1.7 K Rfl = (Rfl0 + Rfl1 HRF) Hext
The minimum values are obtained using Kr as sputter gas: Rfl0 = 3n/G ; Rfl1 = 0.4 n/G/mT
1
10
10
100
1+0/2
Rfl0[n/G]
(a)
1
10
1
10
Rfl1[n/G/mT]
1+0/2
(b)
Triangles: bulk Nb
Squares: coatings on oxide-free copper
Circles: coatings on oxidized copper
Note: This intrinsic values apply for full trapping, without fancy cool-down techniques for flux expulsion

## Slide 7: High-Q, High field cavities
Coatings performed using krypton
Fully EP (and EP only) substrates
Measurement at 1.7 K
Question:
Why can’t bulk niobium cavities be as good as coated ones ?
…. At low field….
3 nOhm

## Slide 8: Remainder of film properties
RRR (on quartz) : 274 (mfp = RRR * 2.7 nm)
H2 content: ~0.1 % atomic (TDS on Cu, non-epi and epi)
Coating angle of incidence < 30 degrees
(best coating temperature 150 °C)
µ-SR measurements in agreement with RF-measured mfp
Things can be tricky, though (next: old slides again)
(on Cu) | non-epitaxial | epitaxial
RRR | 11.5 ± 0.1 | 28.9 ± 0.9
Tc | 9.51 ± 0.01 K | 9.27 ± 0.09 K
Grain size | 110 ± 20 nm | >1 µm
Orientation | (110) | (211)(200)(110)
Strain a/a  | 0.636 ± 0.096 % | 0.466 ± 0.093 %
Much more data from JLAB, AASC,
…

## Slide 9: Films as a bulk – Hydrogen becomes a problem!
~1 µm grain size, RRR  28
~5 µm grain size, RRR  55
0.1 µm grain size, RRR  11
H2 content is ~ 0.1 at. % for sputtered Nb/Cu films (in niobium bulk it is
0.02 at.%) and it is picked up from vacuum system during deposition.
A possible solution: high-temperature annealing, but it does not work with copper cavities. Proposal (L. Hand, W. Frisken): molybdenum cavities.
There are more differences between these Nb/Cu films than those listed, this is just a basis for reflection

## Slide 10: Film as a bulk – H2 measurements
From: L. Hand, Cornell U. – W. Frisken, York U.
There are new results on measurements of H2 content by measuring the lattice parameter and the total impurity content
See TuP16

## Slide 11: The future
Time is ripe for restarting R&D
CERN management strongly supports this, also within FCC project
Focus on high-Q, not (only) high-field
We are reviewing internally our goals, resources, means and tools
Collaboration is the new mantra
Many possible items of study have been suggested
More can be discussed

## Slide 12: R&D lines
Structure (film defects, Hc1 and so on)
  HIPIMS
  High-temperature treatments & coatings
  (Substrate preparation)
  ….
Hydrogen
  High-temperature treatments & coatings
  Doping ?
  ….
New materials
  Nb3Sn by sputtering
  ….
Anything else?
  Please suggest and we may consider how to proceed