## Slide 1: Progress in Advanced Ferroelectric Technologies for Fast SRF Cavity Tuning
October 14, 2025
Alexei Kanareykin
on behalf of Euclid’s team
in collaboration with Jefferson Lab, Helmholtz-Zentrum Berlin (HZB) and CERN
LLRF’25
Newport News, VA
Supported by the DOE NP SBIR DE-SC0007630

## Slide 2
Outline
www.euclidtechlabs.com
Introduction Euclid Techlabs
Products & Capabilities Snapshot
SRF Technologies at Euclid
Ferroelectric materials for accelerators
Ferroelectric Fast Reactive Tuner tested at CERN
    Ferroelectric tuner development for CEBAF
    iSAS Program in Europe
    Conclusion

## Slide 3
Euclid Techlabs
www.euclidbeamlabs.com
Euclid Techlabs is a U.S.-based firm specializing in electron devices and advanced materials. After 20+ years serving the particle accelerator R&D market, we now ship a much wider-ranging product portfolio around the globe, from semiconductor photocathodes and superconducting photoinjectors, to ultrafast electron microscopy, to domestically-grown technical diamonds, ferroelectric fast tuners to arc-free high power microwave windows using our proprietary ceramic technologies.
EUCLID EAST • DC HQ and Materials
EUCLID WEST • Chicago Central Shops and Test Labs
As pioneers in advanced electron device engineering, we excel in tackling complex design challenges. Our agile, milestone-driven project management approach ensures optimal resource allocation and timely delivery. We collaborate with leading accelerator laboratories across the United States, the Department of Defense, CERN, and numerous global institutions. Our innovative solutions have garnered a diverse clientele spanning North America, Europe, and Asia.

## Slide 4
Products & Capabilities Snapshot
Products
UltraFast Pulser (UFPTM) for TEM
Compact X-Ray Source
L-band High Peak Current Linac
Electron sources and cathodes
SRF components (cryomodules, cavities)
RF high power windows
Fast reactive tuners for SRF
BPMs other accelerator components
CVD and HPHT diamonds,
Capabilities
Femtosecond Laser Ablation System
Thin Film Deposition Lab
TEM Testing Lab
High precision 4-axis turning/milling
Radiation Shielding/Testing Lab
Diamond Growth Lab
Photocathode Lab
Ceramic/ferroelectric Lab

## Slide 5
MBE system for Cs3Sb/Cs2Te growth
High precision 4-axis turning/milling
In-house Capabilities

## Slide 6
High Power Couplers for SRF
SRF coupler with extra low heat leak to 4K
In collaboration with FNAL (S.Kazakov)
1.3 GHz coupler
Conductive ceramic RF window
Notes: Euclid develops cavity and couplers for electrons and protons machines ranging from low to high beta as well as conduction cooled cryostats. Our coupler design is Crucial for conduction cooling apps with limited cooling capacity

## Slide 7
Euclid’s Conduction Cooled Cryomodule
1.3 GHz SRF Photogun
Development of MeV-range ultrafast electron diffraction/microscopy (UED and UEM) is a priority for the DOE. Euclid is developing the SRF photocathode gun that is a promising candidate to produce highly stable electrons for UEM/UED applications
(in collaboration with FNAL, BNL and Jlab)
SRF Photogun at 4K

## Slide 8
Euclid’s Conduction cooled 4K photoinjector for UEM/UED
Pure Nb cavity tests: Eacc>20MV/m
Nb3Sn test in HeL and CM
Euclid’s Conduction Cooled Cryomodule
The cryomodule was fully commissioned:
  Magnetic field below 5mG
  Cavity was successfully cooled according to specs
LLRF system developed in house and successfully commissioned
Pure Nb SRF gun was tested at 2K resulted in Q0=1010 and reached Ez=47MV/m on axis field and Eacc=22MV/m with just BCP
Nb3Sn test in VTS at 4.2K revealed contamination, nevertheless was tested in conduction cooled cryomodule (CC CM).
Eacc=4.3MV/m achieved in CC CM
The beam test at ANL AWA facility is currently being commissioned.
in collaboration with FNAL, BNL and ANL

## Slide 9
UEM/UED photoinjector beam test:
“SRF grade” (particle free) clean beamline is installed
Rest of the beamline is being built
  Optics
  Laser cross
  Beam diagnostics cross
Beam test is Fall 2025
Laser
Beam
Commissioned
Under construction
Jun 2025
Clean “Glove Box”

## Slide 10
Tight engagement with Chicago Proton Center oncologists, NWU.
Established the expertise in radiation simulation and dosimetry measurement.
Normal conducting LINACs and Electron Sources
Brachytherapy linac system
Photoguns and Thermionic guns

## Slide 11
Euclid Plays an essential role in critical components assembly for ANL-SLAC Cavity-based FEL Experiment at LCLS-II
The X-ray FEL oscillator (XFELO) and the X-ray regenerative amplifier FEL (XRAFEL) concepts use this technique
Both schemes require a high repetition rate electron beam, an undulator to provide FEL gain, and an X- ray cavity to recirculate and monochromatize the radiation.
A joint Argonne National Laboratory (ANL) and SLAC National Laboratory (SLAC) collaboration aimed at enabling these schemes at LCLS-II.
Euclid has been actively participating this project by assembling, testing, and QA all critical components in Euclid Class10k cleanroom at Euclid West facility.
Clean room facility at Bolingbrook IL

## Slide 12
A fast controllable tuners would allow microphonics compensation for the SRF accelerator with low beam loading.
Nonlinear ferroelectric microwave components can control the tuning or the input power coupling for rf cavities. Applying a bias voltage across a nonlinear ferroelectric changes its permittivity. This effect is used to cause a phase change of a propagating rf signal or change the resonant frequency of a cavity. The key was the development of a low loss highly tunable ferroelectric material.
Motivation Fast Ferroelectric Tuner
Courtesy of N. Shipman, CERN
Ferroelectrics have unique intrinsic properties that make them extremely attractive for high-energy accelerator applications. Their response time is ≈ 10-10 s for ceramic compounds which make ferroelectric promising candidates for the tuning and switching RF devices.

## Slide 13
History of the Fast Ferroelectric Tuner Development
In 2013, I. Ben-Zvi (BNL) proposed a new topic for the DOE SBIR/STTR program on the ferroelectric fast reactive tuner (F-FRT) development for microphonics compensation. It allowed Euclid to develop a new improved ferroelectric ceramic with ɛ~ 150, tanδ<1x10-3 at 1.3GHz and the tuning range up to Δε/ε~10% at 15 kV/cm5.
1R. Babbitt et al., 1994. “US Patent, US5334958A, 1993.
2V. Yakovlev et al. AIP Conf.Proc. 691,187, 2003.
3S. Kazakov et al. PRAB 13, 113501, 2010
Initial project to develop an ultra-fast (~1us) phase shifter/tuner using ferroelectric was carried out in collaboration with Omega-P/Yale University (V. Yakovlev, S. Kazakov) and BNL (I. Ben-Zvi) in 2004-20103. The phase shifter/tuner was intended to control of coupling of accelerating structures ( phase/amplitude), and to tune resonance frequency of the cavity. With this project, Euclid developed a ferroelectric material with dielectric constant ɛ~ 500, tanδ~2x10-3 at 1.3GHz but low tuning range, ~2/ kV/cm3,4.
A new, simple coaxial tuner design (S. Kazakov) for the F-FRT became feasible5, and the 400 MHz tuner prototype was fabricated by Euclid and tested at CERN in 2019 with the 400 MHz SRF cavity6.
4A. Kanareykin et al. Proc. EPAC 2006, 3251, 2006.
5A. Kanareykin et al. Proc. IPAC2013, 2486, 2014.
6N.Shipman et al. Proc. SRF2019, Dresden,WETEB7, 2019.
Ferroelectric phase and amplitude control was developed during the 1990’s1, in 2003 V. Yakovlev proposed RF switching by changing the frequency of a ’switching NC cavity’ containing ferroelectric material2. In 2006 Ilan Ben-Zvi initiated F-FRT research at BNL whereby the frequency of a SRF cavity would be controlled by an external ferroelectric tuner

## Slide 14
Fast tuning ferroelectric elements
Dielectric constant has to be low (~ 100-150)
Loss factor has to be low ~ 1x10-3 at 1 GHz and ~1x10-4 at 100 MHz
Tuning range has to be high ~ 6-8% at 15kV/cm
Can be done with (Ba, Sr)TiO4+Mg oxides
Curie temperature dependence on Mg-oxide content. Curie temperature shift with Mg based oxide increase
Dielectric constant of pure BST ~ 1000, and it’s lossy. To reduce both eps and tanδ, one has to develop a mixture (solid solution) of BST ferroelectric and low loss linear ceramic

## Slide 15
ε and tanδ vs. temperature and frequency
Dielectric constant weakly depends on the frequency
Loss tangent increase linearly with frequency
Q×f (GHz)=const
tanδ=1/Q
for ~1 GHz and ε~150
Q×f~1,000, tanδ~1x10-3
Dielectric constant and tanδ measurements in the temperature range T=200С-600С at 400 MHz for the BST(M) ferroelectric material: tanδ=1.3×10-3 T=220С and ~ 17% improvement at T=550С.
For lower dielectric constant, tanδ is significantly reduced.

## Slide 16
Ferroelectric ceramic properties
Parameters | Value
dielectric constant,  | ~150
tunability,  | ~ 10% at 15kVcm-1 of the bias field
response time | < 10 ns
loss tangent at 1.3 GHz, tan | ~110-3
breakdown limit | 200 kV/cm
thermal conductivity, K | 7.02 W/m-K
specific heat, C | 0.605 kJ/kg-K
density,  | 4.86 g/cm3
coefficient of thermal expansion | 10.110-6 K-1
temperature tolerance, T | (1-2 units) K-1

## Slide 17
BST Based Tuner Design (assembly)
design of S. Kazakov and V. Yakovlev

## Slide 18: F-FRT low power tests at Euclid at CERN
Measured at CERN frequency response at 600 ns of a cavity to a 4 kV high voltage pulse (orange) applied to the connected FE-FRT.
Assembled F-FRT
Ferroelectric element before metallization
N. Shipman, et al., IPAC’21, 1305, 2021
Measured at Euclid phase shift vs. time at biasing voltage applied (~ μs range response time)

## Slide 19: F-FRT test with SRF Cavity at CERN
Experimental Setup
FE-FRT mounted on cryostat.
N. Shipman, et al., SRF’19, WETEB7

## Slide 20: Slow Tuning
N. Shipman, et al., IPAC’21,

## Slide 21
First ever Ferroelectric Fast Reactive Tuner (FE-FRT) test with a superconducting cavity
Microphonic Suppression (1)
N. Shipman, et al., IPAC’21,

## Slide 22: Summary of F-FRT Testing at CERN
N. Shipman, et al., IPAC’21,
*N. Shipman. SRF’19

## Slide 23
FRT for 1.5 GHz Single Port Cavity
C100 cavity, and C100 cryomodule with FPCs in CEBAF section SL25, Jlab, upper left – two port cavity.
Ferroelectric tuner and MT (upper corner) in the LLRF schematic of C100
Ferroelectric tuning element (red) with alumina matching section (yellow)
Euclid Techlabs is developing the first fast ferroelectric tuner for a SRF accelerator that is currently in operation – CEBAF at JLAB. In comparison with our first tuner prototype, it requires a new configuration, with a single RF power port for both the klystron and the tuner. This is the only option for the current C100 cryomodules at CEBAF, and many other projects.

## Slide 24
Simulink modeling of the FRT microphonics compensation via the single FPC
Although it is non-ideal to use FRT through FPC, it is possible to maintain Qext and compensate the microphonics simultaneously.
Simulink modeling shows the klystron power demanding can be reduced by ~25% in the case of Jlab C100 cavities.
Emulated microphonics signal
FRT with 10% loss
Cavity voltage
Cavity Phase
~25% reduction
Klystron power as needed to compensate the microphonics
FRT OFF
FRT ON
13.9 MV
900

## Slide 25
3 kW of CW power causes 7 temperature rise with rather small convection coefficient. Water cooling substantially reduces temperature rise.
Current Status of the 1.5 GHz FRT
Euclid has carried out thermal and RF measurements of improved ferroelectric ceramic, completed the tuner RF and thermomechanical design, and is currently finishing the mechanical engineering design for fabrication. HOM analysis is complete too.
Engineering design
Thermal analysis
HOM analysis

## Slide 26: iSAS Program
Goal is establishing collaboration to expedite the development of novel energy-saving technologies to SRF particle accelerators.
Innovate for Sustainable Accelerating Systems (iSAS)

## Slide 27: iSAS Program –cont.
TA#1: energy-savings from RF
TA#2: energy savings from the cryogenics
TA#3: energy savings from the beam
INT#1: integrate into the design of a sustainable LINAC cryomodule
INT#2: integrate into existing LINAC cryomodules at RIs
INT#3: integrate towards turn-key solutions and applications in industry
[1] https://isas.ijclab.in2p3.fr/
[2] https://indico.ijclab.in2p3.fr/event/11291/overview

## Slide 28
The Horizon Europe iSAS project [1] focuses on improving accelerator efficiency and includes the integration of a ferroelectric fast reactive tuner (FE-FRT) to enhance energy conservation. Applications under this initiative include an
FE-FRT for 400 MHz transient beam loading compensation in the LHC (CERN),
FE-FRT systems for microphonics compensation in 1.3 GHz SRF cavities (HZB),
FE-FRTs for energy recovery linac (ERL) applications (HZB),
retrofitting FE-FRTs into existing HL-LHC cryomodules (CERN)
iSAS Program
Innovate for Sustainable Accelerating Systems (iSAS)

## Slide 29: FRT in the U.K.
FRT can reduce power demands for low beamloading machines by reducing the overhead needed for microphonics. For machines with reactive beamloading by switching the frequency during abort gaps
Graeme Burt, Daresbury Lab
Lancaster University

## Slide 30: Tree-stub tuner for variable loads, CEBAF
Using a three-stub tuner to minimize the reflected power only works if the load has a constant impedance, which is often, but not always, true. If the load is varying in time, the best that can be done is to match the stub tuner to the average value.
HFSS model of a single stub tuner attached to a WR650 rectangular waveguide (b) S₁₁, parameters vs. the ferroelectric sleeve’s dielectric.
In collaboration with JLab
A. Hutton, A.Costilla, JLab

## Slide 31: First Workshop on Ferro-Electric Fast Reactive Tuners (FE-FRTs)
HZB to host First Workshop on Ferro-Electric Fast Reactive Tuners (FE-FRTs)
Join us for the first-ever workshop on Ferro-Electric Fast Reactive Tuners (FE-FRTs), taking place at Helmholtz-Zentrum Berlin (HZB) on November 13–14, 2025
https://indico.ijclab.in2p3.fr/event/11291/overview

## Slide 32
In conclusion,
New ferroelectric ceramic material was developed with the set of parameters satisfying the Ferroelectric Fast Reactive Tuner (F-FRT) requirements for microphonic compensation, transient detuning, and fast switching.
First F-FRT prototype was designed, fabricated and successfully demonstrated at CERN
The Horizon Europe iSAS project focuses on improving accelerator efficiency and includes the integration of a ferroelectric fast reactive tuner (FE-FRT) to combat microphonics and enhance energy conservation.
In the U.S., the FE-FRT technology is under development for microphonics compensation in CEBAF