## Slide 1
Total-reflection high-energy positron diffraction: Principle and application
Yuki Fukaya
Advanced Science Research Center, Japan Atomic Energy Agency, JAPAN
LEEPP@Jefferson Lab
CEBAF Center Room F113
March 24, 2026
Notes: 1

## Slide 2
Acknowledgements
This work was performed under the approval of the Photon Factory Program Advisory Committee (Proposal No. 2014S2-004 and No. 2017G639).
The present work was partly supported by JSPS KAKENHI Grants No. JP18H01877 and No. JP19K22134.
I. Mochizuki, K. Wada, T. Shidara, T. Hyodo (KEK)
M. Maekawa, A. Kawasuso, S. Entani, S. Sakai (QST)
I. Matsuda, B. Feng, Y. Zhao (Univ. Tokyo), H. Fukidome (Tohoku Univ.)
G. Zhou, L. Wang, Q.-K. Xue (Tsinghua Univ.), F. Zheng, P. Zhang (IAPCM)
H.-W. Kim, J. R. Ahn (Sungkyunkwan Univ.)
Y. Endo, S. Hasegawa (Univ. Tokyo), A. Takayama (Waseda Univ.)
J. Yoshinobu, Y. Hasegawa, T. Ozaki (Uni. Tokyo)
C.-C. Lee (Tamkang Univ.), A. Fleurence, Y. Yamada-Takamura (JAIST)
S. Shamoto (RADA)
A. Ichimiya (Nagoya Univ.)
1/35

## Slide 3
Contents
1. Introduction
  A brief background of 2D materials
2. Method
  Surface sensitivity of total-reflection high-energy positron diffraction (TRHEPD)
3. Topics
  Structure determination of 2D materials
    Bismuthene (Bi counterpart of graphene)
    Intercalated graphene
4. Summary
2/35
Notes: 3

## Slide 4
2D materials: Graphene
M. I. Katsnelson, Mater. Today 10, 20 (2007).
Band structure
Dirac cone
Extremely high carrier mobility (~100,000 cm2/Vs)
Many other promising features (high thermal conductivity, robust mechanical property…)
3/35
Notes: 4

## Slide 5
Group-IV element 2D materials
+
Extremely high carrier mobility (~100,000 cm2/Vs)
Many other promising features (high thermal conductivity, robust mechanical property…)
Good affinity to current Si-based technology
2D topological insulator
Si or Ge
Germanium
Germanene
-ene
Silicon
Silicene
『一家に１枚』シリーズ（https://www.mext.go.jp/stw/series.html）より
4/35

## Slide 6
Silicene/Ag(111)
P. Vogt et al., PRL 108, 155501 (2012).
C.-L. Lin et al., APEX 5, 045802 (2012)
2D materials on various substrates
Silicene/ZrB2(0001)
A. Fleurence et al., PRL 108, 245501 (2012).
Germanene/Pt(111)
Germanene/Au(111)
Germanene/Al(111)
M. E. Dávila et al., New J. Phys 16, 095002 (2014).
L. Li et al., Adv. Mater. 26, 4820 (2014).
M. Derivaz et al., Nano Lett. 15, 2510 (2015)
5/35

## Slide 7
Plumbene/Pd(111)
J. Yuhara et al., Adv. Mater. 31, 1901017 (2019).
2D materials on various substrates
Stanene/Pd2Sn(111)
J. Yuhara et al., Phys. Rev. Mater. 5, 053403 (2021).
Germanene/Al(111)
Germanene/Ag(111)
J. Yuhara et al., ACS Nano 12, 11632 (2018).
J. Yuhara et al., 2D Mater. 8, 045039 (2021).
J. Deng et al., Nat. Mater. 17, 1081 (2018).
Stanene/Cu(111)

## Slide 8
Positron
pair creation (LINAC etc)
― positron-electron pair creation
due to high-energy x-rays
β+ decay (22Na etc)
― β+ decay for radioactive isotope
antiparticle of electron
― positron: positive charge
― electron: negative charge
age > 6.4×1024y
annihilation
― annihilation with electron
Property
X-ray
p → n + e+ + νe
e+
Production
method
(probability < 10-6 )
(= electron age)
7/35
Notes: 8

## Slide 9
e+: 10 keV
Total-Reflection High-Energy Positron Diffraction TRHEPD
Sample
surface
Glancing angle:
θ = 0.1°~ 6.0°
Experimental setup
Diffraction pattern
Screen
(Spot intensity as a function of  )
Rocking curve
(at fixed  )
Potential energy of positron & electron
Intensity analysis
(based on dynamical diffraction theory)
Atomic configuration
8/35
Notes: 9

## Slide 10
Refraction of positron at surface
surface
vacuum
e+
crystal
positron
θ
θ'
surface
vacuum
e-
crystal
electron
θ
θ'
for e+ (q = +e)
Refractive index (n)
n(e-) > 1 > n(e+)
qV: Inner potential energy
E: Incident beam energy
Critical angle of total reflection (θc)
for e- (q = -e)
k
k'
k
k'
9/35
Notes: 10

## Slide 11
Penetration depth of positron beam
Si crystal
surface
only 1 atomic layer
positron
electron
(E = 10 keV)
critical angle
(θc = 2.0º)
Total reflection region
bulk
deeper
10/35
Notes: 11

## Slide 12
High Energy Accelerator Research Organization (KEK)
Google Map
http://www-linac.kek.jp
40 miles
(65 km)
11/35
Notes: 12

## Slide 13
(stations are not shown)
SPF-B1
(Ps-)
SPF-A1
SPF-A3
(TRHEPD)
Basement floor
Ground floor
SPF-B2
(Ps-TOF)
Positron converter/moderator assembly
(0.1 - 35 kV)
Linear accelerator (linac)
電子線形加速器
Slow-positron beam line
(grounded potential)
e-
e+
Slow Positron Facility, KEK
SPF-A2
TRHEPD chamber
12/35
Notes: 13

## Slide 14
e-
Positron converter/moderator assembly (0.1 - 35 kV)
13/35
Notes: 14

## Slide 15
14/35
Notes: 15

## Slide 16
Development of LINAC-based TRHEPD
(2010～)
Slow Positron Facility, KEK
Iron plate
Magnetic lens
Helmholtz coils
Remoderator and
electrode assembly
Feedthrough
Objective lens
Manipulator
Sample holder
Microchannel
plate
Gate valve
Magnetic lens
B
Positron beam
-B
200mm
Maekawa et al., Euro. Phys. J. D 68, 165 (2014).
Intensity is ~100 times larger than RI beam
e+
Linear accelerator (LINAC)
e-
Converter/
moderator
5×107 e+/sec
~5×105 e+/sec
Energy-tunable (< 35 keV)
15/35
Notes: 16

## Slide 17
Improvement of quality of data
(Diffraction pattern & rocking curve)
LINAC-based
RI-based
(22Na)
~100 times
RI-based (22Na)
LINAC-based TRHEPD (this study)
1/7
0
2/7
3/7
4/7
5/7
6/7
1
θ = 2.1°
θ = 2.1°
Si(111)-7×7 surface
Clear diffraction pattern was successfully obtained
16/35
Notes: 17

## Slide 18
Penetration depth of positron beam
(experimental evidence)
We verified experimentally that positron beam sees only topmost layer
exp
(total reflection condition)
cal
(inc. only adatoms)
well-reproduced
Si(111) surface (side view)
exp
cal
(inc. only adatoms)
RHEED (electron beam)
Y. Fukaya et al., Appl. Phys. Express 7, 056601 (2014).
adatoms
1st layer
2nd layer
17/35
Notes: 18

## Slide 19
Topics
Graphene
  Graphene/Co(0001)
  Graphene/Cu(111)
  Intercalated graphene
Silicene
  Silicene/Ag(111)
Germanene
  Germanene/Al(111)
Y. Fukaya et al., Phys. Rev. B 88, 205413 (2013).
Y. Fukaya et al., Carbon 103, 1 (2016).
Y. Fukaya et al., Phys. Rev. B 108, 155422 (2023).
Y. Fukaya et al., 2D Materials 3, 035019 (2016).
in collaboration with
Prof. I. Matsuda group
in collaboration with
Prof. I. Matsuda group
18/35
Notes: 19

## Slide 20
Topics
2D superconductor
  Ca-intercalated bilayer graphene/SiC(0001)
  Single-layer FeSe/SrTiO3(001)
2D bitriangular lattice
  Ge/ZrB2(0001)
2D quasicrystal
  Bilayer Gr/SiC(0001)
A. Fleurence et al., Phys. Rev. B 102, 201102(R) (2020).
Y. Endo et al., Carbon 157, 857 (2020).
Y. Fukaya et al., Phys. Rev. B 104, L180202 (2021).
Y. Fukaya et al., J. Phys.: Condens. Matter 31, 055701 (2019).
in collaboration with
Prof. S. Hasegawa group
in collaboration with
Prof. Y. Yamada-Takamura group
in collaboration with
Prof. I. Matsuda group
in collaboration with
Prof. Q.-K. Xue group
19/35
Notes: 20

## Slide 21
Bismuthene
Y. Fukaya and I. Matsuda, Appl. Phys. Lett. 127, 263102 (2025).
Notes: 21

## Slide 22
R. Bhuvaneswari et al., Phys. Lett. A 383, 125975 (2019).
Bismuthene: Bi counterpart of graphene
Bismuthene (free-standing)
Bismuthene/Ag(111)
Y. Guo et al., ACS Appl. Mater. Interfaces 9, 23128 (2017).
X. Liu et al., Chem. Soc. Rev. 49, 263 (2020).
・Large buckling
・√7×√7 structure
1.78 Å
2.61 Å
21/35

## Slide 23
S. Sun et al., ACS Nano 16, 1436 (2022).
Synthesis of bismuthene on substrate
Bismuthene/Ag(111)
Bismuthene/SiC(0001)
F. Reis et al., Science 357, 287 (2017).
K. Takahashi et al., Phys. Rev. B 108, L161407 (2023).
K. Yaegashi et al., Langmuir 38, 13401 (2022).
22/35

## Slide 24
TRHEPD rocking curves of 2×2 spots
[] azimuth
[] azimuth
Bismuthene has mirror symmetry with respect to both azimuths
[]
[]
Flat structure
Ag(111)
Bi
Ts = 170 K
Ts = 170 K
23/35
Notes: 24

## Slide 25
Comparison with calculations
[] azimuth
[] azimuth
Averaged (weighted) Rp = 0.14 < 0.2
[]
[]
Flat honeycomb structure
Ag(111)
Bi
zBi
zAg1b
zAg1b
zBi
zAg1a
zAg1a
ΘBi
ΘAg1
24/35
Notes: 25

## Slide 26
Structural and non-structural parameters
[]
[]
Ag(111)
Bi
2.48 Å
3.34 Å (fixed)
 | zBi-Ag1 (Å) | zAg1a-Ag2 (Å) | zAg1b-Ag2 (Å) | ΘBi (K) | ΘAg1 (K)
This study | 2.48 | 2.31 | 2.31 | 92 | 112
2.31 Å
K. Takahashi et al., Phys. Rev. B 108, L161407 (2023).
Ag(111)-√3×√3-Bi: ΘBi = 77 K, ΘAg1 = 160 K
I.M. McLeod et al., Surf. Sci. 604, 1395 (2010).
(Ag bulk: 2.36 Å)
25/35
Notes: 26

## Slide 27
Intercalated graphene
Y. Fukaya, S. Entani, and S. Sakai, Phys. Rev. B 108, 155422 (2023).
Notes: 27

## Slide 28
Single-layer graphene on substrate
M. I. Katsnelson, Mater. Today 10, 20 (2007).
Band structure (ideal)
Extremely high carrier mobility (~100,000 cm2/Vs)
Many other promising features (high thermal conductivity, robust mechanical property…)
≠
(freestanding) graphene
Dirac cone
G. Giovannetti et al., Phys. Rev. Lett. 101, 026803 (2008).
Band structure (theory)
Missing
graphene on metal substrate
27/35
Notes: 28

## Slide 29
Graphene-substrate spacing
G. Giovannetti et al., Phys. Rev. Lett. 101, 026803 (2008).
M. Vanin et al., Phys. Rev. B 81, 081408(R) (2010).
C. Gong et al., J. Appl. Phys. 108, 123711 (2010).
I. Hamada, M. Otani, Phys. Rev. B 82, 153412 (2010).
Interlayer distance is crucial to elucidate origin of electronic property of graphene adsorbed on metal substrate
Band structure
Atomic configuration
G. Giovannetti, PRL (2008).
Wide
Narrow
28/35
Notes: 29

## Slide 30
Intercalation between Gr and substrate
Insertion of Au atoms between graphene and Ni (intercalation)
Dirac cone appears
However, interface structure is unknown
Ni
Gr
Au
Interface structure between graphene and Co substrate
for Ag or Au intercalation was investigated using TRHEPD
A. Varykhalov et al., Phys. Rev. Lett. 101, 157601 (2008).
29/35
Notes: 30

## Slide 31
Change in structure by intercalation
pristine
as-deposited
(room temp.)
annealing at ~400ºC
Au (5 ML)
Au
Co
Co
Ag (5 ML)
Ag
Co
Co
annealing at ~700ºC
Ag intercalation
Au intercalation
Notes: 31

## Slide 32
Ag or Au intercalated interface
Change of spacing between Gr and metal
Change in intensity
by Ag or Au intercalation
From strong to weak (van der Waals) interaction
by noble metal intercalation
Co
Co
3.32 Å
3.24 Å
2.06 Å
2.06 Å
≈ d (graphite)
(3.35 Å)
d (Gr/Ag)
d (Gr/Au)
Y. Fukaya et al., Phys. Rev. B 108, 155422 (2023).
Au (5 ML)
Ag (5 ML)
31/35
Notes: 32

## Slide 33
Theory
Giovannetti, Phys. Rev. Lett. (2008).
Vanin, Phys. Rev. B (2010).
Gong, J. Appl. Phys. (2010).
Hamada, Phys. Rev. B (2010).
Graphene-metal spacing
32/35
Notes: 33

## Slide 34
Change in structure by intercalation
pristine
as-deposited
(room temp.)
annealing at ~400ºC
Au (5 ML)
Au
Co
Co
Ag (5 ML)
Ag
Co
Co
annealing at ~700ºC
Ag intercalation
Au intercalation
Notes: 34

## Slide 35
Summary
Graphene height from the underlying atoms is shifted from ~2.0 Å to ~3.3 Å due to Ag or Au intercalation
Intercalation results in the transformation to quasifreestanding graphene, like hydrogen intercalation
Intercalated graphene
flat honeycomb structure and Interlayer distance of 2.48Å
Interlayer distance paves the way to elucidate the origin of the magnitude of coupling between bismuthene and Ag(111) substrate
Bismuthene
M. Dodenhöft et al., Phys. Rev. B 108, 155438 (2023).

## Slide 36
Summary
Y. Fukaya（分担執筆）
“Chapter 4: Diffraction: Determination of Atomic Structure”
MONATOMIC TWO-DIMENSIONAL LAYERS: Modern Experimental Approaches for Structure, Properties, and Industrial Use, edited by I. Matsuda (Elsevier, 2018) p. 75-111.
Y. Fukaya, A. Kawasuso, A. Ichimiya, and T. Hyodo
“Total-reflection high-energy positron diffraction (TRHEPD) for structure determination of the topmost and immediate sub-surface atomic layer”
J. Phys. D: Appl. Phys. 52, 013002 (2019).
Y. Fukaya
“Total-Reflection High-Energy Positron Diffraction Study on Topmost Surface Structure”
Vacuum and Surface Science (表面と真空) 68, 91 (2025) (in Japanese).
Review articles
Total reflection occurs owing to the positive charge of positron
TRHEPD enables to determine the topmost surface structure without any information on deeper layers
TRHEPD
TRHEPD will help to solve the complicated structure of 2D materials

## Slide 37
Online Workshop on Positron Diffraction
https://asrc.jaea.go.jp/soshiki/gr/sis-gr/reimei-ws2026/reimei-ws2026-home.html
“Positron Diffraction Studies on 2D Materials and
Related Novel Surface Analysis Techniques”
30 March 2026, 13:30 – 17:20 JST – Online
Registration deadline: 25 March 2026
29 March 2026, 23:30 – 30 March 2026, 03:20 EST/EDT
(If you happen to stay up late, please feel free to join us!)

## Slide 39
Positron brightness enhancement by remoderation
Brightness
I : Beam intensity（I → I/10）
r : Beam radius（r→r)
E : Beam Energy (5 keV→3 eV )
θ：Beam divergence （～50° → ～10°）
(W foil)
Transmission-type remoderator
Notes: 39

## Slide 40
Transmission-type remoderator
Remoderator
W (t100 nm)
Magnetic lens
(enlarged)
side view
Magnetic lens
electrode
During annealing
100 mm
120 mm
Notes: 40

## Slide 41
Brightness enhanced positron beam
decrease by a factor of 1/8
Beam image
20 mm
decrease by a factor of 1/4
flux : 5×105 e+/sec
collimator
remoderation
φ = 0.5 mm
8 eV
61 eV
Energy spread
>> 104 -103 e+/sec (RI)
Notes: 41

## Slide 43
2×2 Bismuthene formation on Ag(111)
RHEED patterns during Bi growth on Ag(111) surface at ~140 K ([] azimuth)
1 min
2 min
3 min
4 min
5 min
6 min
7 min
8 min
Bi coverage = 0.16 ML
Bi deposition rate = 0.02 ML/min
alloying-to-dealloying transition ((p × √3) phase) occurs above 0.55ML. K. H. L. Zhang et al., Phys. Rev. B 83, 235418 (2011).
Notes: 43

## Slide 44
Intensity analysis
Pendry R-factor
: excellent agreement
J. B. Pendry, J. Phys. C 13, 937 (1980).
: anti-correlation
: no correlation
Intensity calculations
Dynamical diffraction theory (multi-sliced method)
A. Ichimiya, Jpn. J. Appl. Phys. 22, 176 (1983).
(w : peak width)
Notes: 44

## Slide 46
Rocking curves for
graphene/Co(0001) & graphene/Cu(111)
E = 10 keV
①
②
13°
<111>
<110>
<112>
fcc crystal
Incident azimuth of positron beam

## Slide 47
Effect of atomic displacements on rocking curves for graphene/Co(0001)
d = 2.2 Å
Δ = 0 Å
side view
Δ
d
Graphene on Co(0001)
d & Δ dependences of rocking curves (calculations)
Rocking curve is very sensitive to values of Δ & d