## Slide 1: Theoretical perspective of SRF performance
Nov. 12, 2025
SRF Frontiers Workshop
High energy Accelerator Research Organization (KEK)
Innovation Center for Applied Superconducting Accelerators (iCASA)
Takayuki Kubo
T. Kubo
(2013)

## Slide 2
Overview of
the theoretical frameworks

## Slide 3
Mean
free
path
0
Temperature

## Slide 4
Mean
free
path
0
Temperature
Ginzburg-Landau ()

## Slide 5
Mean
free
path
0
Temperature
Ginzburg-Landau ()
Eilenberger
Formalism
Applicable to
Any temperature
Any mean free path

## Slide 6
Mean
free
path
0
Temperature
Ginzburg-Landau ()
Eilenberger
Formalism
Applicable to
Any temperature
Any mean free path
Usadel
Formalism
Applicable to
Any temperature

## Slide 7
Under the ac field
Thermal Equilibrium
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)

## Slide 8
Linear response
regime
Thermal Equilibrium
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Under the ac field

## Slide 9
Linear response
regime
Thermal Equilibrium
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Under the ac field

## Slide 10
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory

## Slide 11
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 12
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 13
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Mattis-Bardeen
Theory
Unfortunately, this is
the SRF accelerator regime

## Slide 14
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 15
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 16
Mattis-Bardeen
Theory
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh
Eilenberger
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 17
Mattis-Bardeen
Theory
Keldysh
Eilenberger
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
Under the ac field
Unfortunately, this is
the SRF accelerator regime

## Slide 18
Quality factor
: dissipation per RF cycle
: how many cycles it takes for the stored energy to completely dissipate

## Slide 19
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Nonlinear response
Regime
Keldysh-Usadel
Thermal Equilibrium
The SRF accelerator regime

## Slide 20
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Keldysh-Usadel
Thermal Equilibrium
Let us start from
the linear response

## Slide 21
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.

## Slide 22
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
We apply a small ac electromagnetic field and calculate the first-order perturbation to the current.
Some
factor

## Slide 23
We apply a small ac electromagnetic field and calculate the first-order perturbation to the current.
Then,
the complex conductivity is given by
D. Rainer and J. A. Sauls,
Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
Start from the Keldysh-Eilenberger equations (a set of equations for Green‘s functions and pair potential )
Some
factor
Some
factor

## Slide 24
W. Zimmermann, E. Brandt, M. Bauer, E. Seider, and L. Genzel, Optical conductivity of BCS superconductors with arbitrary purity, Physica C 183, 99 (1991).
D. Rainer and J. A. Sauls, Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
T. Kubo, Effects of Nonmagnetic Impurities and Subgap States on the Kinetic Inductance, Complex Conductivity, Quality Factor, and Depairing Current Density, Physical Review Applied 17, 014018 (2022)
Complex conductivity formula for arbitrary MFP (for )

## Slide 25
W. Zimmermann, E. Brandt, M. Bauer, E. Seider, and L. Genzel, Optical conductivity of BCS superconductors with arbitrary purity, Physica C 183, 99 (1991).
D. Rainer and J. A. Sauls, Strong coupling theory of superconductivity, in Superconductivity: From Basic Physics to the Latest Developments, edited by P. N. Butcher and Y. Lu (World Scientic, Singapore, 1995), p. 45.
T. Kubo, Effects of Nonmagnetic Impurities and Subgap States on the Kinetic Inductance, Complex Conductivity, Quality Factor, and Depairing Current Density, Physical Review Applied 17, 014018 (2022)
Complex conductivity formula for arbitrary MFP (for )
In the dirty limit
()
The well-known
dirty-limit Mattis-Bardeen formula

## Slide 26
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear response
regime
Leading order
nonlinear
correction
Keldysh-Usadel
Thermal Equilibrium

## Slide 27
Keldysh–Usadel Equation for SC under a strong ac field
We solve these equations to obtain the nonequilibrium corrections ( and ).
arXiv:2509.09766

## Slide 28
Keldysh–Usadel Equation for SC under a strong ac field
To obtain the current response,
we substitute the solutions (, ) into
We solve these equations to obtain the nonequilibrium corrections ( and ).
← Linear response
← Nonlinear correction of
arXiv:2509.09766

## Slide 29
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
← Linear response
← Nonlinear correction of

## Slide 30
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
← Linear response
← Nonlinear correction of

## Slide 31
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections

## Slide 32
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and

## Slide 33
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and
AAA contribution
Contribution mediated
by the nonequilibrium
pair-potential variation

## Slide 34
Schematically, the results can be illustrated as
Linear
response
Nonlinear corrections
and
Time dependent :
Higgs
Time averaged :
Eliashberg effect
Note: This theory automatically includes
the Eliashberg effect (microwave-induced gap enhancement) as well as the Higgs-mode contribution.
AAA contribution
Contribution mediated
by the nonequilibrium
pair-potential variation

## Slide 35
Eliashberg effect?
Higgs?

## Slide 36
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.

## Slide 37
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.

## Slide 38
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation

## Slide 39
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation

## Slide 40
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
qausiparticles

## Slide 41
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
Microwave induced
gap enhancement
qausiparticles

## Slide 42
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
Microwave induced
gap enhancement

## Slide 43
Eliashberg effect?
Higgs?
The variation of order parameter does not appear in standard linear-response theories such as Mattis–Bardeen theory because is an effect, but it does emerge in nonlinear response.
Time-averaged nonequilibrium gap variation
Time dependent nonequilibrium gap variation
Microwave induced
gap enhancement
Not important for
at SRF’s

## Slide 44
Nonlinear correction
arXiv:2509.09766

## Slide 45
Nonlinear correction
arXiv:2509.09766

## Slide 46
Nonlinear correction
Higgs
Contribution:
Time dependent
Eliashberg
Contribution:
Time averaged
arXiv:2509.09766

## Slide 47
Results

## Slide 48
Results
The resonance peak at Δ
comes from the Higgs mode

## Slide 49
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
is a decreasing function of the ac amplitude (q).

## Slide 50
Results
The resonance peak at Δ
comes from the Higgs mode
At lower frequencies,
is a decreasing function of the ac amplitude (q).
The AAA term is
the dominant contributor
at low frequencies

## Slide 51
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
arXiv:2509.09766
Dirty limit ()

## Slide 52
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
arXiv:2509.09766
Dirty limit ()
Experiments:
Moderately dirty ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)

## Slide 53
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
ac amplitude dependent dissipative conductivity
Note: this corresponds to a few (mT)
arXiv:2509.09766
Dirty limit ()
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
Experiments:
Moderately dirty ()
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)

## Slide 54
ac amplitude dependent dissipative conductivity
M. Martinello et al., Phys. Rev. Lett. 121, 224801 (2018)
DOI: https://doi.org/10.1103/PhysRevLett.121.224801
To deal with the red-framed region, the theory must be extended nonperturbatively to capture the quasiparticle spectrum modified by strong AC currents (DOS smearing).
Gurevich, PRL 113, 087001 (2014)
Kubo-Gurevich, PRB 100, 064522 (2019)
Experiments:
Moderately dirty ()
M. Martinello et al., PRL. 121, 224801 (2018)
P. Dhakal et al., PRAB 27, 062001 (2024)

## Slide 55
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
Kubo, arXiv:2509.09766

## Slide 56
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
Kubo, arXiv:2509.09766
The SRF theory
(Deep Nonlinear Regime)

## Slide 57
Keldysh
Eilenberger
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Linear
response
regime
The SRF theory
(Deep Nonlinear Regime)
Keldysh-Usadel
Thermal Equilibrium
Leading order
nonlinear
correction
Kubo, arXiv:2509.09766
Gurevich, PRL 113, 087001 (2014)
Kubo-Gurevich, PRB 100, 064522 (2019)
T. Kubo, arXiv:2509.09766 (2025)
Nonperturbative treatment (DOS smearing et al.)

## Slide 58
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
arXiv:2509.09766
Dirty limit ()
Theoretical prediction: effects of the inelastic scattering rate

## Slide 59
360MHz for Nb
720MHz for Nb
3.6GHz for Nb
1.8GHz for Nb
arXiv:2509.09766
Dirty limit ()
360MHz for Nb
3.6GHz for Nb
36GHz for Nb
7.2GHz for Nb
Theoretical prediction: effects of the inelastic scattering rate
arXiv:2509.09766
appendix
Dirty limit ()

## Slide 60
Quality factor at lower temperatures (K)
Accelerator cavity
Quantum memory cavity
for quantum computing
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 61
High-Q superconducting cavities allow us to store quantum information redundantly, enabling bosonic error correction.
1 photon loss
1 photon loss
a remainder of 2
when divided by 3
a remainder of 1
when divided by 3
correct
correct
Known to reduce the required number of qubits by one to two orders of magnitude.
e.g. binomial code
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 62
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
3D coaxial cavity progress
Yale University
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 63
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
3D coaxial cavity progress
Yale University
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y
University of Innsbruck

## Slide 64
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
Oriani et al., Phys. Rev. Applied 24, 044080 (2025)
Niobium (1:1:2 water buffered chemical polishing below 10℃),
(single photon level)
3D coaxial cavity progress
↑
The world record (as of 2024)
Yale University
University of Chicago
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y
University of Innsbruck

## Slide 65
Sometimes, I do experiments (BCP etc)
Kubo
↓
cavity→

## Slide 66
Kubo
↓
cavity→
Sometimes, I do experiments (BCP etc)
Nb coaxial cavity of KEK-NTT collaboration
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.

## Slide 67
Kubo
↓
cavity→
Sometimes, I do experiments (BCP etc)
Corresponding to
photon lifetime of
~0.1 sec.
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
We broke
the world record!!!→
20mK & Single photon level
Nb coaxial cavity of KEK-NTT collaboration
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.

## Slide 68
Reagor et al., Phys. Rev. B 94, 014506 (2016)
Aluminum,
(single photon level)
Heidler et al., Phys. Rev. Applied 16, 034024 (2021)
Niobium (1:1:1 buffered chemical polishing at 0-5℃),
(single photon level)
Oriani et al., Phys. Rev. Applied 24, 044080 (2025)
Niobium (1:1:2 water buffered chemical polishing below 10℃),
(single photon level)
T. Takenaka, T. Kubo et al., arXiv:2510.01819 (2025)
Niobium (1:1:1 BCP at 25℃ + 900℃ anneal
+ 1:1:1 BCP flush at 25℃ + 600℃ anneal)
Q=3×109 (single photon level)
3D coaxial cavity progress
Yale University
University of Innsbruck
University of Chicago
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
KEK&NTT
The world record
Brock et al., Nature 641, 612 (2025)
https://doi.org/10.1038/s41586-025-08899-y

## Slide 69
TLS fit
Even in this record-high-Q cavity, TLS defects still limit the quality factor.
Understanding TLS physics and developing engineering methods to mitigate them are necessary to realize ultra-high-Q cavities for accelerators and quantum computing.
TLS fit
TLS fit
TLS fit
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
Maybe, my next project.

## Slide 71
Gradient (microwave amplitude)
Electric field
Magnetic field

## Slide 72
Electric field
T. Kubo
(2013)

## Slide 73
170mT
0mT
85mT
of Nb
of Nb
210mT
Magnetic field

## Slide 74
170mT
0mT
85mT
of Nb
of Nb
210mT
Magnetic field
Low field (Meissner state)
(⌐■_■) good

## Slide 75
170mT
0mT
85mT
of Nb
of Nb
210mT
Magnetic field
Low field (Meissner state)
(⌐■_■) good

## Slide 76
170mT
0mT
85mT
of Nb
of Nb
210mT
Magnetic field
High field (vortex state)
＼(^o^)／I’m doomed

## Slide 77
170mT
0mT
85mT
of Nb
of Nb
210mT
Magnetic field
The ultimate limit of cavities made from bulk material is considered as
:​ the lower critical field, above which the Meissner state becomes energetically unfavorable.
: the superheating field, which represents the stability limit of the Meissner state. Ultimate limit for the ideal material.

## Slide 78
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?

## Slide 79
Purity
(mfp )
Intrinsic
Theory
(applicable to SRF temperature )
Summary of the superheating field

## Slide 80
Purity
(mfp )
Intrinsic
(e.g., Nb3Sn,
NbN, NbTiN etc.)
Summary of the superheating field
Theory
(applicable to SRF temperature )

## Slide 81
Purity
(mfp )
Intrinsic
(clean)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
Summary of the superheating field
Theory
(applicable to SRF temperature )

## Slide 82
Purity
(mfp )
Intrinsic
(clean)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
Summary of the superheating field
Theory
(applicable to SRF temperature )
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
for

## Slide 83
Purity
(mfp )
Intrinsic
(clean)
any
(from clean limit
to dirty limit)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
Summary of the superheating field
Theory
(applicable to SRF temperature )
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
for
for

## Slide 84
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
Purity
(mfp )
Intrinsic
(clean)
any
(from clean limit
to dirty limit)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
(dirty)
for
Summary of the superheating field
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
Analytical result for T=0.
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
T. Kubo, Supercond.Sci. Tecnol. 34, 045006 (2021)
Theory
(applicable to SRF temperature )
for
for

## Slide 85
Purity
(mfp )
Intrinsic
(clean)
any
(from clean limit
to dirty limit)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
(e.g., Nb)
(dirty)
Summary of the superheating field
Theory
(applicable to SRF temperature )
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
for
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
Analytical result for T=0.
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
T. Kubo, Supercond.Sci. Tecnol. 34, 045006 (2021)
for
for

## Slide 86
Purity
(mfp )
Intrinsic
(clean)
any
(from clean limit
to dirty limit)
(e.g., Nb3Sn,
NbN, NbTiN etc.)
(e.g., Nb)
(dirty)
any
(from clean limit
to dirty limit)
N/A
Summary of the superheating field
We don’t know of clean Nb
Theory
(applicable to SRF temperature )
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
for
G. Catelani and J. P. Sethna,
Phys. Rev. B 78, 224509 (2008)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
F. Pei-Jen Lin and A. Gurevich,
Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
Analytical result for T=0.
V. P. Galaiko, Sov. Phys. JETP 23, 475 (1966)
Analytical result for T=0.
T. Kubo, Phys. Rev. Research 2, 033203 (2020)
T. Kubo, Supercond.Sci. Tecnol. 34, 045006 (2021)
for
for

## Slide 87
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?

## Slide 88
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .

## Slide 89
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .
Ginzburg–Landau (GL) theory, valid near , gives
A. J. Dolgert et al., Phys. Rev. B 53, 5650 (1996)
M. K. Transtrum et al., Phys. Rev. B 83, 094505 (2011)

## Slide 90
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Maximum field achieved so far
Already close to the theoretical limit?
The answer: we currently have no reliable estimate, because there is no theory of applicable to clean Nb at .
Ginzburg–Landau (GL) theory, valid near , gives
If we naively extrapolate this to low temperatures — not theoretically justified — we obtain the rough estimate
?
mT ?
A. J. Dolgert et al., Phys. Rev. B 53, 5650 (1996)
M. K. Transtrum et al., Phys. Rev. B 83, 094505 (2011)

## Slide 91
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
If we believe this rough
estimate of based on GL, we get
T. Kubo, Jpn. J. Appl. Phys. 64, 018002 (2025)
Note: To achieve , it is necessary to eliminate all surface defects. However, this alone is not sufficient to reach ; it is also essential to ensure that the thermal runaway field exceeds .
This condition is not always satisfied, particularly at 2 K. It is better to test the cavity at lower temperatures (e.g., 1.8K or 1.6K) to ensure that the condition is satisfied.

## Slide 92
Keldysh
Eilenberger
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh-Usadel
Thermal Equilibrium
The above superheating-field theories calculate the dc (equilibrium) superheating field.
NOTE

## Slide 93
Keldysh
Eilenberger
Driving force of
Nonequilibrium
Dynamics
(e.g, strength of microwave)
Keldysh-Usadel
Thermal Equilibrium
The above superheating-field theories calculate the dc (equilibrium) superheating field.
Is the ac (nonequilibrium) superheating field equivalent to the dc one?
NOTE

## Slide 94
Summary of my perspective
We are only one step away from establishing the SRF theory.
Nonperturbative treatment (DOS smearing et al.)
Gurevich, PRL 113, 087001 (2014)
Kubo-Gurevich, PRB 100, 064522 (2019)
T. Kubo,
arXiv:2509.09766 (2025)
+
→
the SRF theory
Understanding TLS is essential to realizing ultra-high- cavities.
The dc superheating field is largely understood, whereas that of clean Nb has not yet been fully understood. In addition, the ac superheating field remains largely unexplored.
(hat I am interested in)

## Slide 96
Backup

## Slide 97
dc + ac

## Slide 98
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 99
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 100
If the AC field is absent, this reduces to a problem of equilibrium superconductivity.
That case was already well understood decades ago.
See also, T. Kubo, Phys. Rev. Research 2, 033203 (2020); F. Pei-Jen Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024) DOI: https://doi.org/10.1103/PhysRevApplied.22.044042

## Slide 101
However, once an AC field is present, the problem becomes much more complicated. In that case, we need to use the theory of nonequilibrium superconductivity.
The Keldysh-Eilenberger theory is a microscopic theory of nonequilibrium superconductivity. It is applicable at any temperature () and for arbitrary mean free path. In this sense, it serves as the “theory of everything for conventional superconductivity”.
The Keldysh–Usadel theory represents the dirty-limit reduction of the Keldysh–Eilenberger theory of nonequilibrium superconductivity, applicable at any T ().
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
A. Moor et al., Phys. Rev. Lett. 118, 047001 (2017)
T. Jujo, J. Phys. Soc. Jpn. 91, 074711 (2022)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 102
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 103
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
Higgs
↓
Particle physics

## Slide 104
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
Particle physics
Superconductivity
Oscillation of
superfluid density
Higgs
↓

## Slide 105
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs?
The Higgs mode in superconductivity is an effect. It does not appear in standard linear-response theories such as Mattis–Bardeen, but it does emerge in nonlinear response. In our case, we apply both DC and AC fields. As a result, the Higgs mode shows up as , and responds linearly to the AC field.
Higgs
↓
Oscillation of
superfluid density
Superconductivity
See the famous review paper:
R. Shimano and N. Tsuji,
Annu. Rev. Condens. Matter Phys. 11, 103 (2020)

## Slide 106
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 107
Keldysh–Usadel Equation: DC Current with AC Perturbation
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)
To obtain the ac response,
we substitute the solutions (, ) into
We solve these equations to obtain the AC-induced nonequilibrium corrections ( and ).
Higgs
↓

## Slide 108
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 109
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 110
and
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 111
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 112
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.
Nonequilibrium corrections due to the Doppler fluctuation of flow

## Slide 113
Then, the complex conductivity is given by
and
AAA cotribution
Instead of showing the rigorous algebraic calculations, we will look at schematic illustrations that represent the final results.

## Slide 114
Complex conductivity formula
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 115
Complex conductivity formula
case
case
Nonequilibrium corrections due to the Doppler fluctuation of flow
No Doppler fluctuation
Higgs
mediated contribution
AAA
contribution
T. Kubo, Phys. Rev. Applied 23, 054091 (2025)

## Slide 116
ac dc
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 117
ac dc
ac dc
Resonance peak due to the Higgs mode.
Already observed in experiments!
S. Nakamura et al.,
PRL 122, 257001 (2019)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)
T. Kubo,
Phys. Rev. Applied 23, 054091 (2025)

## Slide 118
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 119
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Surface resistance
or
quality factor
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 120
Direct AAA photon action
Higgs mediated contribution
The contributions from the nonequilibrium corrections are significant even at low frequencies
Surface resistance
or
quality factor
Kinetic inductance
Significantly contributes to
even at low frequencies
Significantly contributes to
,
even at low frequencies

## Slide 121
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Current dependent
curve
in ac+dc system
dc: arbitrary strength
ac: perturbation

## Slide 122
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
7GHz for Nb

## Slide 123
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:

## Slide 124
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 125
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
Let’s see the orange curves (),which correspond to 7GHz for Nb.
Dotted curve:
Dashed curve:
Re[
Solid curve:
Re[
Significant contribution from
the direct AAA action term

## Slide 126
(dirty)
T. Kubo, Phys. Rev. Applied 22, 044042 (2024)
The current-induced reduction of is pronounced as the frequency increases
The key player is the direct AAA photon action
Big clue to understand the pronounced anti Q-slope with increasing frequency
3.6 GHz for Nb
7 GHz for Nb
14 GHz for Nb
36 GHz for Nb
1.8 GHz for Nb

## Slide 128
The biggest differences between cavities for accelerators and those for quantum applications
photon number
Electric field
distribution
Accelerators
Quantum computing
photon number
K
mK
T. Takenaka, T. Kubo et al.,
arXiv:2510.01819.
T. Kubo et al.,
IPAC2014, Dresden, Germany,
WEPRI022, p.2519