## Slide 1: Mechanisms of nonlinear surface resistance in superconducting cavities
Alex Gurevich
Department of Physics, Old Dominion University, Norfolk VA
Supported by DOE under grant SC 0025560

## Slide 2: Variety of field dependencies of Q(H)
Reentrant shape
Single-cell: 59 MV/m (223 mT) 1.3 GHz at 2 K
53.3 MV/m in 650 MHz single-cell!
Positive Q slope,
high Q and highest
breakdown fields
Negative Q slope,
high Q, reduced
breakdown fields,
usually after infusion
of Ti, N O, or not
Lechner et al,
APL. 119, 082601 (2021)
Dhakal, Ciovati et al.
PR STAB 16. 042001 (2013)
Grasselino et al, FNAL

## Slide 3: Contributions to SRF losses
Intrinsic:
Quasiparticle losses due to thermal dissociation of Cooper pairs, field-dependent Rs(H) of a nonequilibrium superconductor driven by strong rf currents
Extrinsic:
Nonsuperconducting precipitates and surface layers (hydrides, suboxides)
Grain boundaries, arrays of dislocations, impurity segregation on GBs, nonstoichiometric regions
Vortices trapped in the cavity during cooldown through Tc, hotspots on cavity surface
Materials-related subgap quasiparticle states: TLS in surface oxides.
intrinsic (BCS)
extrinsic (residual)
Complex interplay of mechanisms contributing to Q(H) slope and Q(H) rise
BCS and residual parts of Rs depend on frequency, temperature and rf field

## Slide 4: What do we know (or do not know)?
Field limit
The GL theory of dc superheating field Hs(T) is applicable near Tc but not at T << Tc.
Only Hs(0) = 0.84Hc at was calculated (Galaiko 1966, Catelani and Sethna, 2008; Lin and Gurevich, 2012).
at T << Tc and arbitrary has not yet been calculated even in the BCS model.
in the Eliashberg theory has not been calculated at any T.
Dynamic superheating field Hd(T,f). How different can it be from the static Hs(T) at GHz frequencies?
(Sheikhzada and Gurevich, 2020) but at is unknown
Low-field Q limit
Low-field BCS surface resistance Rs(T,f) is well-understood. How far can the residual resistance be decreased? Many contributions to Ri: trapped vortices, subgap quasiparticles, two-level states, proximity-coupled suboxide layers, …..
Complex effects of nonequilibrium superconductivity on Q(H)
Field-dependent RBCS controlled by nonequilibrium kinetics of quasiparticles driven by strong rf current.
Extreme dynamics and nonlinear losses of trapped vortices driven by strong rf current
Multiple mechanisms of negative Q(H) slope.

## Slide 5: BCS surface resistance
Dirty:
normal skin
effect
Clean:
anomalous
skin effect


D.C. Mattis and J. Bardeen, Phys. Rev. 111, 412 (1958)
Vanishes at T 0.
Nb cavities have RBCS  10-20 n
at 2 GHz and 2K
Is the optimal Q at GHz
frequencies and low T
limited by the idealized
BCS surface resistance?
The factor
is minimum at = 20 nm
In the dirty limit of l < ξ, the relation between current density J(r)
and the electric field E(r) is local:
The larger the gap the better:
Nb3Sn has lower RBCS than Nb at low fields

## Slide 6: Broadening the gap peaks in DOS can reduce Rs
Low-frequency surface resistance at 1-2 GHz, hf/kT ≈ 10-2
Idealized
BCS
Broadened gap
peak and subgap
states in the
Dynes model
Density of states with broadened gap peaks:
Rs can be reduced by:
electron-phonon inelastic
scattering
proximity-coupled
metallic suboxides
Dilute magnetic impurities
Optimal inhomogeneities
The BCS log singularity in Rs at is removed by the DOS broadening:
Optimal broadening the gap peaks can reduce Rs by 4-5 times

## Slide 7: Residual surface resistance from subgap states
Gurevich, SUST 30, 034004 (2017)
Gurevich and Kubo, PRB 96, 184515 (2017)
Ri = 10 nohm at 1.5 GHz and nm at
Residual resistance is a part of BCS surface resistance which takes into account the broadening of gap peaks in
Ri increases with but Rs(T) at higher T is decreased by moderate DOS broadening

## Slide 8: Reduction of SC gap and superfluid density by current pairbreaking
Maki, Prog. Theor. Phys. 29, 10; 333 (1963);
Fulde, Phys Rev. 137, A783 (1965)
clean
dirty
The effect of current on the DOS:
Gap singularities are smeared out
The quasiparticle gap is smaller
than , both and
decrease with H
Clean limit: the gap vanishes at H < Hs
Dirty limit: the gap remains finite at Hs
Supercurrent density reduces the
density of Cooper pairs
Supercurrent reduces the SC gap
Lin and Gurevich, PRB 85, 054513 (2012)
The gap reduction with H
does not mean that Rs(H)
always increases with H:

## Slide 9
Current-induced broadening of DOS peaks causes a negative Q(H) slope
Subgap states caused by finite quasiparticle lifetimes.
Surface layer of reduced BCS pairing constant (surface nonstoichiometry)
Proximity coupled thin normal (suboxide) layer on the surface
Small density of magnetic impurities
S
N
magnetic
impurities
Gurevich, PRL 113, 087001 (2014)
Gurevich and Kubo, PRB 96, 184515 (2017)
Kubo and Gurevich, PRB 100, 064522 (2019)
Gurevich, SUST 36, 063002 (2023)
Calculations of Rs in the dirty limit
based on the Usadel equations
Engineering optimal DOS broadening by pairbreaking mechanisms
Current-induced DOS broadening
DOS oscillating under RF currents
Reducing Rs by engineering an optimum DOS by surface nanostructuring and impurity management
Surface resistance can be reduced by RF current, surface nanostructuruing and magnetic impurities

## Slide 10
DOS broadening
Tc suppression
Gurevich and Kubo, PRB 96, 184515 (2017)
Reduction of Rs by magnetic impurities and interface resistance
optimum DOS broadening
Proximity effect increase of Rs

## Slide 11
Negative and positive Q slopes caused by current pairbreaking
Negative Q slope can appear
due to current-induced DOS
broadering
Negative and positive
Q slope can be changed
by materials treatment
Equilibrium
Change the suboxide thickness
Change N/S diffusivity ratio by impurities
Kubo and Gurevich,
PRB 100, 064522 (2019)

## Slide 12
1.3 GHz
1.5 GHz
3 GHz
Dhakal, Khanal, Gurevich, Ciovati, PR-AB 27, 062001 (2024)
Consistent with the earlier FNAL results
Martinello et al PRL 121, 224801 (2018).
What does the experiment say?
Negative Q slope becomes more pronounced as the frequency increases.
Negative Q slope becomes more pronounced as the temperature decreases.
Strong nonequilibrium effects at low T
Likely caused by nonequilibrium SC
but can trapped vortices do it too?

## Slide 13: RF dissipation of a trapped vortex in a random pinning potential
Numerical simulation of nonlinear dynamics of a curvilinear elastic vortex driven by strong RF current
Mesoscopic effects in RF response for different pinning configurations
LO instability in the presence of surface, bulk and cluster pinning
Vortex losses as function of frequency and rf field have been calculated.
Pathirana and Gurevich, PRB 101, 064504 (2020);
PRB 103, 184518 (2021)

## Slide 14: Residual resistance due to trapped vortices
Residual resistance increases with field due to depinning of vortices
Residual resistance increases with frequency: (weak pinning), (strong pinning)
At lower frequencies trapped flux gives dominant contribution to Rs as compared to
Contribution of Ri(H,f) can reverse the NQS as the frequency decreases
Can the NQS also come from trapped vortices?
rf depinning
weak pinning
strong pinning
viscous losses
pinning
hysteretic losses

## Slide 15: What happens to the vortex drag at high velocities?
Slow vortex
Fast vortex
v
v
Velocity-dependent Larkin-Ovchinnikov vortex drag:
A nearly round vortex core
Cloud of dissipative quasiparticles is
locked onto the moving core
Bardeen-Stephen vortex drag
TDGL simulations show that the fast vortex core stretches along v
A cloud of nonequilibrium quasiparticles lags behind a fast vortex core
Decrease of the drag force with velocity can cause
runaway acceleration of the vortex above a threshold current

## Slide 16: Velocity dependence of vortex drag
Reduction of the vortex drag due to diffusive depletion of quasiparticles in the moving core
LO critical velocity:
Larkin-Ovchinnikov mechanism
Larkin and Ovchinnikov. JETP 41, 960 (1975)
Electron overheating
The drag coefficient depends on the electron temperature Tv of the vortex
Power balance:
Thermal conductivity contains both quasiparticle and phonon contributions
Solving for Tv yields the LO vortex drag with v0(T) decreasing as T decreases:
Bezuglyj and Shklovskii, Physica C 202, 234 (1992)
Kunchur, PRL 89, 137005 (2002)
Gurevich and Ciovati, PRB 77, 104501 (2008)
The energy relaxation time due to scattering on phonons:
Hence, decreases as T decreases of the
the impurity density increases

## Slide 17: Larkin-Ovchinnikov instability
Balance of drag and Lorentz forces for a vortex:
Observations on different materials:
Musienko et al, JETP Lett. 31, 567 (1980); Klein et al., JLTP 61, 413 (1985);
Amenio et al, PRB 76, 054502 (2007); Grimaldi et al, J Phys C97, 012111 (2008);
Villard et al, JLTP 131, 957 (2003); Doettinger et al, PRL 76, 1691 (1994) ;
Samoilov et al, PRL 75, 4118 (1995); Bezuglyj et al PRB 99, 174518 (2019)
Runaway acceleration of a vortex at v > v0 , jumps on V-I curves
dc transport
in Nb films:
Peroz and Villard,
PRB 72, 014515 (2005)
The LO critical field decreases as T decreases:
In In Nb km/s near Tc and decreases as T decreases.

## Slide 18: LO nonlinear drag of a trapped vortex
What happens to the vortex if its supersonic tip driven by rf current is LO-unstable while the rest of the elastic vortex is LO-stable?
Field dependence of RF residual surface resistance caused by
trapped vortices with nonlinear LO drag?
H(t)
u(z,t)
LO
unstable
LO
stable
At mT the superflow velocity of Cooper pairs in Nb reaches the pairbreaking threshold
Terminal velocity of the vortex tip at the pairbreaking limit:
For Nb, vd = 10 km/s exceeds both the speed of sound (2-4 km/s) and vc = /pF = 1 km/s. Velocities = 10-20 km/s were observed by Embon et al. Nature Comm. 8, 85 (2017); Dobrovolsky et al, Nature Comm. 11, 2391 (2020).
Since km/s is 10-102 times smaller than vortex velocities at H = 10 -100 mT, the LO nonlinearity of is essential for SRF.

## Slide 19: Residual resistance with the LO drag
Fit to the experimental data
for a 1.47 GHz Nb cavity
Ciovati, JAP 96, 1591 (2004)
The control parameter
The initial Ri(H) rise at low H is
followed by Ri(H) drop due to
the LO reduction of vortex drag.
Negative Q slope from Ri (H) which
gets more pronounced as:
Frequency is increased
Temperature is decreased
Surface gets dirtier
Suppressed by overheating
if flux density is too high
f0 = 22 GHz for dirty Nb with nm.
Pathirana and Gurevich, PRB 101, 064504 (2020);
PRB 103, 184518 (2021)

## Slide 20: Conclusions
Interplay of even two basic mechanisms: current-induced DOS broadening and nonlinear rf losses of trapped vortices can produce a great variety of Q(H) behaviors tunable by materials treatments
Negative Q slope:
The DOS broadening by rf current in RBCS(H) (weakens as lower temperatures and higher frequencies)
The LO reduction of vortex drag with velocity (gets stronger at lower temperatures and higher frequencies)
Can be suppressed by overheating at high flux density
At low frequencies, the raising Ri(H) can overwhelm the decreasing RBCS(H) and reverse the Q slope
These predictions are consistent with experiments, but how do we know that the NQS is not coming from nonequilibrium kinetics of quasiparticles driven by strong rf fields?
Separate the thermally-activated RBCS(H) from the residual Ri by doing the Arrhenius plots in a broad
range of T and f. Detailed Q(H,T,f) measurements below 1.5K in a dilution fridge can show which component of Rs gets dominant upon increasing f and decreasing T.
But different frequencies imply different cavities with different surface properties and trapped flux.