## Slide 1: First Beam Test of Nb3Sn Cryomodule Gray Enid I at UITF and Next Steps
November 12, 2025
Rongli Geng
SRF Frontier Workshop, Nov 12-14, 2025, Jefferson Lab
Notes: Tip: Keep titles under 60 characters for readability
To change the photo: Right-click on photo and select change photo

## Slide 2: Outline
Introduction
UITF facility and cryomodule/cavity design
Cryomodule preparation and check out
Beam acceleration test results
Next steps
Conclusion
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets

## Slide 3: Introduction
Nb3Sn cavity development at JLAB started in 2010
  DOE BES inverse Compton light source development
  DOE NP Advanced Technology Research and Development
Major boost due to DOE NP ECA to Grigory Eremeev in 2016
  Aim to develop Nb3Sn coated 5-cell CEBAF-style cavities
Demonstration of two 5-cell CEBAF-style Nb3Sn coated cavities in a CEBAF-style quarter cryomodule in 2024
  13 MV/m and 8 MV/m
  Cavity coating at FNAL & JLAB
Nb3Sn cryomodule dedication Nov 2024
  Gray Enid I
G Eremeev et al 2025 Supercond. Sci. Technol. 38 07LT01
DOI 10.1088/1361-6668/ade82d
Cryomodule performance test at CMTF
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets

## Slide 4: Gray Enid I Beam Acceleration Testing at UITF
Upgraded Injector Test Facility (UITF): a test bed that can be quickly reconfigured for testing new accelerator technologies.
  Test cryomodules, RF cavities, photocathodes, and polarimeters.
  Provide venue to perform low energy physics experiments with polarized electron beam.
200 keV beam from photocathode in DC gun.
Laser pulse length 35 ps, rep rate 1497 MHz nominal and adjustable
Cryomodule interfaces
  Cryomodule installation and connection to beamline
  RF waveguide connection to upstairs 5 kW Klystrons
  Cryogenic lines connection to Cryogenic Test Facility
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 5: Cryomodue and Cavity Design
An existing CEBAF-style quarter cryomodule
https://proceedings.jacow.org/srf87/papers/srf87a09.pdf
https://proceedings.jacow.org/SRF91/papers/srf91a02.pdf
Two CEBAF-style 5-cell cavity (new cavity cells)
F. Marhauser et al., JLAB‐TN‐17‐055
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 6: Cryomodule Cooldown
Ambient magnetic field in cavity space monitored with two fluxgate magnetometer.
  < 5 mG
Slow cooldown with uniform temperature distribution across the length of the cavity pair during the normal conducting to superconducting transitioning period.
Magnetic fluxgate and Cernox sensors for monitoring ambient magnetic fields and controlling the cooldown process.
T2
T1
Requirement: T2-T1 <= 0.3 K
Staring time: When T1 reaches 18.5 K
Ending time: When T2 reaches 17.5 K
After T2 is lower than 17 K, cooldown can proceed at larger rate
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 7
Best Achieved Delta_T 0.17 K
Process optimization
Understanding attributes of the integrated system of cryomodule, cryo-lines, and cryo-plant

## Slide 8: Cryomodule Cold Checkout
 | Unit | Cavity 1/ Upstream Cav | Cavity 2/Downstream Cav
Landing frequency at 4K | MHz | 1496.545 | 1496.405
Qext – Incident RF power coupler | - | 1.37E7 | 1.75E7
Qext – Field probe | - | 5.13E11 | 9.18E11
Emax, 4 K | MV/m | 11.8 | 7.4
Eops, 4 K | MV/m | 11.3 | 7.0
Emax, 2 K | MV/m | 12.6 | 7.5
Eops, 2 K | MV/m | 11.0 | 7.0
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 9
4 K Q0 1-2E9 at low field
  Measurements done post certain number of quench events during the initial power rise for determining Emax
  0.17 K Delta_T cooling across Tc
A 30 K thermal cycle was carried out, larger 4 K Q0 values were then observed: 3-4E9 at low field
  0.33 K Delta_T cooling across Tc

## Slide 10
Helium pressure fluctuation at 4 K peak-to-peak 45 Torr
  3.2 Torr at 2 K
Filter fit of detuning against pressure gives df/dp = 19 Hz/Torr for upstream cavity (cavity 1)

## Slide 11
Fast detuning with “slow” detuning from pressure removed: peak-to-peak 575 Hz for upstream cavity
Fourier transform spectrum reveals the leading mode at 113 Hz.

## Slide 12: Beam Acceleration Test at UITF
Metric | Value
Beam energy | 6.9 MeV
Cavity 1 Eacc | 10 MV/m
Cavity 2 Eacc | 6 MV/m
Metric | Value
Beam energy | 5.1 MeV
Cavity 1 Eacc | 7 MV/m
Cavity 2 Eacc | 4 MV/m
2 K
4 K
Beam spot on viewer
Beam cross-section profiles
Both cavities tuned by ~ 50 kHz to common frequency of 1496.500 MHz. Laser pulse rate at 1496.500 MHz as well
Cavity 1 compressed by tuner
Cavity 2 stretched by tuner
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 13
Beam energy was measured with varying cavity gradient set point at 2 K
  Cavity 1 held at fixed gradient and phase
  Cavity 2 gradient and phase scanned
Cavity phase was optimized for maximum beam energy
Simulation results are compared with experimental results
  Field map by ACE3P
  Beam dynamics by GPT

## Slide 14
Cavities regulated by LLRF for amplitude & phase
  Cavity phase instability problem was initially encountered and more pronounced at 4 K relative to 2 K
  Apparent correlation with fast helium bath pressure fluctuations
This problem was mitigated by
  Cryomodule thermal cycle to 30 K followed by uniform cooldown (Delta_T 0.3K)
  Adjustment of JT control and return valve control
  Optimization of tuner step motor control
Cavity gradient capability at 4 K (LLRF regulates only the amplitude)
  Cavity 1: 10 MV/m
  Cavity 2: 6 MV/m
Beam current [nA]
Eacc Cav 1 [MV/m]
Eacc Cav 2 [MV/m]
Cav 1 phase [deg]
Cav 2 phase [deg]
Helium pressure [ATM]

## Slide 15: Summary of Beam Test Results
Metric | Value |  | Unit
 | 4 K | 2 K | 
Beam energy | 5.1 | 7.1 | MeV
Beam current | 10 | 0.1 | µA
Beam mode | CW |  | 
Bunch rep rate | 1496.500 |  | MHz
Cavity 1 Eacc | 7 | 10 | MV/m
Cavity 2 Eacc | 4 | 6.5 | MV/m
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 16: What’s Next?
Deliver beam for target irradiation experiment in early 2026 with beam energy 5 MeV.
Install Gray Enid II to extend the beam energy to 10 MeV
3 ft
3 ft
3 ft
Gray Enid II
A 3’x3’x3’ box cryomodule with conduction-cooled 3-cell 1.5 GHz cavity cooled by cryo-coolers and powered by a solid-state amplifier
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 17: Conclusion
First electron beam acceleration was accomplished with two 5-cell CEBAF-style Nb3Sn coated SRF cavities hosted in a CEBAF-style cryomodule, Gray Enid I, installed in JLAB’s UITF.
Integration of Nb3Sn cavities and cryomodules in an accelerator systems, including beamlines, high-power RF sources, and cryo-plant went well.
Gradient performance of both Nb3Sn cavities was preserved in UITF accelerator relative to that measured at CMTF. Eacc 10 MV/m with a CW beam current 100 nA was demonstrated at 2 K.
Stable CW beam at 4 K demonstrated with a beam current of 10 µA and beam energy 5.1 MeV with amplitude and phase regulated operation of two 5-cell Nb3Sn cavities at Eacc 7 and 4 MV/m, respectively (previously published record beam acceleration Eacc 2.3 MV/m, Z. Yang et al., SUST 38(2025) 015009).
Unloaded quality factor Q0 3-4E9 demonstrated at low field at 4 K (previously published record 7E7 at 4 K in a 3-cell 8 GHz Nb3Sn cavity, G. Arnolds et al., IEEE Tran. Nucl. Sci., NS26, (1979)3775-73 ).
Plan to deliver beam with Gray Enid I for a target irradiation experiment in early 2026.
Plan calls for installation of a conduction-cooled Nb3Sn cryomodule to double the 4 K beam energy from 5 MeV to 10 MeV by end of 2026
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 18: Acknowledgements
Work presented in this talk is the result of colleagues from several groups in JLAB’s Accelerator Division and Engineering Division.
Special thanks to Matt Poelker, the UITF manager, for his effort in guiding and coordinating the test, Uttar Pudasaini for his outstanding contribution to the Nb3Sn technology development at JLAB and to the following people for their direct contribution for the beam test of Grain Enid I at JLAB’s UITF: R. Bachimanchi, G. Ciovati, J. Creel, M. Drury, S. Dutton, J. Fischer, N. Gale, K. Hesse, L. King, S. Kuzikov, J. Latshaw, G. Marble, J. Musson, P. Owen, T. Plawski, H. P. Wang, S. H. Wang, Y. Wang, M. Weaks, X. Gomez.
Thanks to Grigory Eremeev of FNAL for his leadership in starting the Nb3Sn effort at JLAB, his vision of 4K operation of Nb3Sn cavities at medium gradients, and his continued effort in advancing the two 5-cell Nb3Sn cavities to be successfully tested in a cryomodule at JLAB’s CMTF. Thanks to FNAL colleagues who contributed to the coating and testing of one of the two 5-cell cavities.
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under contract DE-AC05-06OR2317.

## Slide 19: QUESTIONS?
Notes: Before sharing your presentation, confirm:
Fonts are consistent
Images meet quality standards
Charts use template colors
Footer information is current
Spell check completed
Links are working
File size is optimized