## Slide 1: Activities at INFN LASA towards HighQ/HighG
D. Sertore
INFN Milano – LASA
for the SRF group

## Slide 2: Outline
Motivation
  High Q and High G
  Treatment selection
  Industrialization
INFN activities
  PIP-II
  ESSP
Synergies
  ITN
  EPITA
  BriXSinO

## Slide 3: Motivation

## Slide 4: Requirement for future accelerator: HighQ & HighG
Future machines require increasingly high SRF cavity performance -> HighQ & HighG
  HighQ -> power saving
  HighG -> shorter machine
Example of High Q0 e High Eacc (ESS, 704.4 MHz, β=0.67)
Project | Frequency | Cavity type | Emax (MV/m) | Q0
FCC-ee | 800 MHz | 5-cell | 20 | 3.1010
ILC, pulsed | 1.3 GHz | 9-cell | 31.5 | 1.1010
muon collider (base scenario), pulsed | 1.3 GHz | 9-cell | 30 | 
E-XFEL, pulsed / CW E-XFEL | 1.3 GHz | 9-cell | 23.6 / 17 | 1.1010 / 2.1010
PIP-II (low β), from 20Hz to CW | 650 MHz | 5-cell | 16.7 | 2.4.1010
LCLS-II (CW) | 1.3 GHz | 9-cell | 16 | 2.7.1010
Specs for cavities in operational condition (cryomodules)
9-cell 1.3 GHz cavity for ILC Japan
Cavity qualification goal (vertical test) typically 10% higher w.r.t operational goal
As an example, for ILC:
Eacc ≥ 35 MV/m @ Q0 ≥ 1.1010 (qualification)
Eacc ≥ 31.5 MV/m @ Q0 ≥ 1.1010 (operational)
  Sustainability & Cost reduction

## Slide 5: R&D up today
Typical treatments (HighQ/HighG):
  EP cold (best surface finishing)
  High temperature Annealing
    From 800 °C a 900 °C
  Final heat treatment
    Two-step baking
    Mid-T baking
    …but on-going R&D suggests possible improvements (different Ts, etc.)
Mid-T baking
China
PIP-II
Two step baking
US/EU/Japan
baseline
Two-step
Mid-T
Possible treatments
EU (INFN)/US
US
Japan
«New» 200 °C bake treatment

## Slide 6: R&D and industrialization
R&D results vs time & Large Machines
Snapshot: 28 December 2018
Reproducibility over large series
Q0 goal : 2.7x10^10
Vertical Test
LCLS-II
Vertical Test
E-XFEL
280 cavities
800 cavities
R&D (Single and Multi-cells): select “recipes” for performance optimization (cold VT @ 2K)
  Clean room, High pressure rinsing (HPR), Buffer Chemical Polishing (BCP), Electropolishing (EP), low T baking, N doping, 2-step baking, Mid-T baking, etc.
  Optimization of cavity geometry (RF and geometry)
  Field Emission Reduction
Migration to multi-cells and industrialization for large machines: Yield and reproducibility

## Slide 7: INFN LASA Activities

## Slide 8: INFN Milano LASA strategy
The SRF group at LASA is a leader in the field of bulk niobium SRF cavities, with participation in international projects such as European-XFEL, ESS, and PIP-II.
To maintain this excellence, in view of future high-performance accelerators such as lepton
colliders and light machines, it is essential to develop SRF cavities with high Q0 and High G.
Our strategy consists of R&D activities with 1.3 GHz single cells to develop treatments to extend the high Q towards the high gradient required by projects such as ILC, FCC-ee, CePC, Muon Collider, etc.
It is also essential to transfer the recipe to multi-cell cavities for possible large-scale production.
The activities we propose can be summarized as follows:
Development of recipes for high Q/high gradient (high-Q/high-G)
Process transfer to multi-cells
R&D on cavity ancillary systems (tuners, magnetic screens, etc.)
Profit from synergic program as our contribution to PIP-II (high Q) or other international programs.

## Slide 9: PIP-II: INFN contribution
Cryomodule picture is a courtesy of Nicolas Bazin, CEA, France
Low-Beta (LB650, b=0.61) cryomodule
INFN firstly provided a novel RF design for the LB650 cavities, fully plug compatible with the Fermilab technical interfaces and performances specifications.
Cavity design meets the CW RF performance requirements
INFN contribution aims to cover the needs of LB650 section, and this includes:
38 (36+2) SC cavities required to equip 9 cryomodules with 2 spares, delivered as ready for string assembly.
Qualification via vertical cold-test through a qualified cold-testing infrastructure acting as a subcontractor
Compliance to the PIP-II technical management plans and interfaces: System Engineering, Project Review, Quality Assurance and Risk Management.
PIP-II LB650 Project Specifications | 
Acc. Gradient | 16.9 MV/m
Q0 in operation | 2.4 1010
RF rep rate | 20 Hz to CW
b | 0.61
RT
SC

## Slide 10: PIP-II: INFN LB650 cavity challenges
The successful cavity design from INFN-LASA is the result of an interplay of multiple, state-of-the-art competences in electromagnetic, mechanical and technical domains.
PIP-II LB650 cavities are among the key scientifical challenges of the project:
an unprecedented quality factor is required for these resonators.
Accelerating and High-Order Modes must be assessed so that neither instabilities nor additional cryogenic losses are posing critical issues.
PIP-II operational scenario is an uncharted territory in terms of detuning control, and this requires deep understanding of Lorentz Force detuning, pressure sensitivity and mechanical leading parameters as rigidities, yield limits, stresses.
Detailed finite element analysis to ensure compliancy to ASME codes.
INFN LB650 for PIP-II, cold cavity | 
βgeometric | 0.61
Frequency | 650 MHz
Number of cells | 5
Iris diameter | 88 mm
Cell-to-cell coupling, kcc | 0.95 %
Frequency separation π-4π/5 | 0.57 MHz
Eq. diameter - IC | 389.8 mm
Eq. diameter - EC | 392.1 mm
Wall angle – Inner-End cells | 2 °
Effective length (10*Lhc) | 704 mm
Optimum beta βopt | 0.65
Epeak/Eacc @ βopt | 2.40
Bpeak/Eacc @ βopt | 4.48 mT/(MV/m)
R/Q @ βopt | 340 Ω
G @ βopt | 193 Ω
Inner cells stiffening radius | 90 mm
External cells stiffening radius | 90 mm
Wall thickness | 4.2 mm
Longitudinal stiffness | 1.8 kN/mm
Longitudinal frequency sensitivity | 250 kHz/mm
LFD coefficient kext at 40 kN/mm | -1.4 Hz/(MV/m)2
Pressure sensitivity kext at 40 kN/mm | -11 Hz/mbar
Maximum Pressure VM stress at 50 MPa | 2.9 bar
Maximum Displacement VM stress at 50 MPa | 1.5 mm
Last HOM in 3rd monopole passband
LFD frequency shift (blue) and pressure coefficient (red) as a function of external cavity stifness at cold.
Example of FEM structural analyses on LB650

## Slide 11: PIP-II: Latest achievements
Single and 5-cell cavities test results
  5-cell B61-EZ-002 fully treated and tested jointly with FNAL.
    Now available at CEA for the pLB650 CM
  B61-EZ-103 tested at INFN and at FNAL. Data analysis cross-check in progress.
  Single cell tested with full magnetic field compensation to validate cancellation procedure.
LASA test stand update for High-Q measurement
  Upgraded LHe filling line installed, it improves cooldown rate and reduce losses. Expected faster Tc crossing.
  Helmholtz coils for single and multi-cell cavity developed and successfully tested in cryogenic conditions. Dedicated optimization procedure developed and applied during cavity test.

## Slide 12
    Use of single-cell and multi-cell cavities at 1.3 GHz in bulk Nb
  2 Single cells: study and development of surface and thermal
    Mechanical production (Production is on-going)
    Baseline treatment (Eu-XFEL optimized with EP cold and 900 °C)
    Innovative treatments (two-step baking, mid-T baking, etc.)
    2K testing at LASA; cross-checking in other international laboratories (e.g., CEA)
  2 Multicells: migration of treatment identified for industrialization
    Mechanical fabrication
    Reproducibility of treatments and robustness verification
    Upgrade of the SRF system for LASA cold VT:
  New cryostat for cold vertical testing (2K) of single cells:
    Lower LHe consumption, reduced test duration, fast transition to 4.2K
    Implementation for active magnetic field cancellation (Helmholtz coils)
    Sensors for diagnostics
  New cold vertical test acquisition system (2K):
    1.3 GHz amplifier
    From analog to digital (PLL design completed)
INFN LASA R&D Activity Plan

## Slide 13
Dedicated cryostat
  L = 3000 mm, OD 610 mm
  Useful volume 730 liters
  Specific design for 1.3 GHz cavity
  Cold testing up to 2 single cells or one 9-cell.
  Overall faster test cycle time
  ¼ of total liquid helium inventory required (w.r.t. to present cryostat)
Dedicated insert
  Optimized cavity installation and removal process
New Cryostat for Cold Vertical Testing
Test Configuration

## Slide 14
2 frames for Helmholtz coils
Spacers between screen and cryostat to secure the structure
Spacers between the 2 frames to adjust their height
Support structure for positioning and handling the coils L 2000mm
Material for the coil windings
Cryostat
Cryoperm shield
Helmholtz coils support structure
Helmholtz coil frame design

## Slide 15
  Magnetic screen already available (L=2500 mm, ID 680 mm)
  Characterization of current screen
  Triaxial measurements of residual field (on axis and at equatorial positions)
  Optimizations underway using high mu materials
  Modification of bottom (plate)
  Closing plate machining
  Firing to restore high μ
  Characterization of modified screen
  Triaxial measurements of residual field
  Optimization of shielding efficiency
External Magnetic Shield

## Slide 16: Synergies

## Slide 17
ILC Technology Network (ITN)
Belong to ILC IDT, ITN is a network that collects labs/institutes from Asia, US and EU whose final goal is R&D in three technical areas: SRF, Sources, Beams
March ’23: budget approved by Japan; KEK-CERN agreement: signed in July 2023
Activities scheduled 2023-2026
ITN-EU main activities (coordinated by CERN)
INFN Milano LASA involved in WP1 (cavity production) and WP2 (cryomodule design) for:
  Treatments targeted to ILC goal (single and 9-cell cavities) towards industrialization with qualified vendors
  Harmonization of pressure vessel codes (PED/ASME/HPGS)
  Fine Grain and Mid Grain Nb studies for cost reduction
  VT and diagnostics at cold in a dedicated cryostat
  Assembly at KEK of an ILC cryomodule with 2 EU cavities
ITN-EU
International Technology Network - Europe
WP1 & WP2 EU partners: CEA, CERN, CEA, DESY, INFN

## Slide 18
ITN-EU: R&D strategy from 1-cells to 9-cells (1.3 GHz)
Single-cells for R&D studies of the “best recipes” for ILC
  Baseline (Eu-XFEL modified) on FG and MG cavities -> only one industry (mechanical and baseline) for trustable comparison in performances
  Only FG will be later used for “new” recipes studies
  Mid-T, two-step baking and their combination -> Optimization of parameters (EP cold, T-treatments) -> Cold VT cross check between labs
  Migration to MG for cross-check performances of the “best” recipe
9-cells for industrialization
  Best recipe will be migrated to 9-cell FG cavities:
  EU industries will be involved
  HPGS requirements must be fulfilled
  Final goal -> install two EU cavities in the ILC cryomodule planned at KEK
Active participation also in:
  Cryomodule activities, string assembly, development of diagnostics, and cryomodule test
900°C HT for better flux expulsion
Cold EP with 2-step baking may help to improve cavity performance
Mid-T at 200°C could reach a higher gradient and is promising for in-situ treatment
Mid-T at 300°C -350°C in combination with 2-step baking

## Slide 19
ITN-EU: Single-cell R&D activity, status and goal
Material procurement and ECS (Nb):
Done
Mechanical production and treatments:
  Specs prepared by CEA-INFN-CERN (treatments as option)
  Order (mechanical + baseline) placed in industry (RI) in March 2025
  2 single-cell cavities mechanical fabricated in September 2025
  Baseline treatment of FG & MG cavities will start soon at RI -> expected within the end of November 2025
  Cross-check of performances at 2 K -> MG/FG comparison
  FG treated with most promising recipes (mid-T at low temperature & a combination of mid-T and low-T baking)
  NEXT STEPS:
  R&D on FG single-cell will continue for fine tuning of the best recipe
  MG/FG performance comparison (best recipe)
  OUR STRATEGY:
  Quality Control (QC) used for large series production applied also on single-cells fabrication and treatment (in view of the industrialization)
  Treatments will be done preferable at industries (industrialization goal)
  Part of the activities could be done in ITN-EU labs (VT, HPR, cleaning and final assembly operation, annealing, etc.).
  CEA/INFN responsible of the technical support at industry
MG
FG

## Slide 20
ITN-EU: 9-cells industrialization goals, strategy, status
ITN-EU main goals for 9-cells cavities:
Production of 9-cells jacketed cavities at the EU Industries (RI and Zanon)
  Material procurement and ECS
  Mechanical specs prepared by KEK-CEA-INFN (treatments as option)
  Tender underway (ends on November 21), started just after KEK one (2 cavities at RI, mech. fab.)
  Order expected in December
Qualification of EU Industries in term of pressure vessel code (harmonization with HPGS)
Installation into the ILC type cryomodule of 2 EU cavities
Timescale and strategy:
  To accomplish the timescale, our priorities are:
    produce and prepare (best recipe) 2 (+2) 9-cells cavities, check of performances (VT cross-check)
    deliver 2 surface treated cavities to KEK for jacketing phase within Oct 2026
      CEA-INFN will follow the jacketing process at KEK, HPGS qualification, string assembly operation, and participate to cryomodule test
    remaining 2 naked cavities will be jacketed in the EU industries and qualified in term of HPGS, VT used as cross-check of the jacketing process
        Even if they will not be installed into ITN cryomodule, this step is needed to qualify the industrialization process

## Slide 21: EPITA Enabling Partnerships for Innovation & Accelerator Technology Advancement
HORIZON-INFRA-2025-01 Proposal for a 4 years program – Decision expected in Spring 2026
“EPITA is a consortium of 43 beneficiaries from 16 countries with a total budget exceeding €21 million, funded by a €10 million EU contribution and over €11 million in matching funds. The project's main goal is to integrate various research and development initiatives into a coordinated, vision-driven program, aligned with the established roadmap for accelerator research infrastructures (RIs). EPITA is structured around three key technology tracks: Accelerating Systems, Magnets and Beamlines, and Frontier Technologies”

## Slide 22: EPITA – SRF related Work Packages

## Slide 23: WP Detailed Structures
Strategy and Industrialization
Horizontal Cavity Integration and RF tests
1.3 GHz Cavity Production and Coating
Superconducting Thin Film Development
WP 4.1
WP 4.2
WP 4.3
WP 4.4
Surface preparation for High-Q at High-G
HPR and Cleanroom Assembly Improvements
Performance preservation and recovery
Test and Diagnostics
WP 10.1
WP 10.2
WP 10.3
WP 10.4

## Slide 24: BriXSinO Brilliant Source of X-Rays Based on Sustainable and Innovative Accelerators
A “newly” conceived scheme of ERL with counter propagating beams is proposed in BriXSinO.
This scheme allows:
  ERL operation
  two-pass operation: the beam is reaccelerated when reinjected in the accelerating module (low current)
The importance of the full BriXSinO is then twofold.
  a test facility for fundamental questions of accelerator physics and strategies of Dynamics and Energetic by maximizing the energy sustainability and minimizing the AC power consumption.
  A user facility by providing large quality coherent THz and X-Rays emission from its high brightness accelerated electron beam, enabling important and advanced applications.
Parameter | two-pass acc. | ERL
Energy (MeV) | 80 | 45
Bunch charge (pC) | 100 | 100
Repetition rate (MHz) | 0.9286 | 92.86
Average Current (mA) | 5 10-3 | 5
Beam power @ dump (W) | 22.5 103 | 400
enx,y (mm − mrad) | < 1.6 | < 1.6
Energy spread (%) | < 0.2 | < 0.2

## Slide 25
... BriXSinO aims at developing at INFN LASA laboratory a test-facility that would enable addressing the physics and technology challenges posed by the ERL generation ...
Activities for BriXSinO
HB2TF – A 5mA 300 kV DC gun injector with photocathode and bunchers
Superconducting Booster Conceptual design of a 3, two-cells 1.3 GHz cavities Superconducting module
Superconducting Linac Conceptual design of a 3, 7-cells 1.3 GHz cavities SC module for ERL and two-pass acceleration
BriXSinO Parameters | 
Beam Current Max | 5 mA
Bunch Charge | 50 pC
ERL energy | 45 MeV
Two-pass energy (5 uA) | < 80 MeV
SCB Cavity | 
Q0 | 2 1010
Eacc [MV/m] | 7.5
QL | 1.5 106
SCL Cavity | 
Q0 | 2 1010
Eacc [MV/m] | 16.5
QL | 3.25 107

## Slide 26
Staff exchange network for accelerator R&D within elementary particle physics
  Exchange between:
    EU labs/university and US-Japan labs/universities
    EU labs/university and EU industries
  started in March 2023, 4 years duration
  Six WP
INFN responsibility WP2 (L. Monaco, co-leaded with E. Cenni CEA):
  State-of-the-art high-gradient, high-efficiency, reduced-cost radio-frequency structures and power Sources
INFN in other WPs: WP1 (R&D&I at currently operating state-of-the-art accelerator facilities); WP4 (Sustainable technologies for scientific facilities); WP5 (Investigation of potential early applications of novel and advanced technologies for colliders)
Marie Skłodowska-Curie Actions Staff Exchanges
EAJADE
Deliverables

## Slide 27: LASA SRF Group: expertise and experience in SRF
E.M. Design
Mechanical DEsign
Prototypes
2K Vertical Test
Series Production
SRF cavity from design to series production
SRF cryomodule components developments
Contribution to International Projects
Cavity String
Cold Mass
Tuner
Cryomodule
S1- Global
VT bunker

## Slide 28
ACKNOWLEDGEMENT
“This work was partially supported by the European Union’s Horizon Europe Marie Sklodowska-Curie Staff Exchanges programme under grant agreement no. 101086276.”

## Slide 29
Thanks for your attention. Questions?

## Slide 30
ITN-EU: R&D strategy from 1-cells to 9-cells (1.3 GHz)
Single-cells for R&D studies of the “best recipes” for ILC
  Baseline (Eu-XFEL modified) on FG and MG cavities -> only one industry (mechanical and baseline) for trustable comparison in performances
  Only FG will be later used for “new” recipes studies
  Mid-T, two-step baking and their combination -> Optimization of parameters (EP cold, T-treatments) -> Cold VT cross check between labs
  Migration to MG for cross-check performances of the “best” recipe
9-cells for industrialization
  Best recipe will be migrated to 9-cell FG cavities:
  EU industries will be involved
  HPGS requirements must be fulfilled
  Final goal -> install two EU cavities in the ILC cryomodule planned at KEK
Active participation also in:
  Cryomodule activities, string assembly, development of diagnostics, and cryomodule test
900°C HT for better flux expulsion
Cold EP with 2-step baking may help to improve cavity performance
Mid-T at 200°C could reach a higher gradient and is promising for in-situ treatment
Mid-T at 300°C -350°C in combination with 2-step baking
H. Ito doi:10.18429/JACoW-SRF2021-FROFDV01

## Slide 31
ITN-EU: R&D strategy from 1-cells to 9-cells (1.3 GHz)
Single-cells for R&D studies of the “best recipes” for ILC
  Baseline (Eu-XFEL modified) on FG and MG cavities -> only one industry (mechanical and baseline) for trustable comparison in performances
  Only FG will be later used for “new” recipes studies
  Mid-T, two-step baking and their combination -> Optimization of parameters (EP cold, T-treatments) -> Cold VT cross check between labs
  Migration to MG for cross-check performances of the “best” recipe
9-cells for industrialization
  Best recipe will be migrated to 9-cell FG cavities:
  EU industries will be involved
  HPGS requirements must be fulfilled
  Final goal -> install two EU cavities in the ILC cryomodule planned at KEK
Active participation also in:
  Cryomodule activities, string assembly, development of diagnostics, and cryomodule test
900°C HT for better flux expulsion
Cold EP with 2-step baking may help to improve cavity performance
Mid-T at 200°C could reach a higher gradient and is promising for in-situ treatment
Mid-T at 300°C -350°C in combination with 2-step baking
H. Ito doi:10.18429/JACoW-SRF2021-FROFDV01
L. Steder et al., arXiv:2407.12570v1 [physics.acc-ph] 17 Jul 2024

## Slide 32
ITN-EU: R&D strategy from 1-cells to 9-cells (1.3 GHz)
Single-cells for R&D studies of the “best recipes” for ILC
  Baseline (Eu-XFEL modified) on FG and MG cavities -> only one industry (mechanical and baseline) for trustable comparison in performances
  Only FG will be later used for “new” recipes studies
  Mid-T, two-step baking and their combination -> Optimization of parameters (EP cold, T-treatments) -> Cold VT cross check between labs
  Migration to MG for cross-check performances of the “best” recipe
9-cells for industrialization
  Best recipe will be migrated to 9-cell FG cavities:
  EU industries will be involved
  HPGS requirements must be fulfilled
  Final goal -> install two EU cavities in the ILC cryomodule planned at KEK
Active participation also in:
  Cryomodule activities, string assembly, development of diagnostics, and cryomodule test
900°C HT for better flux expulsion
Cold EP with 2-step baking may help to improve cavity performance
Mid-T at 200°C could reach a higher gradient and is promising for in-situ treatment
Mid-T at 300°C -350°C in combination with 2-step baking
H. Ito doi:10.18429/JACoW-SRF2021-FROFDV01
L. Steder et al., arXiv:2407.12570v1 [physics.acc-ph] 17 Jul 2024
HZB