## Slide 1: Superconducting Thin Film Development for Microelectronics
A versatile platform around NbTiN
11/12/25
Anne-Marie Valente-Feliciano
Notes: Tip: Keep titles under 60 characters for readability
To change the photo: Right-click on photo and select change photo

## Slide 2: Motivation
Leveraging Next-Generation SRF Materials Developments for SRF cavity materials based on thin film technologies.
Beyond cavity applications, the developments in SRF thin film technologies find a variety of applications in the fields of superconducting metamaterials, electronics, sensors and quantum devices.
Unifying theme across these technologies is that the same physics and material properties such as extreme low loss, stability, and manufacturability are required.
NbTiN film based structures
Functionalization of SRF Materials

## Slide 3
Superconducting Digital Logic (SCD): Main Goals
Support the on-going development of quantum and classical superconducting electronics and complement R&D program on superconducting fabrication stack consisting of several metal layers by exchanging information, samples and/or complementary characterization.
Main research vision = develop a deep-submicrometer, scalable superconducting process for future generations of computing hardware for ultra-high-compute-density and high-energy-efficiency superconducting autonomous AI systems with ExaScale performance.
New fabrication process to enable dense logic and memory, and inform performance architectural optimizations on the hardware- software level.
Develop improved superconducting and barrier materials that perform better and tolerate higher processing temperatures, making them fully compatible with the fabrication processes of conventional electronics technology.
Proposed backend process based on NbTiN wires recently introduced by the quantum and RF superconducting communities.

## Slide 4: Superconducting Digital Logic (SCD)
CMOS
technology
High power
dissipation
RC Delay
Thermal
Limitations
SCD
Low power dissipation
High speed
operations
Cryo-
temperature
100x faster execution time
Interconnect bandwidth
1000x compute density
Emersion cooling, 3DHI
100x energy efficiency
Zero resistance, JJ
Classical technology leveraging CMOS EDA, process flow, and packaging

## Slide 5: Superconducting Digital Logic (SCD)
Bridging the gap from CMOS to Quantum Superconducting Digital Logic based on NbTiN
AI & Quantum Compute Loads Sustainable with Advanced Superconducting Integration Process
From a football field to a shoe box
The same performance as NVIDIA EOS: 79.32 ExaFlOPS
18 Trillion devices 150 x 320 x 100 mm

## Slide 6: Superconducting Digital Technology: Focus Areas
40/28 nm design rules for fabrication
Scalable fabrication (300mm wafers)
Standard processes
Compatible BEOL thermal budget
Scaling path  N+2
 Fundamentals and failure mechanisms
“Re-starting Moore’s law”
4 chips/die
7.8mmx7.8mm dies
241 dies/wafer

## Slide 7
Base Material: NbTiN
ACCELERATE SCD
The uncertainties are underestimated, but linear behavior is very clean.
b is the linear coefficient of the fits.
Tc = 17.2 K in both field directions
Hc1 = 70 mT
Hc2(0) ~12-13 T
Δ= 3.1 meV
SQUID meas – RAL & KU Leuven
PCT meas – CEA Saclay
2µm NbTiN (001)/MgO(001)
Tc~17.25 K
TEM at NbTiN/MgO interface

## Slide 8: Preliminary Results on NbTiN Wires
SEM images of two metal layers with 50 nm critical dimension.
Anna Herr, et al. ,arXiv:2303.16792 [physics.app-ph]
Images in a single cooldown in 12 µT field (a) and average across 50 cooldowns (b-c) of a 20 µm-wide, 100 nm-thick strip show grouping of vortices along the center of the strip with 42% trapping probability per site. d)-f) Similar data for a 50 nm-thick strip field-cooled in 14 µT. Preferred trapping sites here include locations near the edge of the strip indicating more defectivity. g) Low-field images of a 180 µm x180 µm NbTiN film with 0.5 µm moats spaced 20 µm in a single cooldown (top) and average across 15 thermal cycles (middle). Extracted locations of vortices (bottom) show 100% trapping probability in the holes.
Images of field-cooled NbTiN patterned films
Number of vortices as a function of applied field in 10 µm strips fabricated from 50 nm and 100 nm-thick films

## Slide 9: Superconducting Digital Technology: the Vision
Optical
Network)
Copper
Plate (12K)
Copper
Plate (4K)
Copper
Plate (77K)
Optical
Network)
FP2
M6
M5
MF
M4
M3
M2
M1
M0
GND
MP5
MP4
MP3
MP2
MP1
FP1
Design, Automation and Test in Europe Conference (DATE2025 on Arxiv)
Superconducting interposer (4K)
Superconducting compute stacks
Superconducting network stacks
Glass bridge/ thermal break
4K-77K link
Cryo-CMOS interposer (77K)
Cryo-DRAM
Cryo-optical modulators
Tech & process
Device/component
Integrated Circuits
Architecture
System

## Slide 10: Superconducting Digital Technology: Focus Areas
Tech & process
Device/component
Integrated Circuits
Architecture
System
16ML stack vision to enable scalable superconducting digital technology
FP2
M6
M5
MF
M4
M3
M2
M1
M0
GND
MP5
MP4
MP3
MP2
MP1
FP1
Flux trapping layer
Flux trapping layer
Superconducting BEOL
(wires & vias)
AC Power delivery network
(tunable capacitors)
Superconducting FEOL
(JJs)
Full NbTiN platform
420°C budget
> 13 K
High
Stoichiometry

## Slide 11: Superconducting Digital Technology: Focus Areas
FP2
M6
M5
MF
M4
M3
M2
M1
M0
GND
MP5
MP4
MP3
MP2
MP1
FP1
Flux trapping layer
Flux trapping layer
16ML stack vision to enable scalable superconducting digital technology
M5
M1
V1
M2
SiN
SiOx
40nm
Wires & vias
100nm
αSi
M1’A’
M2
M1’B’
V1
CD 330nm
CD 130nm
CD 500nm
HZO
SiN
SiOx
50nm
M1’A’
M1’B’
HZO MIMCAP
Moats & flux trapping structures
α-Si barrier JJs
Tech & process
Device/component
Integrated Circuits
Architecture
System

## Slide 12: Superconducting Digital Technology Scale-up
Material set B, PCM, resonators
Material set
&
Process flow defined
Material and process flow development
Integration
2 & 5 ML stack, failure modes vehicles
Material set A, PCM, resonators
Imec VZW
NYCreates
JJ with integrated transfer, UPD scaling
Design, test, performance modeling
NYCreates
Validation optional
Test functional vehicles
UPD scaling, knowledge transfer
NbTiN optimization by EC, material science, advanced experimental techniques
Jefferson Lab
Integrated stack defined.
Imec USA
NYCreates
imec
imec
NbTiN, Si, HZO
NbN, NbTiN
Material science, advanced experimental techniques
Cornell
7 ML stack characterization complete: density, power, failure modes
Demo Design & Test:
5ML stack meets material specifications
Unit processes characterization complete, PDK alpha.

## Slide 13: NbTiN Engineering/Flavor Portfolio
Single-target, 7nm
Single-target, 200nm
Single-target, 200nm
(annealed at 650C)
<001>
<110>
<111>
Single-target, 200nm
50nm on SiO2
200nm on SiO2
50nm on Si
Crystallinity (XRD)
Grain size (PED)
Roughness (AFM)
Stress (bow/Stoney)
Stoichiometry (RBS/ERD)
MT
ST
ST Low N
C
E
C
E
C
E
(111)
(200)
Transfer research lab development to Nanoelectronics research hub to develop processes for foundries

## Slide 14: 1ML BEOL electrical testing
CD lines:
Width: 70 nm
Meanders:
Width: 70 nm
CD lines:
Width: 70 nm
Length: 10 um
Wafer distribution
50nm S-T
200nm S-T
Wire electrical measurements are in line with film properties

## Slide 15: 3ML BEOL
Wires with width scaled down to 50nm (yield >95%)
Uniform distribution of Nb, Ti and N with clean O-free interfaces
Optimized via etch and Ar pre-clean for optimal via filling QA
M3
M2
M1

## Slide 16: Electrical testing
Critical current dependence on length, etch, and temperature
Process generation
2024
2025
B. Hodges et al., IITC 2025

## Slide 17: Josephson Junctions (JJ) fabrication flow
17
Base Patterning
Via Etch and Fill
Top Patterning
Stack Deposition
JJ Etch
NbTiN
aSi barrier
HM SiN
HM SiOx
Thermal SiOx
ALD SiOx
Si substrate
Encapsulation SiN
NbTiN
aSi
NbTiN
HM SiN
SiN encap
HM SiOx
JJ
Base
New stack: NbTiN/aSi/NbTiN
Litho: 193i (210nm CD)
Process: PVD & etch

## Slide 18: Cryogenic performance
Typical nonhysteretic behavior corresponding to low capacitance and IcRn of ~1.1 mV
Ic between 27-55 μA corresponding to Jc of 0.8 mA/μm2 and scales with device area
A. Pokhrel et al.,
IEDM 2024

## Slide 19: Cryogenic performance
Critical current density scales with Si
Jc: 0.5-2.9 mA/µA2
IcRn: 1.1-1.3 mV
Olaya et al., Appl. Phys. Lett. 2023
Tolpygo et al., IEEE Trans. Appl. Superconduct. 2023
Cyberey et al. IEEE Trans. Appl. Supercond.2024

## Slide 20: MIM Capacitor Fabrication
20
Base Patterning
Via Etch and Fill
Top Patterning
Stack Deposition
JJ Etch
NbTiN
HZO
HM SiN
HM SiOx
Thermal SiOx
ALD SiOx
Si substrate
Encapsulation SiN
New stack: NbTiN/HZO/NbTiN
Litho: 193i (195nm CD)
Process: PVD (NbTiN), ALD (HZO) & etch
Devices with diameters of 195-600 nm
CD control of <2% across the 300 mm wafer
Clean interfaces between different layers.
Uniform distribution of Nb, Ti, and N in the electrodes

## Slide 21: Capacitors are Tunable at Cryogenic Temperature
Capacitance and ferroelectric properties are temperature independent between 3-15 K
Leakage current at 2.6K is 2 orders of magnitude lower than at 300K
Cf: 3 µF/cm2 @RT, 2.9 µF/cm2 @4.2K
Tunability: 10% @RT, 5% @4.2K
RT
Cryo
spec
49000 caps
Tunability ~5%
Symmetric CV
Coercive Voltage = 1V
Saturation = 2V
49000 caps
S. Ibrahim et al.,
Arxiv 2025

## Slide 22: Conclusions and outlook
NbTiN based 3ML wires and vias, 2ML αSi JJs and 2ML HZO MiMCaps meet specifications for SCD circuits targeting 0.4BJJ/cm2.
These properties and processing temperature budget of 420 oC open a path for fabrication of SCD circuits compatible with current 300mm CMOS technology.
Continuous improvement of performance through
      Better process control
      New integration schemes
      Material engineering
      Pushing scaling limits
      Failure Mode analysis
Incrementally develop processes to 7 ML
Technology Transfer to foundries for full stack (16 ML) fabrication