## Slide 1: Nb3Sn coating on Cu via CVD
Shreyas Balachandran
Department of Mechanical Engineering, FAMU- FSU College of Engineering, Tallahassee, FL.
Acknowledgement: The work was performed under the DOE- ACCELERATE program, and DOE grant- DE-SC0026206. Additional support for the National High Magnetic Field Laboratory facilities is from the NSF: NSF-DMR-2128556, and the State of Florida. This work is authored by Jefferson Science Associates, LLC, under U.S. DOE Contract No. DE-AC05-06OR23177.
Collaborators and work presented on behalf of colleagues at Ultramet, Jefferson Lab, and FSU

## Slide 2
Beyond SRF Nb- Alternative materials: Focus on Nb3Sn
4W
at ~4 K
Posen, S., Lee, J., Seidman, D. N., Romanenko, A., Tennis, B., Melnychuk, O. S., & Sergatskov, D. A. (2021). Advances in Nb3Sn superconducting radiofrequency cavities towards first practical accelerator applications. Superconductor Science and Technology, 34(2), 025007.

## Slide 3: Cryocooled Nb3Sn on Nb successfully tested in Jefferson Lab- 1MW, 1MeV compact electron accelerator possible.
10 MeV, 1 MW system in the works!

## Slide 4: Nb3Sn on Cu for SRF applications
Cu melts at ~1100°C.
Cu-based Nb3Sn is a widely studied system.
Cost of RRR 100 Cu ~ 1/20 of RRR 300 Nb
Cu
Nb3Sn
~ 5 times improvement in thermal conductivity at 4K with Cu
Cu
Nb3Sn
Nb
Current
Proposed

## Slide 5: CVD Nb3Sn by Nb and Sn chloride reactions
Deposition temperature is 700℃
Ribbon or wire heated to ~1000 ℃
December 1970, RCA Reviews
Nb: Sn vapor ratio control is important

## Slide 6: Ultramet, Inc deposited Nb3Sn on Cu cavities at temperatures of 750℃ - 900℃
Cu
Nb3Sn (75:25)
Cu
Ta
Nb3Sn (77-78:23-22)
Nb
Nb3Sn (75:25)
50 µm
50 µm
50 µm
Precursors are largely proprietary.
Process details are unknown.

## Slide 7: High Tc, Nb3Sn is possible in the temperature range of 750- 900℃.
Cavity performance needs to improvement

## Slide 8: Issues beyond obtaining high-quality CVD Nb3Sn need to be addressed for success in SRF applications.

## Slide 9: Cu in Nb3Sn {grain boundaries}
Degradation of performance due to Cu in GB’s.
Cu Diffusion barriers are important

## Slide 10: Thermal strains: Coefficient of thermal expansion.
Cu: 17 x 10-6/℃
Nb3Sn: 7.6 x 10-6/℃
Nb/ Ta: ~8 x 10-6/℃
Thermal expansion mismatch:

## Slide 11: Surface roughness: Substrate + growth
Nb3Sn
Ta / Nb
Cu
Nb3Sn
Ta / Nb
Grain sizes are µm in size
Polishing processes for Nb3Sn

## Slide 12
Structural stability of Cu structures after heat treatments

## Slide 13: RD&D at Jefferson Lab to weld Inconel 625 to Cu
Element | Weight percent
Chromium | 22.0
Molybdenum | 9
Niobium + Tantalum | 1.2
Iron | 1.8
Aluminum | 0.3
Titanium | 0.26
Silicon | 0.16
Manganese | 0.3
Carbon | 0.04
Sulphur + Phosphorus | <0.005
Nickel | Bal.
Cu- C10100, off the shelf- 3.1 mm sheet
Inconel 625- 3.1mm sheet and 1 in. plate
Sample ID | Weld speed (mm/s) | Beam Offset (mm) | Energy per unit length (W/mm)
O1-C | 6.8 | 0.4 | 328
O2-C | 6.8 | 0.6 | 328
O3-C | 6.8 | 0.9 | 328
O4-C | 6.8 | 1.1 | 328
V1-C | 7.6 | 1.0 | 328
V2-C | 6.8 | 1.0 | 369
V3-C | 5.9 | 1.0 | 422
V4-C | 5.1 | 1.0 | 492
O7-I | 7.2 | 0.4 | 328
O8-I | 7.2 | 1.0 | 328
Welding parameters for 3mm thick sheets of Cu and Inconel 625. Beam current = 50 mA, beam Voltage = 50 kV, and oscillation diameter of 2mm, 10 kHz.
Beam
Offset
In Cu
In A-625

## Slide 14: EB welds Cu to Inconel 625. Offset in Cu NOT in Inconel
0.4 mm
0.6 mm
0.9 mm
1.1 mm
V= 7.6 mm/s
V= 6.8 mm/s
V= 5.9 mm/s
V= 5.1 mm/s
O = 1 mm
Cu
Alloy 625
Cu
Alloy 625
Offset in Cu, v = 6.8 mm/s
Varying speed, Offset in Cu = 1mm
Offset in Inconel 625, v = 6.8 mm/s
1.0 mm
0.4 mm
3 mm

## Slide 15
Inconel Flange welded to Cu tube

## Slide 16: Cu- Inconel welds maintain high strength after welding.

## Slide 17: And continue to maintain higher strength after heating to 950℃ for 3 hours.

## Slide 18: Mechanical testing: Fracture in Cu (weakest spot)
Offset in Cu 1mm
Offset in Cu 0.4 mm

## Slide 19: So what?
Inconel 625 could be further explored for vacuum flanges.
  Weakly paramagnetic at 4K. Susceptibility of 1.01- 1.03
How about using Inconel 625 for structural support as needed?
EBW of Cu- Inconel 625 is straightforward.
Applications in a CVD (hot chloride) environment need to be evaluated.

## Slide 20: CVD Nb3Sn on Cu is possible BUT needs significant developments in the following areas
Process standardization for Cu cavity preparation.
  Polishing method, Metric: Surface roughness?
Nb3Sn deposition on Cu
  Process control to obtain a stoichiometric superconductor with desired smoothness.
  Post processing: No post processing is best…
    Heat treatment?
  Thickness control- Address cavity shape
  Developing Nb3Sn polishing strategies to remove layers controllably- new electro/ chemical/ mechanical polishing recipes?
Dealing with soft Cu structures
  Reinforcements
  Support structures, flanges etc.