## Slide 1: Experience with the Cornell Conduction-Cooled Nb3Sn Cryomodule (C4M)
With lessons learned
November 13, 2025
Neil Stilin
Notes: Tip: Keep titles under 60 characters for readability
To change the photo: Right-click on photo and select change photo

## Slide 2: Outline
Brief Motivation & System Design
Cavity Fabrication & Testing
Cryomodule Assembly & First Results
Lessons Learned
Notes: Use for: Introducing new topics
To change the photo: Right-click on photo and select change photo

## Slide 3: Brief Motivation
Applications for small-scale operations:
Energy and environment
  Sterilizing waste water, sludge, medical waste
  Flue gas treatment
  Remediation of contaminated soil
  Asphalt treatments (durability)
Medicine
  Radioisotope production
Security & defense
  Cargo inspection
Industry
  Producing biofuel
  Curing carbon fiber composites
… and many more!
U.S. DOE Report, “Accelerators for America’s Future”
U.S. DOE Report, “Workshop on Energy and Environmental Applications of Accelerators”
Typical beam parameters
Moderate Energy: 1 – 10 MeV
High Current: ≥ 100 mA
High Avg. Power: ≥ 1 MW
High average current & power can be better obtained with superconducting cavities
Continuous-wave (CW) operation enables higher throughput
Decontamination cross section for a 10 MeV beam into a high-clay-content 5% contaminated soil
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 4: System Design
Energy Gain | 1 MeV
Beam Current | 100 mA
Average Power | 100 kW
Finalized Cavity
Single-cell 1.3 GHz Nb3Sn cavity
​Nb rings at cavity equator (2) and near cavity irises (2)
​​1 PT420 + 1 PT425 cryocoolers (Cryomech)
  Total capacity: 4.15 W at 4.2 K; 100 W at 45 K
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 5: Simulation Results
4.6 K
Cold head: 4.2 K
Small thermal gradients across cavity & cold heads
Low-power (no coupler) heat loads:
  18.6 W at 1st stage (45 K)
  1.9 W at 2nd stage (4 K)
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 6: Cavity Fabrication & Testing
Notes: Use for: Introducing new topics
To change the photo: Right-click on photo and select change photo

## Slide 7: Electron-beam Welding
Careful planning required for complicated shape
Beam parameters optimized for different weld types
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 8: Cavity Treatment & Coating
Defects uncovered during chemical workup
Tin furnace interlock failure: interrupted coating
Witness sample images still look typical
Actual
Planned
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 9: Cavity Test Results
Nb baseline: typical performance (no special treatments), ran into two multipacting bands
Nb3Sn baseline: good low-field Q0, strong Q-slope
Sufficient for low-power testing in cryomodule; long-term performance could be improved
Nb
Nb3Sn
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 10: Cryomodule Assembly & First Results
Notes: Use for: Introducing new topics
To change the photo: Right-click on photo and select change photo

## Slide 11: Beamline Assembly
Partial top-down assembly method
Simplifies structure but requires more parts in cleanroom
Tight connections
Cavity Suspended from Frame
Lowering into Vacuum Vessel
Final Seals & Support Connections
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 12: 2nd Stage (4 K) Assembly
5N-purity Aluminum split rings & mounting plates
OFHC braided thermal straps for flexible connection
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 13: 1st Stage (45 K) Assembly
1100 Aluminum mounting plate with pass-through extensions
Final connections made after cryocoolers & vessel lid attached
2nd stage
1st stage
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 14: Cryomodule Cooldown
Cooldown completed in < 20 hrs
Ambient magnetic field at cavity ≈ 10 mG
Beam Tubes
4 K Stage
45 K Stage
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 15: First Low-Power RF Results
Nb3Sn performance dependent on ∆Tcavity at SC transition
Basic system cooldown: ∆Tcavity = 890 mK
Fast controlled cooldown: ∆Tcavity = 140 mK
Thermal intercept rings
PT425
PT420
Key Result: RF performance matches baseline test after thermal cycling!
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 16: Cavity Temperatures
Baseline (RF off) Tcav ≈ 3.6 K
With Pdiss = 1 W, Tcav ≈ 4.4 K
Small ∆T across cavity indicates even, effective cooling
Estimated heat loads within expected range
Key Result: Cavity temperatures and heat loads match predictions!
 | SR 1 | SR 2 | SR 3 | SR 4 | BT | Coldhead
Baseline | 3.85 K | 3.52 K | 3.54 K | 3.67 K | ~5.05 K | 3.46 K
1 W Diss. | 4.45 K | 4.35 K | 4.38 K | 4.33 K | ~6.41 K | 4.05 K
1.5W Sim | 4.36 K | 4.37 K | 4.37 K | 4.36 K | ~4.6 K | 4.2 K
BT
SR 1-4
 | Static Heat Load | Predicted (No coupler)
4 K | < 2.0 W | ~ 1.9 W
45 K | < 20 W | ~ 18.6 W
1
2
3
4
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 17: Lessons Learned
Notes: Use for: Introducing new topics
To change the photo: Right-click on photo and select change photo

## Slide 18: Lessons Learned
Consolidate / centralize records of design choice rationale, not just end results
  Especially important when project leadership is passed on
Examine practical assembly concerns early in design process
  Spatial restraints on hardware, tools, arms / hands, etc.
  Bare minimum room for tools does not guarantee practical use
Develop more standardized procedure for temperature cycling with cryocoolers
  Using heater control can achieve smaller gradients vs basic cryocooler “off-on” method
Use only Lakeshore CD/CU Cernox sensors rather than SD Cernox
  SD Cernox sensor readings become unreliable in dry (e.g. conduction-cooled) environments
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 19: QUESTIONS?
Notes: Before sharing your presentation, confirm:
Fonts are consistent
Images meet quality standards
Charts use template colors
Footer information is current
Spell check completed
Links are working
File size is optimized

## Slide 20: Extra – Interference on 4 K Mounts
Some thermal strap connections interfere with cold head connections
Cold head
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo

## Slide 21: Extra – Thermal Shield Simulation
Semi-combined thermal simulation to compare temperature and heat load results
Notes: Guidelines: 6-8 bullets per slide; Use sentence fragments for bullets
To change the photo: Right-click on photo and select change photo