## Slide 1
Irradiated Ammonia for Polarized Solid Targets
Chris Keith
JLab Target Group

## Slide 2
Irradiated ammonia: a brief history
Behavior of irradiated ammonia
Radicals in ammonia
Summary, conjectures, and questions
Outline

## Slide 3
1979: Niinikoski and Rieubland [CERN] irradiate NH3 with a low dose of protons at 77 K. Reaches 90+% at 2.5 T and 0.3 K.
Chronology of irradiated ammonia
1980: Meyer et al. [Bonn] irradiate NH3 and ND3 with high dose of electrons at 87 K. Reaches 60% (NH3) and 16% (ND3) and 2.5 T and 0.5 K.
1980: Seely et al. [SLAC] irradiate NH3 and ND3 with a low dose of 20 GeV electrons at 1 K.
Reaches 75% (NH3) and 25% (ND3) at 5 T and 1 K.
1990: Crabb et al. [Michigan] irradiate NH3 with 10 GeV electrons at 87 K. Reaches 95% at 5 T and 1 K.
Tapio Niiniikoski
Werner Meyer
Mike Seely
Don Crabb

## Slide 4
It turns purple
Behavior of irradiated ammonia
Alexander Berlin, PhD thesis, Bochum University (2015)
One week
Two weeks
Four years
At 77 K the color slowly fades over time (not so for ND3).
The polarizability remains (albeit slower).
Spin relaxation also slows.
→ Color centers are not essential for dynamic polarization.
A single exponential can describe the spin-up curve.
Two spin-lattice times are required for the relaxation curve. This is especially true for freshly-irradiated materials.
Alexander Berlin, PhD thesis, Bochum University (2015)
NH3

## Slide 5
Behavior of irradiated ammonia
Radiation damage to NH3 can be repaired multiple times by annealing the sample, up to a practical end of life of about 20 Pe- cm-2
The polarization of ND3 benefits significantly from a “cold dose” at 1 K.
It is up to 4x more radiation resistant than NH3.

## Slide 6
In NH3 at 1K/5T the optimum frequencies are initially about 300 MHz apart and separate to 450 MHz with cold dose
Behavior of irradiated ammonia
300 MHz
(10 mT)
James Maxwell, PhD thesis,
University of Virginia (2010)
450 MHz
(16 mT)
Alexander Berlin, PhD thesis, Bochum University (2015)
The frequency separation (warm dose only) is about the same at 2.5 T
Mike Seely, PhD thesis, Yale University (1992)
0.16 kG
(450 MHz)
Cold dose only
5 x 1015 e-/cm2
330 MHz

## Slide 7
Behavior of deuterated ammonia
Mike Seely, PhD thesis, Yale University (1992)
0.11 kG
(310 MHz)
3.8 x 1015 e-/cm2
W. Meyer, NIM A 526 (2004) 12
Warm dose
130 MHz
(5 mT)
Cold dose
330 MHz
(12 mT)
250 MHz
P.M. McKee, NIM A 526 (2004) 60
400 MHz

## Slide 8
SE: 10 TM: 1.6
SE: 19 TM: 5
SE: 14 TM: 30
SE: 2 TM: 110
1H enhancement factors at 7 T and 20 K in DMSO*/water + trityl-OX063 due to the Solid Effect and Thermal Mixing
Equbal et al, J. Phys. Chem. Lett (2020) 3718
*dimethyl sulfoxide
A transition from the SE to TM with increasing concentration of trityl OX063
10 mmol
100 mmol

## Slide 9
Behavior of deuterated ammonia
Courtesy of James Maxwell
150 MHz
330 MHz
Run Group C
Protons follow the usual script
250 MHz
450 MHz
Run Group C
Deuteron data is inconclusive

## Slide 10
The ammonia molecule
N
H
H
H
2sp3
2sp3
2sp3
2sp3
1s
2s
2p
N
1s
H
1s
H
1s
H
1s
Physicist’s model (incorrect!)
Hydrogen bonds with nitrogen’s 2p electrons
Chemist’s model
Hydrogen & Nitrogen bond via four 2sp3 hybrid orbitals
Spin up
Spin down
1s
1s
1s

## Slide 11
EPR studies at 0.33 T (X-band) and 2.5 T (V-band) have found that the dominate species produced by radiation at 87 K is the amine radical •NH2 (or •ND2)
M. Symons, 2nd Pol. Target Materials Workshop (1979)
“At 77 K only •NH2 radicals are obtained.”
NH3 → •NH3+ + e-
•NH3+ + NH3 → •NH2 + NH4+
NH4+ + e- → NH3 + •H
NH3 + •H → •NH2 + H2
Radicals in irradiated ammonia
N
H
H
2sp3
2sp3
2sp3
1s
Spin up
Spin down
2p
Amine radical •NH2 2B1 configuration
1s
1s

## Slide 12
•NH2 radical trapped in solid Argon matrix at 7.7 K
E.Y. Misochko et al, Low Temp. Phys. 26, 727–735 (2000)
The hyperfine interaction with the Nitrogen and Hydrogen nuclei produces
(2nNIN+1) (2nHIH+1) = 3 x 3 = 9 lines
The HFS width is about 9 mT (250 MHz),
independent of the field
Hyperfine splitting:
Radicals in irradiated ammonia
N
H
H

## Slide 13
•NH2 radical in warm-irradiated NH3
Dipolar Broadening:
Alexander Berlin, PSTP2011, St. Petersburg
Dipolar broadening increases the width by about 50%, independent of field.
Radicals in irradiated ammonia
N
H
H

## Slide 14
•NH2 radical at 2.5 T
g-factor anisotropy
Jorg Heckmann PhD Thesis, Bochum (2004)
g-factor anisotropy increases the width by about 20%, proportional to the field.
Radicals in irradiated ammonia
N
H
H

## Slide 15
•NH2 radical at 2.5 T
g-factor anisotropy
Jorg Heckmann PhD Thesis, Bochum (2004)
Radicals in irradiated ammonia
Integrated line shape
Microwave frequencies for warm and cold irradiation
N
H
H

## Slide 16
•NH2 radical in fresh,
warm-irradiated NH3
Alexander Berlin, PSTP2011, St. Petersburg
•NH2 radical 16-year-old
warm-irradiated NH3
Is the color center missing?
Alexander Berlin, PSTP2011, St. Petersburg
Radicals in irradiated ammonia
N
H
H

## Slide 17
Other radicals have been observed at 77 K, such as
  atomic hydrogen
  atomic deuterium
  atomic nitrogen-14
  atomic nitrogen-15
  “hydrazine radical?”
L.G. DeMarco, A.S. Brill, and D.G. Crabb
J. Chem. Phys 108 (1998) 1423
Also J. Heckmann & A. Berlin (Bochum)
-
1s
1s
Radicals in irradiated ammonia
H
D
1s
2s
2p
N

## Slide 18
Radicals in irradiated ammonia
•NH2 and •H radicals in warm irradiated NH3
Jorg Heckmann, PhD thesis, Bochum (2004)
-
•H
•H
  Atomic hydrogen
The HFS of hydrogen is about 50 mT (1.4 GHz), far outside our microwave scan
❌ DNP
✔️ Spin-relaxation
It decays about 30 K warmer than •NH2
Symons: NH3 + •H → •NH2 + H2 ??

## Slide 19
Atomic deuterium
HFS is much smaller than 1H,
about 15 mT, low-to-high
Radicals in irradiated ammonia
Demarco: “… the free radicals (•ND2) decay at a higher temperature than do the D atoms.”
•D
•D
Microwave freq.
warm & cold doses
x-band spectra of irradiated ND3 at 100 K
Alexander Berlin, PhD thesis, Bochum (2015)

## Slide 20
Radicals in irradiated ammonia
By 130 K, the •ND2 radicals have completely disappeared, leaving resonance lines from one or more unidentified species.
•14N
7 mT separation
“Hydrazine radical”?
HFS in 14N is narrower still, 1 mT
x-band spectra of irradiated ND3 at 130 K
Alexander Berlin, PhD thesis, Bochum (2015)

## Slide 21
Summary, Conjectures, Questions
When ammonia is irradiated at 87 K, the dominant species are •NH2 and •ND2
The principle broadening mechanisms are the hyperfine and dipolar interactions
Other radicals are produced, each with a different activation temperature
Atomic hydrogen •H is probably the main source of radiation damage in NH3
Atomic deuterium •D is not as damaging and may improve the polarization of ND3
What is the “cold dose”?
Does it have to be cold?
How cold?
How long does it last at 77 K?
Can we perform in situ monitoring at 1 K?

## Slide 22
Decay of H-atom resonance at 102 K.
Solid line: First-order fit
Dotted line: Second-order fit
L. DeMarco et al, J. Chem. Phys., Vol. 108, No. 4, 22 January 1998