## Slide 1: Cool-down Studies in Horizontally Cooled Cavity
M. Martinello, A. Romanenko, M. Checchin, A. Grassellino
TTC Meeting - 04/23/2015

## Slide 2: Outline
Cool-down Dynamics via T-map:
Introduction
Fast Cool-downs T-map
Slow Cool-down T-map
2. Geometrical consequences of trap flux:
Vertical vs Horizontal configuration
Axial vs Orthogonal field in horizontal configuration
Temperature rising on top:
  Axial vs Orthogonal Field
  Fast vs Slow Cool-down
Conclusions

## Slide 3: 1. Cool-down Dynamics via T-map

## Slide 4: Introduction
A. Romanenko, A. Grassellino et al. J. Appl. Phys. 115, 184903 (2014)
Fast cool-down gives higher Q0
2 predicted mechanism:
  1. High thermo-gradient helps magnetic field expulsion
  2. Slow cool-down has different SC nucleation regime

## Slide 5: Introduction
High thermal gradient provides depinning force allowing efficient magnetic field expulsion
Ultra-high Q0 even in 190mG
A. Romanenko, A. Grassellino et al. J. Appl. Phys. 115, 184903 (2014)
A. Romanenko, A. Grassellino et al. Appl. Phys. Lett. 105, 234103 (2014)
  1. High thermo-gradient helps magnetic field expulsion

## Slide 6: Introduction
Fast cool-down: sharp transition between NC and SC phases
Slow cool-down:
          NC zones encircled by SC area
          Magnetic field not energetically favorable to escape
A. Romanenko, A. Grassellino et al. J. Appl. Phys. 115, 184903 (2014)
  2. Slow cool-down has different SC nucleation regime

## Slide 7: T-map apparatus
Cornell-based T-map system
36 boards with 16 thermometers each
576 thermometers
all around the cavity

## Slide 8: T-map apparatus
Thermometers calibrated from 2K to 100K during a warm-up

## Slide 9: T-map images
EQUATOR
IRIS L
IRIS R
EQUATOR
IRIS L
IRIS R
SC REGION
TOP
13
BOTTOM
31
BOARD #13
BOARD #31
BOARDS #22,4
Top
Mid
Bottom
NC REGION

## Slide 10: Fast Cool-down T-map
Starting T: 250K

## Slide 11
Fast Cool-down From 250K

## Slide 12
Fast Cool-down From 250K

## Slide 13
Fast Cool-down From 250K

## Slide 14
Fast Cool-down From 250K

## Slide 15
Fast Cool-down From 250K

## Slide 16
Fast Cool-down From 250K

## Slide 17
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 18
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 19
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 20
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 21
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 22
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 23
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 24
Fast Cool-down From 250K
NC zones encircle by SC material

## Slide 25
Fast Cool-down From 250K
NC zone encircle by SC material

## Slide 26
Fast Cool-down From 250K

## Slide 27: Fast Cool-down T-map
Starting T: 50K

## Slide 28: Fast Cool-down From 50K

## Slide 29
Fast Cool-down From 250K

## Slide 30
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 31
Fast Cool-down From 250K
Sharp NC-SC transition interface

## Slide 32
Fast Cool-down From 250K

## Slide 33
Fast Cool-down From 250K
NC zones encircle by SC material

## Slide 34
Fast Cool-down From 250K

## Slide 35: Slow Cool-down T-map
Starting T: 12K

## Slide 36: Slow Cool-down From 12K

## Slide 37
Slow Cool-down From 12K

## Slide 38
Slow Cool-down From 12K

## Slide 39
Slow Cool-down From 12K

## Slide 40
Slow Cool-down From 12K

## Slide 41
Slow Cool-down From 12K

## Slide 42
Slow Cool-down From 12K

## Slide 43
Slow Cool-down From 12K

## Slide 44
Slow Cool-down From 12K

## Slide 45
Slow Cool-down From 12K

## Slide 46
Slow Cool-down From 12K

## Slide 47
Slow Cool-down From 12K

## Slide 48
Slow Cool-down From 12K

## Slide 49
Slow Cool-down From 12K

## Slide 50
Slow Cool-down From 12K

## Slide 51
Slow Cool-down From 12K

## Slide 52
Slow Cool-down From 12K

## Slide 53
Slow Cool-down From 12K

## Slide 54
Slow Cool-down From 12K

## Slide 55
Slow Cool-down From 12K

## Slide 56
Slow Cool-down From 12K

## Slide 57
Slow Cool-down From 12K

## Slide 58
Slow Cool-down From 12K

## Slide 59
Slow Cool-down From 12K

## Slide 60
Slow Cool-down From 12K

## Slide 61
Slow Cool-down From 12K

## Slide 62
Slow Cool-down From 12K

## Slide 63
Slow Cool-down From 12K

## Slide 64
Slow Cool-down From 12K

## Slide 65
Slow Cool-down From 12K

## Slide 66
Slow Cool-down From 12K

## Slide 67: RF Test Results
Fast cool-down shows lower surface resistance:
sharp NC-SC transition
better magnetic field expulsion

## Slide 68: Summary
Cool-down dynamics:
Fast cool down shows sharp NC-SC interface
  Only at the end it shows island of NC-SC phases
Slow cool down shows broad NC-SC interface
  NC randomly distributed island surrounded by SC phase

## Slide 69: 2. Geometrical implications on flux trapping and on residual losses due to trapped flux

## Slide 70: Geometrical Considerations
Gaseous
Helium
Cooling direction
9.25K
9.25K
9.25K
9.25K
Horizontal configuration:
The cavity equator does not pass through transition at the same time
Higher probability to trap flux at the equator because thermogradients are not constant
Gaseous
Helium
Cooling direction
9.25K
9.25K
9.25K
9.25K

## Slide 71: SC-NC interface dynamics
Thermo-gradients change during the cool-down dynamics
At the end of the transition thermo-gradients decrease because of thermalization (as seen from T-map)
Bottom to top thermogradients are not a sufficient indicator of an efficient cooldown!
What matters is thermo-gradient along the NC-SC interface

## Slide 72: More Geometrical Considerations – field orientation
flux-hole
Gaseous
Helium
Cooling direction
9.25K
Orthogonal magnetic field concentrated on top during the cool-down can not be expelled ()
→ flux-hole on top on the cavity equator
Axial magnetic field concentrated on top can be expelled with fast cool-down
Orthogonal
Axial

## Slide 73: Instrumentation 1st experiment
2 Helmholtz Coils (orthogonal and axial field)
4 Thermometers (bottom, mid, mid-top and top positions)
4 Fluxgates (orthogonal and axial field mid and top positions)

## Slide 74: RF Test Result – Cool-downs in 10mG
Temperature rising on top only with orthogonal field applied

## Slide 75: RF Test Result – Cool-downs in 10mG
No heating on-top when magnetic field is fully trapped

## Slide 76: Instrumentation 2nd experiment
2 Helmholtz Coils (orthogonal and axial field)
4 Thermometers (bottom, mid, mid-top and top positions)
4 Fluxgates (orthogonal and axial field mid and top positions)
T-map

## Slide 77: Fast vs Slow 16 MV/m
Fast Cool-down – Orth field
Slow Cool-down – Orth field

## Slide 78: Fast vs Slow 21 MV/m
Fast Cool-down – Orth field
Slow Cool-down – Orth field

## Slide 79: Fast vs Slow 26 MV/m
Fast Cool-down – Orth field
Slow Cool-down – Orth field

## Slide 80: Orthogonal vs Axial 16 MV/m
Orthogonal field – Fast Cool-down
Axial field – Fast Cool-down

## Slide 81: Orthogonal vs Axial 21 MV/m
Orthogonal field – Fast Cool-down
Axial field – Fast Cool-down

## Slide 82: Orthogonal vs Axial MV/m
Orthogonal field – Fast Cool-down
Axial field – Fast Cool-down

## Slide 83: RF Test Results
Heating on-top with fast cool down and orthogonal magnetic field
Same performance axial and orthogonal field

## Slide 84: Summary
Horizontal cooling effects:
  Orthogonal magnetic field: for the first time, heating on top due to trapped flux concentration is observed
  Fast cooling in orthogonal field creates flux concentration, while slow cooling distributes flux all along, what is better? Higher Q is always achieved with fast. But if too much flux is concentrated at the top, quench may degrade. It is a balance, dependent upon ambient fields.
  Axial magnetic field: efficiency of magnetic flux expulsion depends on cool-down dynamics, but all flux can be expelled

## Slide 85: Conclusion
Horizontal configuration is more complicated than vertical because thermo-gradients change along the equator
Slow cool-down
  trapped flux randomly into whole cavity
Fast cool-down
  better flux expulsion
  residual flux trapped on top (only orthogonal component)
Orthogonal component is worst than axial
  the heating effect can be relevant in case of high amount of field trapped

## Slide 86: References
A. Romanenko, A. Grassellino et al. J. Appl. Phys. 115, 184903 (2014)
A. Romanenko, A. Grassellino et al. Appl. Phys. Lett. 105, 234103 (2014)
M. Martinello, M. Checchin, A. Grassellino et al. arXiv:1502.07291v3 (2015)
M. Martinello, A. Romanenko, M. Checchin et al. arXiv:1504.04441v2 (2015)
A. Romanenko, FCC conference (2015)
A. Grassellino, LCLS-II meeting (2015)